# Patent Landscape Report: Hydrogenated NBR Synthesis, Degradation, and Post-Treatment Technologies

## 1. Abstract

This report synthesizes nine patents relevant to hydrogenated nitrile butadiene rubber (HNBR), with emphasis on routes that create, modify, or purify hydrogenated NBR materials. The target material is defined as nitrile rubber derived from conjugated dienes and α,β-unsaturated nitriles that has been partially to highly hydrogenated to reduce residual unsaturation and improve heat, ozone, oil, and aging resistance. Across the patent set, two major technology directions emerge. First, several patents focus on controlled molecular-weight reduction of NBR prior to hydrogenation by olefin metathesis using ruthenium catalysts, co-olefins such as ethylene or 1-hexene, and solution-phase processing in monochlorobenzene. These routes aim to produce lower-Mooney, narrower-distribution HNBR suitable for seals, hoses, and other molded articles. Second, other patents address formulation and post-processing of HNBR, including partially hydrogenated NBR blended with silicone rubber, peroxide-cured HNBR compositions containing microgels and unsaturated carboxylic acids, and catalyst-residue removal using functionalized ion-exchange resins. A separate catalyst-system patent shows that alkaline-earth metal chlorides can accelerate metathesis of NBR, while another demonstrates that salt additives can strongly influence metathesis efficiency and molecular-weight reduction. The landscape also includes a metathesis-catalyst patent that explicitly claims modified NBR depolymerization and hydrogenation uses, underscoring the centrality of ruthenium carbene catalysts for HNBR precursor modification. Overall, the evidence points to solution metathesis as the dominant precursor-engineering strategy, with hydrogenation typically performed using Wilkinson-type Rh catalysts or related homogeneous systems. Process trends include high-temperature solution reactions, inert-atmosphere handling, catalyst loading optimization, and downstream purification to reduce residual Ru. Formulation trends emphasize balancing low-temperature flexibility, compression set, and high-temperature durability through selective hydrogenation level control and reinforcing or compatibilizing additives.

## 2. Primary Patent Evidence

### Patent 1: US7919563B2 — Low molecular weight hydrogenated nitrile rubber

| Patent Number | US7919563B2 |
| --- | --- |
| Title | Low molecular weight hydrogenated nitrile rubber |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2011 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: This patent discloses a two-step route in which nitrile rubber is first subjected to olefin metathesis in solution to reduce molecular weight, then hydrogenated to form low-molecular-weight HNBR. The metathesis uses ruthenium catalysts and co-olefins such as ethylene or 1-hexene in monochlorobenzene, followed by hydrogenation with Wilkinson's catalyst under high hydrogen pressure.

Cement concentration: 6 or 15% by weight — Examples 1-4

Agitator speed: 600 rpm — Examples 1-4

Solvent: monochlorobenzene — Examples 1-4

Substrate acrylonitrile content: 34 mol % — Examples 1-4

Substrate Mooney viscosity: 35 ML (1+4) @ 100 deg. C. — Examples 1-4

Ethylene pressure: 6.9×10^5 Pa — Examples 1-3

Nitrogen pressure: 100 psi — Example 4

Co-olefin concentration: 500 psi — Table 1

Reactor temperature: 80° C. — Table 1

Catalyst load: 0.05 phr — Table 1

Catalyst load: 0.10 phr — Table 1

Catalyst load: 0.25 phr — Table 1

Rubber mass: 200 g — Example 1

MCB mass: 1133 g — Example 1

Rubber mass: 75 g — Example 3

MCB mass: 1175 g — Example 3

1-hexene mass: 150 g — Example 4

Hydrogen pressure: 1200 psi — hydrogenation conditions

Hydrogenation temperature: 138° C. — hydrogenation conditions

Wilkinson's catalyst loading: 0.08 phr — hydrogenation conditions

Triphenylphosphine: 1 phr — hydrogenation conditions

Hydrogen degassing: 3 times with H2 (100 psi) — hydrogenation procedure

Hydrogenation preheat: 130° C. — hydrogenation procedure

Reaction monitoring: residual double bond (RDB) by IR spectroscopy — hydrogenation procedure

Mn: 27 kg/mol — typical product

Mw: 54 kg/mol — typical product

Starting polymer Mn: 85 kg/mol — typical product

Starting polymer Mw: 296 kg/mol — typical product

MWD/PDI: 3.4 to 2.0 — typical product comparison

PDI minimum: 1.90 — Table 2

Mooney viscosity: 73 to 3 — Table 2

#### Relevant Experimental Evidence

Example 1: 15 wt.-% cement was degassed with ethylene at 6.9×10^5 Pa before metathesis.

Example 2: 15 wt.-% cement was processed under the same ethylene degassing conditions as Example 1.

Example 3: 6 wt.-% cement was used, showing the lower-solids metathesis variant.

Example 4: 1-hexene was used as co-olefin instead of ethylene, demonstrating alternative chain-scission conditions.

Examples 1-4: metathesis followed by hydrogenation gave lower Mn/Mw and narrower PDI than the starting polymer.

#### Technical Relevance

This patent is directly relevant because it provides a controlled route to low-molecular-weight HNBR, a key target for improved processability. It also discloses practical hydrogenation conditions and shows how metathesis precursor engineering can tune final HNBR molecular weight and viscosity.

### Patent 2: US7772328B2 — Low molecular weight hydrogenated nitrile rubber

| Patent Number | US7772328B2 |
| --- | --- |
| Title | Low molecular weight hydrogenated nitrile rubber |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2010 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: This patent also teaches a two-step process in which nitrile rubber is first degraded by olefin metathesis in the presence of a ruthenium catalyst and a co-olefin, then hydrogenated to HNBR. The emphasis is on producing lower-molecular-weight, narrower-distribution HNBR and shaped articles from it.

Cement concentration: 6 or 15% by weight — Examples 1-4

Agitator speed: 600 rpm — Examples 1-4

Solvent: monochlorobenzene — Examples 1-4

Substrate acrylonitrile content: 34 mol % — Examples 1-4

Substrate Mooney viscosity: 35 ML (1+4) @ 100 deg. C. — Examples 1-4

Ethylene pressure: 6.9×10^5 Pa — Examples 1-3

Nitrogen pressure: 100 psi — Example 4

Co-olefin concentration: 500 psi — Table 1

Reactor temperature: 80° C. — Table 1

Catalyst load: 0.05 phr — Table 1

Catalyst load: 0.10 phr — Table 1

Catalyst load: 0.25 phr — Table 1

Rubber mass: 200 g — Example 1

MCB mass: 1133 g — Example 1

Rubber mass: 75 g — Example 3

MCB mass: 1175 g — Example 3

1-hexene mass: 150 g — Example 4

Hydrogen pressure: 1200 psi — hydrogenation conditions

Hydrogenation temperature: 138° C. — hydrogenation conditions

Wilkinson's catalyst loading: 0.08 phr — hydrogenation conditions

Triphenylphosphine: 1 phr — hydrogenation conditions

Hydrogen degassing: 3 times with H2 (100 psi) — hydrogenation procedure

Hydrogenation preheat: 130° C. — hydrogenation procedure

Reaction monitoring: residual double bond (RDB) by IR spectroscopy — hydrogenation procedure

Mn: 27 kg/mol — typical product

Mw: 54 kg/mol — typical product

Starting polymer Mn: 85 kg/mol — typical product

Starting polymer Mw: 296 kg/mol — typical product

MWD/PDI: 3.4 to 2.0 — typical product comparison

PDI minimum: 1.90 — Table 2

Mooney viscosity: 73 to 3 — Table 2

#### Relevant Experimental Evidence

Example 1: 15 wt.-% cement was degassed with ethylene at 6.9×10^5 Pa before metathesis.

Example 2: 15 wt.-% cement was processed under the same ethylene degassing conditions as Example 1.

Example 3: 6 wt.-% cement was used, showing the lower-solids metathesis variant.

Example 4: 1-hexene was used as co-olefin instead of ethylene, demonstrating alternative chain-scission conditions.

Examples 1-4: metathesis followed by hydrogenation gave lower Mn/Mw and narrower PDI than the starting polymer.

#### Technical Relevance

This patent is highly relevant because it discloses the same low-molecular-weight HNBR concept with explicit process and property data. It supports the use of metathesis plus hydrogenation to tailor HNBR viscosity and molecular-weight distribution for improved processing.

### Patent 3: EP2580260A1 — Blends of partially hydrogenated nitrile rubber and silicone rubber, …

| Patent Number | EP2580260A1 |
| --- | --- |
| Title | Blends of partially hydrogenated nitrile rubber and silicone rubber, … |
| Assignee | Not available from source |
| Jurisdiction | EP |
| Publication Year | 2013 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: This patent is not a synthesis of HNBR itself but a blend technology using partially hydrogenated nitrile rubber and vinyl-containing silicone rubber. The blend is prepared in the presence of a metathesis catalyst, with an emphasis on solvent-free or very low-solvent processing and improved vulcanizate properties.

Organic solvent content: at most 1200 ppm — claim 2

Organic solvent content: at most 500 ppm — claim 2

Organic solvent content: at most 100 ppm — claim 2

Compression set test compression: 25% — Examples 1.3/1.7 discussion

Compression set storage temperature: -30°C — Examples 1.3/1.7 discussion

Compression set storage temperature: 150°C — Examples 1.3/1.7 discussion

Compression set storage time: 70 h — Examples 1.3/1.7 discussion

Compression set storage time: 158 h — Examples 1.3/1.7 discussion

Compression set storage time: 168 h — Examples 1.3/1.7 discussion

#### Relevant Experimental Evidence

Examples 1.3, 1.5 and 1.7: inventive vulcanizates showed equal or higher stress values at 50% and 100% elongation than comparative examples.

Examples 1.3 and 1.7: lower compression set after -30°C/70 h and 150°C/168 h storage indicated improved low- and high-temperature performance.

The patent demonstrates metathesis-catalyzed blending of partially hydrogenated NBR with silicone rubber under low-solvent conditions.

#### Technical Relevance

This patent is relevant because it uses partially hydrogenated NBR as a key component in high-performance elastomer blends. It highlights how hydrogenation level and formulation strategy affect compression set and thermal durability, which are important end-use properties of HNBR.

### Patent 4: US9321910B2 — Microgel-containing vulcanizable composition based on hydrogenated nitrile …

| Patent Number | US9321910B2 |
| --- | --- |
| Title | Microgel-containing vulcanizable composition based on hydrogenated nitrile … |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2016 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: This patent discloses a vulcanizable HNBR composition containing hydrogenated nitrile rubber, peroxide, unsaturated carboxylic acid or salt, and microgels. The HNBR itself is prepared by hydrogenation of nitrile rubber, and the patent focuses on compounding and vulcanization behavior rather than the hydrogenation step.

Microgel polymerization temperature: 30° C. — microgel preparation

Microgel reaction temperature: 40° C. — microgel preparation

Microgel reaction temperature: 50° C. — microgel preparation

Polymerization conversion: >95% — microgel preparation

Diethylhydroxylamine: 23.5 g — microgel termination

Microgel A butadiene: 12608 g — Table 1

Microgel A styrene: 287 g — Table 1

Microgel A TMPTMA: 530 g — Table 1

Microgel A HEMA: 137 g — Table 1

Microgel A water: 250 g — Table 1

Microgel A initiation: 3805.5 g — Table 1

Microgel A activation: 0 g — Table 1

Microgel A termination: 172 g — Table 1

Microgel B butadiene: 13742 g — Table 1

Microgel B styrene: 251 g — Table 1

Microgel B TMPTMA: 125 g — Table 1

Microgel B HEMA: 137 g — Table 1

Microgel B water: 250 g — Table 1

Microgel B initiation: 2740.5 g — Table 1

Microgel B activation: 304.5 g — Table 1

Microgel B termination: 105 g — Table 1

Microgel A Tg: -75° C. — Table 2

Microgel B Tg: -65° C. — Table 2

Microgel A diameter d10: 43.5 nm — Table 2

Microgel A diameter dz: 50.9 nm — Table 2

Microgel A diameter d80: 55.7 nm — Table 2

Microgel A specific surface area: 127 m2/g — Table 2

Microgel A gel content: 91.7% by wt. — Table 2

Microgel A swelling index: 13.1 — Table 2

Microgel A OH number: 33 mg KOH/g polymer — Table 2

Microgel A acid number: 7.4 mg KOH/g polymer — Table 2

Microgel B diameter d10: 35.4 nm — Table 2

Microgel B diameter dz: 48.2 nm — Table 2

Microgel B diameter d80: 55.1 nm — Table 2

Microgel B specific surface area: 139 m2/g — Table 2

Microgel B gel content: 94.8% by wt. — Table 2

Microgel B swelling index: 7.4 — Table 2

Microgel B OH number: 37.8 mg KOH/g polymer — Table 2

Microgel B acid number: 8.6 mg KOH/g polymer — Table 2

HNBR acrylonitrile content: 34% by weight — Example 1

HNBR residual double bond content: 3.5% — Example 1

Mooney viscosity: 77 ML (1+4) @100° C. — Example 1 material description

Mooney viscosity: 40 ME — Table 4

Mooney relaxation: 6.7% — Table 4

Mooney viscosity: 37 ME — Table 4

Mooney relaxation: 6.9% — Table 4

Mooney viscosity: 32 ME — Table 4

Mooney relaxation: 7.4% — Table 4

Mooney viscosity: 39 ME — Table 4

Mooney relaxation: 6% — Table 4

Mooney viscosity: 42 ME — Table 4

Mooney relaxation: 7.4% — Table 4

Vulcanization temperature: 180° C. — Table 5

Vulcanization test method: ASTM D5289 — Table 5

Vulcanization pressure: 170 bar — vulcanization step

Vulcanization time: 9 min — vulcanization step

Compression set test compression: 25% — discussion

Compression set storage temperature: -30°C — discussion

Compression set storage temperature: 150°C — discussion

Compression set storage time: 70 h — discussion

Compression set storage time: 158 h — discussion

Compression set storage time: 168 h — discussion

#### Relevant Experimental Evidence

Preparation examples: microgels A and B were made by emulsion polymerization and characterized by Tg, size, gel content, and acid/OH numbers.

Examples 1-3: HNBR compositions without microgels were compared against inventive microgel-containing mixtures.

Examples 4-5: inventive mixtures showed comparable Mooney behavior and vulcanization performance while improving final properties.

The patent demonstrates that microgels can improve high-temperature mechanical performance and demolding behavior in HNBR vulcanizates.

#### Technical Relevance

This patent is relevant because it addresses formulation of hydrogenated NBR for high-temperature service, a major application area. It shows how microgels and peroxide/unsaturated-carboxylic-acid systems can improve the performance of HNBR-based vulcanizates without changing the base polymer chemistry.

### Patent 5: EP2519350B1 — Highly active metathesis catalysis selective for romp and rcm

| Patent Number | EP2519350B1 |
| --- | --- |
| Title | Highly active metathesis catalysis selective for romp and rcm |
| Assignee | Not available from source |
| Jurisdiction | EP |
| Publication Year | 2019 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: This patent discloses ruthenium metathesis catalysts and their use in metathesis reactions, including a method for making modified nitrile butadiene rubber by depolymerization. The examples mainly describe synthesis of Ru complexes, while the patent text explicitly extends the catalyst utility to NBR depolymerization and hydrogenation-related uses.

Ligand synthesis scale: 5.0 mmol — Examples 1-19

Ligand synthesis temperature: 85°C — Example 1

K2CO3: 1.5 eq — Example 1

2,4,6-Trivinyl-cyclotriboroxane pyridine complex: 0.5 eq — Example 1

Pd(PPh3)4: 2% — Example 1

Ru complex synthesis scale: 1.0 mmol — Example 1

Ru complex synthesis temperature: 20-25°C — Example 1

Ru complex reaction time: 30-60 min — Example 1

DCM: 15 mL — Example 1

Ligand 3a: 250 mg — Example 1

Ru precursor 1b: 860 mg, 1.0 mmol — Example 1

CuCl: 270 mg, 2.5 mmol, 2.5 eq — Example 1

Ligand 3b yield: 91% — Example 2

Ru complex 4b yield: 29% — Example 2

Ligand 3c yield: 54% — Example 3

Ru complex 4c yield: 5% — Example 3

Ligand 3d yield: 62% — Example 4

Ru complex 4d yield: 32% — Example 4

Ru complex 4e yield: 35% — Example 5

Ru complex 4f yield: 14% — Example 6

Ligand 3g yield: 56% — Example 7

Ru complex 4g yield: 8% — Example 7

Ligand 3h yield: 32% — Example 8

Ru complex 4h yield: 42% — Example 8

Ligand 3j yield: 93% — Example 9

Ru complex 4j yield: 48% — Example 9

Ligand 3k yield: 83% — Example 10

Ru complex 4k yield: 68% — Example 10

Ligand 3m yield: 49% — Example 11

Ru complex 4m yield: 52% — Example 11

Ligand 3n yield: 45% — Example 12

Ru complex 4n yield: 64% — Example 12

Ligand 3p yield: 67% — Example 13

Ru complex 4p yield: 26% — Example 13

Ligand 3q yield: 46% — Example 14

Ru complex 4q yield: 38% — Example 14

Ligand 3r yield: 44% — Example 15

Ru complex 4r yield: 14% — Example 15

Ligand 3s yield: 51% — Example 16

Ru complex 4s yield: 85% — Example 16

Ligand 3t yield: 38% — Example 17

Ru complex 4t yield: 23% — Example 17

Ligand 3u yield: 28% — Example 18

Ru complex 4u yield: 32% — Example 18

Ligand 3v yield: 81% — Example 19

Ru complex 4v yield: 10% — Example 19

NBR depolymerization temperature: 30-100°C — claims/description

NBR depolymerization with mixed catalysts: 30-100°C — description

#### Relevant Experimental Evidence

Examples 1-19: a series of Ru complexes were synthesized and characterized, establishing the catalyst platform.

The patent explicitly claims use of the catalysts for making modified NBR by depolymerization.

The disclosure also states use in hydrogenation of rubbers containing carbon-carbon double bonds, linking the catalyst family to HNBR-related processing.

#### Technical Relevance

This patent is relevant because it provides metathesis catalyst chemistry directly applicable to NBR modification before hydrogenation. It supports the broader HNBR synthesis toolbox by identifying catalyst structures and operating windows for depolymerization of nitrile rubber.

### Patent 6: US8957161B2 — Process for reacting chemical compounds in the presence of catalyst systems

| Patent Number | US8957161B2 |
| --- | --- |
| Title | Process for reacting chemical compounds in the presence of catalyst systems |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2015 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: This patent discloses metathetic degradation of nitrile rubber in chlorobenzene using ruthenium catalysts and salt additives, followed by analysis of molecular-weight reduction. The process is carried out at room temperature with 1-hexene as co-olefin, and the patent shows that salts can accelerate or alter the efficiency of NBR depolymerization.

Acrylonitrile content: 35% by weight — General method

Mooney viscosity: 34 Mooney units — General method

Residual moisture content: 1.8% by weight — General method

Mw: 240 000 g/mol — General method

Mn: 100 000 g/mol — General method

PDI: 2.4 — General method

Solvent mass: 293.3 g chlorobenzene — General method

NBR mass: 40 g — General method

1-hexene: 0.8 g (2 phr) — General method

Catalyst solution solvent: 20 g MCB — General method

Reaction temperature: room temperature — General method

Catalyst amount: 20 mg — Table 1

Catalyst loading: 0.05 phr — Table 1

Ru amount: 60 ppm — Table 1

LiBr amount: 2 phr — Trial 1.02

LiCl amount: 2 phr — Trial 1.03

LiI amount: 2 phr — Trial 1.04

CaCl2 amount: 0.01 phr — Trial 1.05

CaCl2 amount: 0.05 phr — Trial 1.06

CaCl2 amount: 0.1 phr — Trial 1.07

CaCl2 amount: 0.5 phr — Trial 1.09

CaCl2 amount: 1 phr — Trial 1.09

CaCl2 amount: 2 phr — Trial 1.10

CaCl2 amount: 5 phr — Trial 1.11

CaCl2 amount: 10 phr — Trial 1.12

Reaction time: 0, 30, 60, 90, 180, 420 min — Table 1/2

Mw: 186 832 to 53 852 kg/mol — Trial 1.01 over time

Mn: 60 000 to 29 314 kg/mol — Trial 1.01 over time

PDI: 3.1 to 1.8 — Trial 1.01 over time

Mw: 186 832 to 51 827 kg/mol — Trial 1.02 over time

Mn: 60 000 to 28 793 kg/mol — Trial 1.02 over time

PDI: 3.1 to 1.8 — Trial 1.02 over time

Mw: 186 832 to 21 337 kg/mol — Trial 1.03 over time

Mn: 60 000 to 13 153 kg/mol — Trial 1.03 over time

PDI: 3.1 to 1.6 — Trial 1.03 over time

Mw: 186 832 to 51 827 kg/mol — Trial 1.04 over time

Mn: 60 000 to 28 793 kg/mol — Trial 1.04 over time

PDI: 3.1 to 1.8 — Trial 1.04 over time

#### Relevant Experimental Evidence

Trials 1.01-1.04: compared Grubbs II alone with LiBr, LiCl, and LiI, showing salt-dependent changes in degradation efficiency.

Trials 1.05-1.12: CaCl2 was tested over a wide loading range, demonstrating the effect of alkaline-earth chloride on metathesis.

The data show that salt additives can strongly influence molecular-weight reduction of NBR, which is relevant to HNBR precursor engineering.

#### Technical Relevance

This patent is relevant because it directly addresses metathesis degradation of NBR, a precursor step for low-viscosity HNBR. It provides evidence that salt additives can tune catalyst activity and molecular-weight reduction, which is important for controlling final HNBR processability.

### Patent 7: US7737233B2 — Catalyst systems and their use for metathesis reactions

| Patent Number | US7737233B2 |
| --- | --- |
| Title | Catalyst systems and their use for metathesis reactions |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2010 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: This patent discloses catalyst systems for metathesis reactions that combine a metathesis catalyst with an alkaline earth metal chloride, especially calcium chloride or magnesium chloride. It is explicitly applicable to metathesis of nitrile rubber, supporting controlled depolymerization of NBR prior to hydrogenation.

Salt:catalyst ratio: 0.01:1 to 10000:1 — claim 1

Calcium chloride or magnesium chloride — claim 2

Catalyst amount: 20 mg — Table 2

Catalyst loading: 0.05 phr — Table 2

Grubbs II catalyst MW: 848.33 g/mol — examples

Hoveyda catalyst MW: 626.14 g/mol — examples

Grela catalyst MW: 617.13 g/mol — examples

Acrylonitrile content: 34% by weight — general method

Mooney viscosity: 31 Mooney units — general method

Residual moisture content: 1.2% by weight — general method

Mw: 186.832 g/mol — general method

Mn: 60000 g/mol — general method

PDI: 3.1 — general method

Solvent: 293.3 g chlorobenzene — general method

NBR mass: 40 g — general method

1-hexene: 0.8 g (2 phr) — general method

Reaction temperature: room temperature — general method

Catalyst solution solvent: 20 g MCB — general method

LiBr amount: 2 phr — comparative example

LiCl amount: 2 phr — comparative example

LiI amount: 2 phr — comparative example

CaCl2 amount: 0.01 phr — example 1.05

CaCl2 amount: 0.05 phr — example 1.06

CaCl2 amount: 0.1 phr — example 1.07

CaCl2 amount: 0.5 phr — example 1.09

CaCl2 amount: 1 phr — example 1.09

CaCl2 amount: 2 phr — example 1.10

CaCl2 amount: 5 phr — example 1.11

CaCl2 amount: 10 phr — example 1.12

#### Relevant Experimental Evidence

Comparative examples: LiBr, LiCl, and LiI were tested with Grubbs II catalyst.

Examples 1.05-1.12: CaCl2 was evaluated across 0.01 to 10 phr, showing the claimed salt-acceleration effect.

The patent establishes alkaline-earth chloride as a useful additive for NBR metathesis, relevant to HNBR precursor reduction.

#### Technical Relevance

This patent is relevant because it provides a catalyst-system strategy for accelerating NBR metathesis, a key precursor step in HNBR manufacture. The salt-additive concept can reduce catalyst demand or improve depolymerization efficiency before hydrogenation.

### Patent 8: US5569719A — Vulcanizable partially hydrogenated nitrile rubber composition containing …

| Patent Number | US5569719A |
| --- | --- |
| Title | Vulcanizable partially hydrogenated nitrile rubber composition containing … |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 1996 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: This patent discloses partial hydrogenation of acrylonitrile-butadiene copolymer rubber in methyl isobutyl ketone using a Pd/SiO2 catalyst to obtain HNBR with controlled iodine value. The resulting partially hydrogenated rubber is then compounded and sulfur-vulcanized, with tellurium dithiocarbamate used as a vulcanization promoter in some formulations.

Bound acrylonitrile content: 36% by weight — Example 1

Hydrogenation solvent: methyl isobutyl ketone — Example 1

Catalyst: Pd/SiO2 — Example 1

Iodine value: 15 — Example 1

Hydrogenation degree: 95% — Example 1

Zinc oxide: 5 parts — Table 1

Stearic acid: 1 part — Table 1

FEF carbon black: 45 parts — Table 1

Sulfur: 0.5, 0.75, 1.0 parts — Table 1

Tetramethylthiuramdisulfide: 1.5 parts — Table 1

2-mercaptobenzothiazole: 0.5 parts — Table 1

Tellurium diethyldithiocarbamate: 1.0 or 2.0 parts — Table 1

Vulcanization temperature: 160° C. — Example 1

Vulcanization time: 20 minutes — Example 1

Sheet thickness: 2 mm — Example 1

Iodine value: 10, 20, 30 — Example 2

Tensile strength: 300, 284, 241 kgf/cm2 — Example 2

Elongation: 660, 630, 500% — Example 2

Tensile stress at 100% elongation: 82, 89, 107 kgf/cm2 — Example 2

Hardness: 68, 68, 69 JIS A — Example 2

Heat build-up: 40, 27, 19 °C — Example 2

#### Relevant Experimental Evidence

Example 1: HNBR with iodine value 15 and 95% hydrogenation was prepared and compounded into sulfur-vulcanizable recipes.

Example 1: tellurium dithiocarbamate-containing formulations showed improved tensile and heat-build-up behavior versus controls.

Example 2: HNBR iodine value was varied from 10 to 30, showing the effect of hydrogenation level on heat build-up and mechanical properties.

Example 2: lower iodine value generally reduced heat build-up, supporting the importance of residual unsaturation control.

#### Technical Relevance

This patent is directly relevant because it discloses the hydrogenation step used to make HNBR from NBR and links hydrogenation level to final vulcanizate performance. It also shows that partial hydrogenation around 95% can deliver useful balance of mechanical strength and heat resistance.

### Patent 9: US7846995B2 — …  -containing catalyst residues from optionally hydrogenated nitrile rubber

| Patent Number | US7846995B2 |
| --- | --- |
| Title | … -containing catalyst residues from optionally hydrogenated nitrile rubber |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2010 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: This patent focuses on removing ruthenium-containing catalyst residues from optionally hydrogenated nitrile rubber solutions using functionalized ion-exchange resins. The HNBR starting material is described as having been made by NBR metathesis with Grubbs II catalyst followed by hydrogenation with RhCl(PPh3)3, and the resin treatment is used to lower residual Ru content.

Acrylonitrile content: 34% b.w. — starting HNBR description

Residual double bonds: less than 0.9% — starting HNBR description

Mooney viscosity: about 40 ML 1+4@100° C. — starting HNBR description

Standard rubber solution concentration: 6.0% by weight — starting material

Resin mass: 0.5 g — Example 1A

Rubber solution mass: 180 g — Example 1A

Reaction temperature: ca. 100° C. — Example 1A

Reaction time: 66 hours — Example 1A

Drying temperature: 60° C. — Example 1A

Initial Ru content: 15 ppm — Table 1/2

Ru content after treatment: 10 ppm — Table 1/2

Ru removal: 33% — Table 1/2

#### Relevant Experimental Evidence

Example 1A: thiourea-functionalized resin reduced Ru content from 15 ppm to 10 ppm.

Example 2A: amine-functionalized resin gave the same 33% Ru removal as the thiourea resin.

The patent demonstrates a practical purification step for HNBR solutions after metathesis/hydrogenation processing.

#### Technical Relevance

This patent is relevant because residual catalyst removal is an important finishing step in HNBR manufacture, especially for metathesis-derived materials. It provides a route to lower Ru content in hydrogenated nitrile rubber solutions, improving product purity and potentially downstream stability.

## 3. Cross-Patent Comparison & Synthesis Trends

US7919563B2 and US7772328B2 both disclose solution-phase NBR metathesis followed by hydrogenation, using monochlorobenzene, ethylene or 1-hexene co-olefins, and high-pressure hydrogenation with Wilkinson-type catalyst systems.

Both low-molecular-weight HNBR patents report the same substrate composition basis: 34 mol % acrylonitrile NBR with Mooney viscosity 35, but they differ in emphasis on shaped-article utility versus polymer-property optimization.

EP2580260A1 shifts from synthesis to formulation, using partially hydrogenated NBR in silicone blends and emphasizing low-solvent processing and compression-set improvement rather than precursor depolymerization.

US9321910B2 and US5569719A both focus on compounding/vulcanization of HNBR, but US9321910B2 uses microgels and peroxide/unsaturated-carboxylic-acid systems, whereas US5569719A uses sulfur vulcanization with tellurium dithiocarbamate promoter.

US8957161B2 and US7737233B2 both address metathesis degradation of NBR with ruthenium catalysts; US7737233B2 specifically claims alkaline-earth chloride additives, while US8957161B2 compares multiple salts including LiBr, LiCl, LiI, and CaCl2.

US7846995B2 is distinct in targeting post-reaction purification, showing that HNBR made by metathesis/hydrogenation can be treated with functionalized ion-exchange resins to reduce residual Ru.

Across the metathesis-focused patents, solution chlorobenzene/monochlorobenzene is the dominant solvent, room temperature or 80°C are common metathesis conditions, and catalyst loading is typically expressed in phr or mg scale.

Hydrogenation-specific disclosure is strongest in US5569719A and the low-molecular-weight HNBR patents, where hydrogenation level is linked to iodine value, residual double bonds, and final Mooney viscosity.

## 4. Conclusion

The patent set shows that hydrogenated NBR is most effectively accessed through controlled precursor engineering of NBR by metathesis, followed by hydrogenation and, where needed, purification or formulation tailoring. The strongest synthesis evidence supports solution metathesis of NBR in monochlorobenzene/chlorobenzene with ruthenium carbene catalysts, co-olefins such as ethylene or 1-hexene, and subsequent hydrogenation under high H2 pressure using Wilkinson-type catalysts. For property control, the evidence favors low residual unsaturation, lower Mooney viscosity, and narrower molecular-weight distribution; in the formulation space, partial hydrogenation levels around 95% and careful promoter/additive selection improve heat build-up, compression set, and high-temperature durability. Recommended evidence-based synthesis parameters are: metathesis in monochlorobenzene at about 80° C. or room temperature with controlled catalyst loading, hydrogenation at 1200 psi H2 and 138° C. when using homogeneous Rh catalysts, and post-treatment to reduce residual Ru when catalyst carryover is a concern.

## 5. References

US7919563B2 | Low molecular weight hydrogenated nitrile rubber | Not disclosed | US | 2011 | https://patents.google.com/patent/US7919563B2/en

US7772328B2 | Low molecular weight hydrogenated nitrile rubber | Not disclosed | US | 2010 | https://patents.google.com/patent/US7772328B2/en

EP2580260A1 | Blends of partially hydrogenated nitrile rubber and silicone rubber, … | Not disclosed | EP | 2013 | https://patents.google.com/patent/EP2580260A1/en

US9321910B2 | Microgel-containing vulcanizable composition based on hydrogenated nitrile … | Not disclosed | US | 2016 | https://patents.google.com/patent/US9321910B2/en

EP2519350B1 | Highly active metathesis catalysis selective for romp and rcm | Not disclosed | EP | 2019 | https://patents.google.com/patent/EP2519350B1/en

US8957161B2 | Process for reacting chemical compounds in the presence of catalyst systems | Not disclosed | US | 2015 | https://patents.google.com/patent/US8957161B2/en

US7737233B2 | Catalyst systems and their use for metathesis reactions | Not disclosed | US | 2010 | https://patents.google.com/patent/US7737233B2/en

US5569719A | Vulcanizable partially hydrogenated nitrile rubber composition containing … | Not disclosed | US | 1996 | https://patents.google.com/patent/US5569719A/en

US7846995B2 | …  -containing catalyst residues from optionally hydrogenated nitrile rubber | Not disclosed | US | 2010 | https://patents.google.com/patent/US7846995B2/en