# Low Acrylonitrile NBR Patent Landscape: Composition Control, Continuous Feed Strategies, and Emulsion Polymerization Routes

## 1. Abstract

This report synthesizes patent evidence relevant to low-acrylonitrile nitrile butadiene rubber (NBR), with emphasis on how acrylonitrile content is controlled during copolymer synthesis and how process design affects composition uniformity, conversion, and downstream properties. The target material is low-ACN NBR, generally understood as NBR with reduced acrylonitrile content relative to standard grades, often in the approximate 10–18 wt% range and typically below about 20 wt% ACN. The patent set spans three distinct but related approaches: a modern controlled emulsion/block-copolymer platform that explicitly incorporates nitrile-rubber blocks containing acrylonitrile and butadiene; a continuous emulsion copolymerization process designed to manage monomer ratio drift and achieve high bound acrylonitrile; and an older grafting/latex-based route that uses preformed NBR latex as a rubber phase in impact-resistant nitrile polymer compositions.

Across the landscape, the dominant technical theme is monomer composition control. US5770660A shows that incremental butadiene addition in multiple reactors can maintain a more constant acrylonitrile/butadiene ratio and produce NBR with about 48.8–59.5 wt% bound acrylonitrile, demonstrating the importance of feed staging and conversion management. US7592409B2 is not a direct low-ACN NBR patent, but it is relevant because it discloses emulsion polymerization with in-situ emulsifier formation and block architectures that include a nitrile-rubber B block composed of acrylonitrile and 1,3-butadiene; this supports controlled emulsion methods that could be adapted to low-ACN NBR block or seed-latex synthesis. US3426102A discloses preformed NBR latexes with acrylonitrile/butadiene ratios such as 40/60 and 25/75 used as impact modifiers in aqueous polymerization, illustrating early latex-based NBR preparation and the role of low-to-moderate ACN rubber phases in property tuning.

Overall, the evidence favors emulsion-based synthesis, careful monomer feed scheduling, and use of emulsifier/initiator systems that preserve latex stability while controlling composition drift. For low-ACN NBR, the most transferable parameters are staged monomer addition, moderate temperatures in the 45–60 C range for conventional emulsion routes, and maintaining a stable aqueous phase with suitable emulsifier and chain-transfer control.

## 2. Primary Patent Evidence

### Patent 1: US7592409B2 — Styrene acrylonitrile isoprene triblock copolymer

| Patent Number | US7592409B2 |
| --- | --- |
| Title | Styrene acrylonitrile isoprene triblock copolymer |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2009 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: This patent discloses controlled emulsion polymerization using a monomer solution containing a latent surfactant and a controlled free-radical polymerization agent, mixed with an aqueous medium containing a conjugate base to generate the emulsifier in situ. It is used to make block copolymers, including A-B-A architectures where the B block can contain acrylonitrile/methacrylonitrile and a conjugated diolefin such as 1,3-butadiene or isoprene.

Latent surfactant amount: ~0.2 grams — Example 1

Styrene charge: 5 milliliters — Example 1

Aqueous phase volume: 5 milliliters — Example 1

Styrene charge: 1,000 grams — Example 2

Oleic acid charge: 60.0 grams — Example 2

Dibenzyltrithiocarbonate charge: 7.2 grams — Example 2

RO water charge: 4,000 grams — Example 2

Potassium persulfate charge: 40.0 grams — Example 2

Tripotassium phosphate charge: 40.0 grams — Example 2

Potassium hydroxide charge: 16.4 grams — Example 2

Reaction temperature: 65 C — Example 2

Complete conversion time: less than 1.5 hours — Example 2

Styrene charge: 1,000 grams — Example 3

Hexadecyl half ester of maleic acid charge: 60.0 grams — Example 3

Dibenzyltrithiocarbonate charge: 7.2 grams — Example 3

RO water charge: 4,000 grams — Example 3

Potassium persulfate charge: 40.0 grams — Example 3

Tripotassium phosphate charge: 40.0 grams — Example 3

Potassium hydroxide charge: 16.4 grams — Example 3

Reaction temperature: 65 C — Example 3

Complete conversion time: less than 3 hours — Example 3

Butadiene content in B block: 80.4 — Example 3 table

Acrylonitrile content in B block: 39.6 — Example 3 table

Butadiene content in B block: 71.3 — Example 3 table

Acrylonitrile content in B block: 35.2 — Example 3 table

Butadiene content in B block: 72.1 — Example 3 table

Acrylonitrile content in B block: 35.5 — Example 3 table

Butadiene content in B block: 60.9 — Example 3 table

Acrylonitrile content in B block: 29.8 — Example 3 table

Reaction temperature: 149 F — Example 3 table

RO water charge: 200 — Example 4

RO water charge: 241 — Example 5

RO water charge: 197.1 — Example 5

RO water charge: 84.7 — Example 5

RO water charge: 160.5 — Example 5

Styrene charge: 50 grams (0.48 moles) — Example 8

Oleic acid charge: 3.0 grams (0.0106 moles) — Example 8

Phenyl-t-butylnitrone charge: 0.44 grams (0.002485 moles) — Example 8

Distilled water charge: 200 grams — Example 8

Potassium persulfate charge: 2.06 grams (0.00762 moles) — Example 8

Tripotassium phosphate charge: 2.13 grams (0.01 moles) — Example 8

Potassium hydroxide charge: 0.9 grams (0.014 moles) — Example 8

Reaction temperature: 65 C — Example 8

Complete conversion time: about 7 hours — Example 8

Styrene charge: 200 grams (1.923 moles) — Example 10

Oleic acid charge: 12.0 grams (0.0424 moles) — Example 10

Phenyl-t-butylnitrone charge: 2.0 grams (0.0113 moles) — Example 10

Distilled water charge: 500 grams — Example 10

Potassium persulfate charge: 8.0 grams (0.296 moles) — Example 10

Tripotassium phosphate charge: 8.0 grams (0.0377 moles) — Example 10

Potassium hydroxide charge: 3.6 grams (0.056 moles) — Example 10

Reaction temperature: 75 C — Example 10

Complete conversion time: about 3.5 hours — Example 10

Styrene charge: 50.0 grams (0.48 moles) — Example 13

Oleic acid charge: 3.0 grams (0.0106 moles) — Example 13

Benzaldehyde charge: 0.31 grams (0.00292 moles) — Example 13

N-isopropylhydroxylamine solution: 1.4 grams (0.0028 moles) of 15% aqueous solution — Example 13

Stirring time before styrene addition: 1 hour — Example 13

Distilled water charge: 200 grams — Example 13

Potassium persulfate charge: 2.06 grams (0.00762 moles) — Example 13

Tripotassium phosphate charge: 2.13 grams (0.01 moles) — Example 13

Potassium hydroxide charge: 0.9 grams (0.014 moles) — Example 13

Reaction temperature: 75 C — Example 13

Complete conversion time: about 4 hours — Example 13

Styrene charge: 50.0 grams (0.48 moles) — Example 14

Dodecylbenzenesulfonic acid charge: 3.0 grams (0.0092 moles) — Example 14

Water charge: 1 milliliter — Example 14

Sodium nitrite charge: 0.171 grams (0.002485 moles) — Example 14

Distilled water charge: 200 grams — Example 14

Potassium persulfate charge: 2.06 grams (0.00762 moles) — Example 14

Tripotassium phosphate charge: 2.13 grams (0.01 moles) — Example 14

Potassium hydroxide charge: 0.74 grams (0.0115 moles) — Example 14

Reaction temperature: 75 C — Example 14

Complete conversion time: about 3 hours — Example 14

Styrene charge: 50 grams (0.48 moles) — Example 15

Oleic acid charge: 3.0 grams (0.0106 moles) — Example 15

1,1-Diphenylethylene charge: 0.448 grams (0.002485 moles) — Example 15

Distilled water charge: 200 grams — Example 15

Potassium persulfate charge: 2.06 grams (0.00762 moles) — Example 15

Tripotassium phosphate charge: 2.13 grams (0.01 moles) — Example 15

Potassium hydroxide charge: 0.92 grams (0.0143 moles) — Example 15

Reaction temperature: 75 C — Example 15

Complete conversion time: about 2 hours — Example 15

Styrene charge: 2,240 grams — Example 16

Oleic acid charge: 134.4 grams — Example 16

Dibenzyltrithiocarbonate charge: 16.0 grams — Example 16

RO water charge: 3,808 grams — Example 16

Potassium persulfate charge: 13.44 grams — Example 16

Tripotassium phosphate charge: 89.6 grams — Example 16

Potassium hydroxide charge: 36.96 grams — Example 16

Reaction temperature: 65 C — Example 16

Complete conversion time: less than 3 hours — Example 16

Solids: 38.9% — Example 16

Styrene charge: 50 grams (0.48 moles) — Example 17

Sodium nitrite charge: 0.69 grams (0.01 moles) — Example 17

Oleic acid charge: 3.0 grams (0.0106 moles) — Example 17

Concentrated acetic acid charge: 1.0 grams (0.0167 moles) — Example 17

Water charge: 2 grams — Example 17

Distilled water charge: 160 grams — Example 17

Potassium persulfate charge: 2.0 grams (0.00739 moles) — Example 17

Tripotassium phosphate charge: 2.0 grams (0.01 moles) — Example 17

Potassium hydroxide charge: 2.35 grams (0.0367 moles) — Example 17

Reaction temperature: 75 C — Example 17

Complete conversion time: about 2.5 hours — Example 17

Solids: 26.1% — Example 17

Styrene charge: 50 grams (0.48 moles) — Example 18

Oleic acid charge: 3.0 grams (0.0106 moles) — Example 18

1-Chloro-1,1-diphenylethane: approximately 0.01 moles — Example 18

Distilled water charge: 200 grams — Example 18

Potassium persulfate charge: 2.0 grams (0.0074 moles) — Example 18

Tripotassium phosphate charge: 2.0 grams (0.0094 moles) — Example 18

Potassium hydroxide charge: 1.55 grams (0.0242 moles) — Example 18

Reaction temperature: 75 C — Example 18

Complete conversion time: about 4 hours — Example 18

Solids: 22.7% — Example 18

Styrene charge: 1,300 grams (12.5 moles) — Example 19

Oleic acid charge: 78.0 grams (0.2756 moles) — Example 19

Crude 1-chloro-1,1-diphenylethane charge: 39.0 grams — Example 19

Deionized RO water charge: 2,470 grams — Example 19

Potassium persulfate charge: 50.7 grams (0.1875 moles) — Example 19

Tripotassium phosphate charge: 50.7 grams (0.2388 moles) — Example 19

Potassium hydroxide charge: 29.5 grams (0.602 moles) — Example 19

Reaction temperature: 75 C — Example 19

Complete conversion time: about 5.5 hours — Example 19

Solids: 38.6% — Example 19

1-Hexene charge: 25 grams — Example 20

n-Butyl acrylate charge: 25 grams — Example 20

Dipyridyl charge: 0.38 grams — Example 20

Oleic acid charge: 4.0 grams — Example 20

Ethyl 2-bromoisobutyrate charge: 0.47 grams — Example 20

85% KOH charge: 1.7 grams — Example 20

Water charge: 139 milliliters — Example 20

Copper sulfate pentahydrate solution: 60.9 grams of 1% aqueous solution — Example 20

Hydrazine hydrate: 2 drops — Example 20

Reaction temperature: about 67 C — Example 20

Reaction time: 1.5 hours — Example 20

Solids: 10.9% — Example 20

1-Hexene incorporation: 5.5 mole% — Example 20

#### Relevant Experimental Evidence

Example 1: Demonstrated in-situ emulsification using latent surfactant/activator pairs to form emulsions before polymerization.

Example 2: Showed RAFT emulsion polymerization at 65 C with complete conversion in less than 1.5 hours and a stable latex.

Example 3: Demonstrated in-situ generated polymerizable surfactant and rapid microemulsion polymerization at 65 C.

Example 5: Showed preparation of S-NBR-S triblock copolymer latexes from seed latexes.

Example 20: Demonstrated microemulsion ATRP copolymerization and confirmed 5.5 mole% 1-hexene incorporation.

#### Technical Relevance

This patent is relevant because it discloses controlled emulsion polymerization methods that can accommodate nitrile-containing blocks and block architectures, which are useful for designing NBR-based materials with tailored acrylonitrile distribution. Although it is not a direct low-ACN NBR synthesis patent, its in-situ emulsification and seed/block strategies are transferable to controlled NBR latex synthesis.

### Patent 2: US5770660A — Continuous polymerization process for producing NBR rubber having a high bound …

| Patent Number | US5770660A |
| --- | --- |
| Title | Continuous polymerization process for producing NBR rubber having a high bound … |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 1998 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: This patent discloses a continuous free-radical emulsion polymerization process for acrylonitrile and butadiene in which butadiene is added incrementally across multiple reaction vessels. The process is designed to maintain a substantially constant unconverted monomer ratio and produce NBR with high bound acrylonitrile and improved tensile/environmental resistance properties.

Initial monomer ratio: about 80 parts acrylonitrile to 20 parts ±10% butadiene — Claim 1

Unconverted monomer ratio: about 70 to 90 parts acrylonitrile to about 30 to 10 parts butadiene — Claim 1

Bound acrylonitrile content: about fifty percent by weight — Claim 1

Example I initial butadiene charge: 21 parts — Example I

Example I acrylonitrile charge: 54 parts — Example I

Example I conversion: 50.2 percent — Example I

Example I bound acrylonitrile: 59.5 percent by weight — Example I

Example II initial butadiene charge: 21 parts — Example II

Example II acrylonitrile charge: 54 parts — Example II

Example II additional butadiene charge: 16 parts — Example II

Example II conversion: 73.3 percent — Example II

Example II bound acrylonitrile: 52.6 percent by weight — Example II

Example III conversion: 73.6 percent — Example III

Example III bound acrylonitrile: 54.9 percent — Example III

Example IV initial butadiene charge: 21 parts — Example IV

Example IV additional butadiene charge: 16 parts — Example IV

Example IV additional butadiene charge: 9 parts — Example IV

Example IV conversion: 85.2 percent — Example IV

Example IV bound acrylonitrile: 50.5 percent — Example IV

Example V acrylonitrile charge: 56 parts — Example V

Example V total butadiene charge: 43 parts — Example V

Example V initial butadiene charge: 22 parts — Example V

Example V additional butadiene charges: 8 parts, 7 parts, 6 parts — Example V

Example V final conversion: 81.9 percent — Example V

Example V bound acrylonitrile: 50.2 percent — Example V

Example VI final conversion: 86.8 percent — Example VI

Example VI bound acrylonitrile: 50.6 percent — Example VI

Example VII acrylonitrile charge: 56 parts — Example VII

Example VII initial butadiene charge: 20 parts — Example VII

Example VII additional butadiene charges: 6 parts, 6 parts, 6 parts, 6 parts — Example VII

Example VII steady-state conversion in first vessel: 24 percent — Example VII

Example VII steady-state conversion in second vessel: 40 percent — Example VII

Example VII steady-state conversion in third vessel: 56 percent — Example VII

Example VII steady-state conversion in fourth vessel: 72 percent — Example VII

Example VII steady-state conversion in fifth vessel: 82 percent — Example VII

Example VII bound acrylonitrile: 48.8 percent — Example VII

#### Relevant Experimental Evidence

Example I: Conventional batch process with limited butadiene gave 59.5 wt% bound acrylonitrile but only 50.2% conversion.

Example II: Two-increment butadiene addition improved conversion to 73.3% and produced 52.6 wt% bound acrylonitrile.

Example IV: Three butadiene increments raised conversion to 85.2% while maintaining 50.5% bound acrylonitrile.

Example V: Four butadiene increments with 56 parts acrylonitrile and 43 parts butadiene gave 50.2 wt% bound acrylonitrile at 81.9% conversion.

Example VII: Continuous five-vessel operation maintained staged conversions and produced 48.8% bound acrylonitrile with improved tensile and environmental resistance.

#### Technical Relevance

This patent is highly relevant because it directly addresses acrylonitrile/butadiene copolymerization and shows how staged butadiene feed controls composition drift, a key issue in low-ACN and composition-tuned NBR. The continuous feed strategy and monomer-ratio management provide practical guidance for producing more uniform NBR latexes with targeted acrylonitrile content.

### Patent 3: US3426102A — Polymerizates of olefinic nitriles and diene-nitrile rubbers

| Patent Number | US3426102A |
| --- | --- |
| Title | Polymerizates of olefinic nitriles and diene-nitrile rubbers |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 1969 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: This patent discloses preparation of a preformed nitrile rubber latex by emulsion polymerization of acrylonitrile and butadiene under agitation, low oxygen, and controlled pH, followed by use of that latex as a rubber phase in impact-resistant nitrile polymer compositions. The examples also show grafting/latex blending with acrylonitrile-containing monomer systems to form high-impact barrier resins.

Example I-A acrylonitrile charge: 60 parts — Example I

Example I-A butadiene-1,3 charge: 40 parts — Example I

Example I-A emulsifier charge: 2.4 parts GAFAC RE-610 — Example I

Example I-A initiator charge: 0.3 parts azo-bis-isobutyronitrile — Example I

Example I-A chain-transfer agent charge: 0.5 parts t-dodecyl mercaptan — Example I

Example I-A water charge: 200 parts — Example I

Example I-A polymerization temperature: 45 C — Example I

Example I-A pH: about 8 — Example I

Example I-A reaction time: 22.5 hours — Example I

Example I-A conversion: 92% — Example I

Example I-A total solids: 33.1% — Example I

Example I-B acrylonitrile charge: 70 parts — Example I

Example I-B ethyl acrylate charge: 30.0 parts — Example I

Example I-B latex A charge: 31.9 parts — Example I

Example I-B initiator charge: 0.06 parts potassium persulfate — Example I

Example I-B emulsifier charge: 3.0 parts GAFAC RE-610 — Example I

Example I-B chain-transfer agent charge: 1.0 parts n-dodecyl mercaptan — Example I

Example I-B chelating agent charge: 0.05 parts ethylene diamine tetracetic acid — Example I

Example I-B water charge: 200 parts — Example I

Example I-B pH: about 7 — Example I

Example I-B polymerization temperature: 60 C — Example I

Example I-B reaction time: 20 hours — Example I

Example I-B conversion: 97% — Example I

Example I-B total solids: 33% — Example I

Example I-C acrylonitrile charge: 73.6 parts — Example I

Example I-C ethyl acrylate charge: 30 parts — Example I

Example I-C butadiene charge: 5.4 parts — Example I

Example I-C total solids: 38.3% — Example I

Example I-C conversion: 87.7% — Example I

Example 11-A acrylonitrile charge: 40 parts — Example 11

Example 11-A butadiene charge: 60 parts — Example 11

Example 11-A emulsifier charge: 2.4 parts — Example 11

Example 11-A potassium persulfate charge: 0.1 parts — Example 11

Example 11-A t-dodecyl mercaptan charge: 0.5 parts — Example 11

Example 11-A water charge: 200.0 parts — Example 11

Example 11-A polymerization temperature: 45 C — Example 11

Example 11-A pH: about 8 — Example 11

Example 11-A reaction time: 5.5 hours — Example 11

Example 11-A conversion: 97% — Example 11

Example 11-A total solids: 33% — Example 11

Example 11-B acrylonitrile charge: 70 parts — Example 11

Example 11-B ethyl acrylate charge: 30 parts — Example 11

Example 11-B latex A charge: 33 parts — Example 11

Example 11-B potassium persulfate charge: 0.06 parts — Example 11

Example 11-B n-dodecyl mercaptan charge: 1.0 parts — Example 11

Example 11-B emulsifier charge: 3.0 parts — Example 11

Example 11-B ethylene diamine tetraacetic acid charge: 0.05 parts — Example 11

Example 11-B water charge: 200.0 parts — Example 11

Example 11-B polymerization temperature: 60 C — Example 11

Example 11-B reaction time: 20 hours — Example 11

Example 11-B conversion: 96% — Example 11

Example 11-B total solids: 33% — Example 11

Example V acrylonitrile charge: 20 parts — Example V

Example V ethyl acrylate charge: 20 parts — Example V

Example V rubber latex charge: 50 parts — Example V

Example VI rubber latex charge: 20 parts per parts of acrylonitrile-ethyl acrylate monomer mixture — Example VI

Example VII rubber content: about 9 parts by weight — Example VII

Example VIII rubber content: 12 parts per 112 parts of polymer — Example VIII

Example XI-A methacrylonitrile charge: sole monomer — Example XI

Example XI-A t-butyl peroxypivalate charge: 0.4 part — Example XI

Example XI-A n-dodecyl mercaptan charge: 0.5 part — Example XI

Example XI-A emulsifier charge: 2.4 parts — Example XI

Example XI-A water charge: 225 parts — Example XI

Example XI-A polymerization temperature: not explicitly stated in the example text beyond the procedure reference — Example XI

Example XI-A rubber latex loading: 10 parts of 25:75 acrylonitrile:butadiene rubber per 110 parts total polymer — Example XI

Example XII-A methacrylonitrile charge: 90 parts — Example XII

Example XII-A ethyl acrylate charge: 10 parts — Example XII

Example XII-A t-butyl peroxypivalate charge: 0.3 part — Example XII

Example XII-A n-dodecyl mercaptan charge: 0.5 part — Example XII

Example XII-A emulsifier charge: 2.4 parts — Example XII

Example XII-A water charge: 200 parts — Example XII

Example XII-A polymerization temperature: 60 C — Example XII

Example XII-A pH: about 7 — Example XII

#### Relevant Experimental Evidence

Example I-A: Prepared a 60/40 acrylonitrile/butadiene rubber latex at 45 C with 92% conversion and 33.1% solids.

Example I-B: Grafted 70/30 acrylonitrile/ethyl acrylate onto the NBR latex at 60 C to form a high-impact barrier resin.

Example I-C: Showed a terpolymer containing acrylonitrile, ethyl acrylate, and butadiene with 87.7% conversion.

Example 11-A: Repeated the NBR latex preparation at 45 C using 40/60 acrylonitrile/butadiene and obtained 97% conversion.

Example XI-A: Demonstrated use of a 25:75 acrylonitrile/butadiene rubber latex in methacrylonitrile-based graft polymerization.

#### Technical Relevance

This patent is relevant because it explicitly discloses acrylonitrile/butadiene rubber latexes with defined monomer ratios, including a 40/60 acrylonitrile/butadiene example that falls within the low-to-moderate ACN NBR range. It also shows how such latexes can be used as preformed rubber phases in aqueous polymerization, which is important for understanding low-ACN NBR preparation and utilization.

## 3. Cross-Patent Comparison & Synthesis Trends

US5770660A is the only patent in the set that directly targets acrylonitrile/butadiene copolymerization as the primary product; it uses continuous staged butadiene addition to control monomer ratio drift and achieve about 48.8–59.5 wt% bound acrylonitrile.

US3426102A discloses preformed NBR latexes with explicit acrylonitrile/butadiene ratios of 60/40 and 40/60, plus a 25/75 rubber latex used in graft/impact resin systems; its process is batch emulsion polymerization at 45–60 C with emulsifier, initiator, and mercaptan chain transfer agent.

US7592409B2 is mechanistically relevant but not a direct NBR patent; it teaches in-situ emulsifier formation and controlled emulsion/block polymerization, including B blocks containing acrylonitrile and butadiene/isoprene, which could be adapted to controlled NBR architectures.

Compared with the older batch emulsion route in US3426102A, US5770660A provides stronger composition control by staged monomer feeding and multiple reactors, reducing the monomer-ratio swing that normally occurs as butadiene is depleted.

US3426102A uses conventional emulsion ingredients such as GAFAC RE-610, potassium persulfate or azo-bis-isobutyronitrile, and t-dodecyl/n-dodecyl mercaptan; US5770660A emphasizes process staging rather than a novel catalyst system.

US7592409B2 operates at 65–75 C in microemulsion/RAFT/NMP-like systems with oleic acid, potassium persulfate, tripotassium phosphate, and potassium hydroxide, whereas US5770660A and US3426102A are conventional NBR emulsion processes centered on monomer feed and latex stability.

For low-acrylonitrile NBR specifically, the most transferable lesson is from US5770660A: control the acrylonitrile/butadiene feed ratio and avoid complete butadiene depletion to preserve uniform composition.

US3426102A suggests that low-to-moderate ACN rubber phases can be prepared at 45 C with about 8 pH and 33% solids, which may be useful for low-ACN latex design and downstream blending.

## 4. Conclusion

The patent evidence shows that low-acrylonitrile NBR synthesis is best approached through emulsion polymerization with tight monomer-feed control and stable latex formation. The strongest direct guidance comes from US5770660A, which demonstrates that staged butadiene addition across multiple reactors can maintain a more uniform acrylonitrile/butadiene ratio and avoid the composition drift that degrades properties in conventional batch NBR. US3426102A provides older but still useful evidence that acrylonitrile/butadiene latexes can be made at 45 C with emulsifier, initiator, and mercaptan chain-transfer control, including a 40/60 acrylonitrile/butadiene rubber latex that is within the low-to-moderate ACN regime. US7592409B2 is not a direct NBR patent, but it supports controlled emulsion strategies and block/seed architectures that could be adapted to low-ACN nitrile rubber systems. Based on the evidence, recommended synthesis parameters are emulsion polymerization, staged or incremental monomer feed, moderate temperatures around 45–60 C for conventional NBR latex routes, and careful maintenance of unconverted monomer ratio to prevent butadiene depletion and composition drift.

## 5. References

US7592409B2 | Styrene acrylonitrile isoprene triblock copolymer | Not disclosed | US | 2009 | https://patents.google.com/patent/US7592409B2/en

US5770660A | Continuous polymerization process for producing NBR rubber having a high bound … | Not disclosed | US | 1998 | https://patents.google.com/patent/US5770660A/en

US3426102A | Polymerizates of olefinic nitriles and diene-nitrile rubbers | Not disclosed | US | 1969 | https://patents.google.com/patent/US3426102A/en