# Low Acrylonitrile NBR: Patent Landscape and Process/Composition Evidence

## 1. Abstract

This report synthesizes two primary patents that intersect with low-acrylonitrile nitrile rubber chemistry, but they do so in different ways. US7592409B2 is primarily a controlled emulsion polymerization patent for styrene-based block copolymers that explicitly includes a nitrile-rubber block described as randomly distributed acrylonitrile and 1,3-butadiene; it is relevant as a process platform demonstrating aqueous microemulsion polymerization, in-situ emulsifier formation, and block-copolymer architectures containing NBR-like segments. US9624333B2 is more directly aligned with low-acrylonitrile NBR because it discloses ABS/graft-copolymer systems whose graft sheath contains acrylonitrile and/or methyl methacrylate, while the graft substrate is a butadiene-rich rubber prepared by aqueous emulsion polymerization. Across the two patents, the dominant synthesis motif is emulsion polymerization in water, often with potassium persulfate initiation, potassium hydroxide or bicarbonate buffering, and surfactant/soap stabilization. The first patent emphasizes controlled radical polymerization in microemulsion/latex form with in-situ surfactant generation and seed-latex block growth; the second emphasizes conventional aqueous emulsion polymerization of butadiene/styrene rubber substrates followed by agglomeration and grafting. For low-acrylonitrile NBR, the most important evidence is the explicit use of acrylonitrile as a comonomer in a rubber block or graft sheath and the ability to tune rubber composition through feed strategy and aqueous emulsion processing. However, neither patent is a dedicated low-ACN NBR grade patent; instead, they provide enabling process and composition windows that can support low-acrylonitrile rubber design, especially where acrylonitrile is present at controlled, relatively modest levels in a butadiene-rich copolymer. The landscape therefore points to aqueous emulsion routes, staged monomer addition, and composition control as the main levers for low-ACN NBR-related materials.

## 2. Primary Patent Evidence

### Patent 1: US7592409B2 — Styrene acrylonitrile isoprene triblock copolymer

| Patent Number | US7592409B2 |
| --- | --- |
| Title | Styrene acrylonitrile isoprene triblock copolymer |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2009 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: The patent discloses controlled emulsion polymerization in an aqueous polymerization medium, including in-situ formation of an emulsifier from a latent surfactant and surfactant activator. It also describes block-copolymer synthesis using a vinyl-aromatic A block and a B block containing acrylonitrile/methacrylonitrile with a conjugated diolefin such as 1,3-butadiene or isoprene, enabling NBR-like block segments in latex form.

Latent surfactant amount: 0.2 grams — Example 1

Styrene volume: 5 milliliters — Example 1

Surfactant activator solution volume: 5 milliliters — Example 1

Reaction vessel size: 2-gallon — Example 2

Styrene charge: 1,000 grams — Example 2

Oleic acid charge: 60.0 grams — Example 2

Dibenzyltrithiocarbonate charge: 7.2 grams — Example 2

RO water charge: 4,000 grams — Example 2

Potassium persulfate charge: 40.0 grams — Example 2

Tripotassium phosphate charge: 40.0 grams — Example 2

Potassium hydroxide charge: 16.4 grams — Example 2

Polymerization temperature: 65° C. — Example 2

Conversion time: less than 1.5 hours — Example 2

Solids after stripping: 20.6% — Example 2

Mn: 54,000 — Example 2

PDI: 1.17 — Example 2

Reaction vessel size: 2-gallon — Example 3

Styrene charge: 1,000 grams — Example 3

Hexadecyl half ester of maleic acid charge: 60.0 grams — Example 3

Dibenzyltrithiocarbonate charge: 7.2 grams — Example 3

RO water charge: 4,000 grams — Example 3

Potassium persulfate charge: 40.0 grams — Example 3

Tripotassium phosphate charge: 40.0 grams — Example 3

Potassium hydroxide charge: 16.4 grams — Example 3

Polymerization temperature: 65° C. — Example 3

Conversion time: less than 3 hours — Example 3

Solids after stripping: 23.7% — Example 3

Mn: 48,000 — Example 3

PDI: 1.17 — Example 3

RO water charge: 200 grams — Example 4

RO water charge: 241 grams — Example 5

RO water charge: 197.1 grams — Example 5

RO water charge: 84.7 grams — Example 5

RO water charge: 160.5 grams — Example 5

RO water charge: 200 grams — Example 6

Styrene charge: 1,000 grams — Example 6

Oleic acid charge: 60.0 grams — Example 6

PBN charge: 10.0 grams — Example 6

Polymerization temperature: 75° C. — Example 6

Conversion time: less than 2 hours — Example 6

Solids after stripping: 22.7% — Example 6

Mn: 25,000 — Example 6

PDI: 1.80 — Example 6

RO water charge: 241 grams — Example 7

RO water charge: 197.1 grams — Example 7

RO water charge: 84.7 grams — Example 7

RO water charge: 241 grams — Example 7

RO water charge: 197.1 grams — Example 7

Styrene charge: 50 grams (0.48 moles) — Example 8

Oleic acid charge: 3.0 grams (0.0106 moles) — Example 8

PBN charge: 0.44 grams (0.002485 moles) — Example 8

Distilled water charge: 200 grams — Example 8

Potassium persulfate charge: 2.06 grams (0.00762 moles) — Example 8

Tripotassium phosphate charge: 2.13 grams (0.01 moles) — Example 8

Potassium hydroxide charge: 0.9 grams (0.014 moles) — Example 8

Polymerization temperature: 65° C. — Example 8

Conversion time: about 7 hours — Example 8

Mn: 35,000 — Example 8

Mw: 61,000 — Example 8

PDI: 1.74 — Example 8

Styrene charge: 200 grams (1.923 moles) — Example 10

Oleic acid charge: 12.0 grams (0.0424 moles) — Example 10

PBN charge: 2.0 grams (0.0113 moles) — Example 10

Distilled water charge: 500 grams — Example 10

Potassium persulfate charge: 8.0 grams (0.296 moles) — Example 10

Tripotassium phosphate charge: 8.0 grams (0.0377 moles) — Example 10

Potassium hydroxide charge: 3.6 grams (0.056 moles) — Example 10

Polymerization temperature: 75° C. — Example 10

Conversion time: about 3.5 hours — Example 10

Mn: 39,000 — Example 10

Mw: 48,000 — Example 10

PDI: 1.22 — Example 10

PBN substitution: equimolar amount of PIN — Example 11

Conversion time: about 7 hours — Example 11

Mn: 41,000 — Example 11

Mw: 70,000 — Example 11

PDI: 1.70 — Example 11

Seed latex charge: 100 grams of about 22% solids latex — Example 12

Potassium persulfate charge: 0.5 grams (0.00184 moles) — Example 12

Distilled water charge: 100 milliliters — Example 12

n-Butyl acrylate charge: 22.0 grams (0.171 moles) — Example 12

Polymerization temperature: about 65° C. — Example 12

Weak exotherm: about 70° C. — Example 12

Conversion time: about 2 hours — Example 12

Mn: 45,000 — Example 12

Mw: 77,000 — Example 12

PDI: 1.70 — Example 12

Oleic acid charge: 3.0 grams (0.0106 moles) — Example 13

Benzaldehyde charge: 0.31 grams (0.00292 moles) — Example 13

15% aqueous solution of N-isopropylhydroxylamine: 1.4 grams (0.0028 moles) — Example 13

Stirring time: 1 hour — Example 13

Styrene charge: 50.0 grams (0.48 moles) — Example 13

Distilled water charge: 200 grams — Example 13

Potassium persulfate charge: 2.06 grams (0.00762 moles) — Example 13

Tripotassium phosphate charge: 2.13 grams (0.01 moles) — Example 13

Potassium hydroxide charge: 0.9 grams (0.014 moles) — Example 13

Polymerization temperature: 75° C. — Example 13

Conversion time: about 4 hours — Example 13

Mn: 31,000 — Example 13

Mw: 55,000 — Example 13

PDI: 1.76 — Example 13

Styrene charge: 50.0 grams (0.48 moles) — Example 14

Dodecylbenzenesulfonic acid charge: 3.0 grams (0.0092 moles) — Example 14

Distilled water charge: 1 milliliter — Example 14

Sodium nitrite charge: 0.171 grams (0.002485 moles) — Example 14

Distilled water charge: 200 grams — Example 14

Potassium persulfate charge: 2.06 grams (0.00762 moles) — Example 14

Tripotassium phosphate charge: 2.13 grams (0.01 moles) — Example 14

Potassium hydroxide charge: 0.74 grams (0.0115 moles) — Example 14

Polymerization temperature: 75° C. — Example 14

Conversion time: about 3 hours — Example 14

Mn: 97,000 — Example 14

Mw: 147,000 — Example 14

PDI: 1.51 — Example 14

Styrene charge: 50 grams (0.48 moles) — Example 15

Oleic acid charge: 3.0 grams (0.0106 moles) — Example 15

1,1-Diphenylethylene charge: 0.448 grams (0.002485 moles) — Example 15

Distilled water charge: 200 grams — Example 15

Potassium persulfate charge: 2.06 grams (0.00762 moles) — Example 15

Tripotassium phosphate charge: 2.13 grams (0.01 moles) — Example 15

Potassium hydroxide charge: 0.92 grams (0.0143 moles) — Example 15

Polymerization temperature: 75° C. — Example 15

Conversion time: about 2 hours — Example 15

Mn: 51,000 — Example 15

Mw: 92,000 — Example 15

PDI: 1.80 — Example 15

Styrene charge: 2,240 grams — Example 16

Oleic acid charge: 134.4 grams — Example 16

Dibenzyltrithiocarbonate charge: 16.0 grams — Example 16

RO water charge: 3,808 grams — Example 16

Potassium persulfate charge: 13.44 grams — Example 16

Tripotassium phosphate charge: 89.6 grams — Example 16

Potassium hydroxide charge: 36.96 grams — Example 16

Polymerization temperature: 65° C. — Example 16

Solids: 38.9% — Example 16

Conversion time: less than 3 hours — Example 16

Mn: 45,500 — Example 16

PDI: 1.11 — Example 16

Sodium nitrite charge: 0.69 grams (0.01 moles) — Example 17

Oleic acid charge: 3.0 grams (0.0106 moles) — Example 17

Styrene charge: 50 grams (0.48 moles) — Example 17

Acetic acid solution: 1.0 grams (0.0167 moles) in 2 grams of water — Example 17

Distilled water charge: 160 grams — Example 17

Potassium persulfate charge: 2.0 grams (0.00739 moles) — Example 17

Tripotassium phosphate charge: 2.0 grams (0.01 moles) — Example 17

Potassium hydroxide charge: 2.35 grams (0.0367 moles) — Example 17

Polymerization temperature: 75° C. — Example 17

Conversion time: about 2.5 hours — Example 17

Solids: 26.1% — Example 17

Mn: 96,300 — Example 17

Mw: 135,000 — Example 17

PDI: 1.4 — Example 17

Styrene charge: 50 grams (0.48 moles) — Example 18

Oleic acid charge: 3.0 grams (0.0106 moles) — Example 18

1-chloro-1,1-diphenylethane: approximately 0.01 moles — Example 18

Concentrated HCl: 10 milliliters — Example 18

Toluene: 5 milliliters — Example 18

Potassium persulfate charge: 2.0 grams (0.0074 moles) — Example 18

Tripotassium phosphate charge: 2.0 grams (0.0094 moles) — Example 18

Potassium hydroxide charge: 1.55 grams (0.0242 moles) — Example 18

Distilled water charge: 200 grams — Example 18

Polymerization temperature: 75° C. — Example 18

Conversion time: about 4 hours — Example 18

Solids: 22.7% — Example 18

Mn: 40,000 — Example 18

PDI: 1.37 — Example 18

Styrene charge: 1,300 grams (12.5 moles) — Example 19

Oleic acid charge: 78.0 grams (0.2756 moles) — Example 19

Crude 1-chloro-1,1-diphenylethane charge: 39.0 grams — Example 19

RO water charge: 2,470 grams — Example 19

Potassium persulfate charge: 50.7 grams (0.1875 moles) — Example 19

Tripotassium phosphate charge: 50.7 grams (0.2388 moles) — Example 19

Potassium hydroxide charge: 29.5 grams (0.602 moles) — Example 19

Polymerization temperature: 75° C. — Example 19

Solids: 38.6% — Example 19

Conversion time: about 5.5 hours — Example 19

Mn: 32,000 — Example 19

PDI: 1.85 — Example 19

1-hexene charge: 25 grams — Example 20

n-Butyl acrylate charge: 25 grams — Example 20

Dipyridyl charge: 0.38 grams — Example 20

Oleic acid charge: 4.0 grams — Example 20

Ethyl 2-bromoisobutyrate charge: 0.47 grams — Example 20

KOH solution: 1.7 grams of 85% KOH in 139 milliliters of distilled water — Example 20

Copper sulfate pentahydrate solution: 60.9 grams of a 1% aqueous solution — Example 20

Hydrazine hydrate: 2 drops — Example 20

Reaction temperature: about 67° C. — Example 20

Reaction time: 1.5 hours — Example 20

Solids: 10.9% — Example 20

13C-NMR incorporation: 5.5 mole % 1-hexene — Example 20

Medium & Water Role: The core reaction medium is an aqueous emulsion/microemulsion latex system. Water is explicitly used as the aqueous phase in emulsifier formation and polymerization, and the examples repeatedly describe water charges and latex formation.

low acrylonitrile content: Not disclosed in extracted evidence

#### Medium & Water Role

The core reaction medium is an aqueous emulsion/microemulsion latex system. Water is explicitly used as the aqueous phase in emulsifier formation and polymerization, and the examples repeatedly describe water charges and latex formation.

#### low acrylonitrile content

Not disclosed in extracted evidence

#### Relevant Experimental Evidence

Example 1: Demonstrated multiple latent surfactant/surfactant activator combinations that generate emulsions in styrene/water.

Example 2: Showed RAFT-controlled emulsion polymerization to a stable polystyrene latex with low PDI.

Example 3: Showed RAFT polymerization using an in-situ generated polymerizable surfactant and stable latex formation.

Example 4: Demonstrated emulsion triblock copolymer formation from seed latex using water and butadiene/isoprene feeds.

Example 5: Demonstrated preparation of S-NBR-S triblock copolymer latexes from PS seed latexes.

#### Technical Relevance

This patent is relevant because it explicitly discloses a nitrile-rubber block containing acrylonitrile and 1,3-butadiene and provides a water-based controlled emulsion route for making such architectures. Although not a dedicated low-ACN NBR grade patent, it shows how acrylonitrile-containing rubber segments can be synthesized in aqueous latex systems with controlled radical methods.

### Patent 2: US9624333B2 — Thermoplastic moulding materials based on acrylonitrile, styrene and butadiene

| Patent Number | US9624333B2 |
| --- | --- |
| Title | Thermoplastic moulding materials based on acrylonitrile, styrene and butadiene |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2017 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: The patent discloses aqueous emulsion polymerization of a butadiene/styrene graft substrate followed by agglomeration and grafting to form ABS-type thermoplastic molding materials. The graft substrate is prepared in water with staged monomer feed, potassium persulfate initiation, potassium stearate emulsification, and sodium hydrogencarbonate buffering; the graft sheath then incorporates styrene and/or α-methylstyrene with acrylonitrile and/or methyl methacrylate.

Styrene content: 7 wt % — Example B1-1

Reactor size: 150 L — Example B1-1

Polymerization temperature: 67° C. — Example B1-1

Monomer mixture charge: 43,120 g — Example B1-1

Tert-dodecylmercaptan charge: 431.2 g — Example B1-1

Potassium stearate charge: 311 g — Example B1-1

Potassium persulfate charge: 82 g — Example B1-1

Sodium hydrogencarbonate charge: 147 g — Example B1-1

Water charge: 58,400 g — Example B1-1

Conversion: 95% — Example B1-1

Styrene content: 14 wt % — Example B1-2

Styrene content: 21 wt % — Example B1-3

Styrene content: 28 wt % — Example B1-4

Total styrene content: 7 wt % — Table 1

Total styrene content: 14 wt % — Table 1

Total styrene content: 21 wt % — Table 1

Total styrene content: 28 wt % — Table 1

Core styrene content: 7 wt % — Table 1

Gel content: 78.9 wt % — Table 1

Gel content: 72.2 wt % — Table 1

Gel content: 75.9 wt % — Table 1

Gel content: 76.7 wt % — Table 1

QI: 22 — Table 1

QI: 29 — Table 1

QI: 20 — Table 1

QI: 26 — Table 1

d_w: 88.4 nm — Table 1

d_w: 104.0 nm — Table 1

d_w: 87.9 nm — Table 1

d_w: 82.2 nm — Table 1

d_10: 72.3 nm — Table 1

d_10: 90.5 nm — Table 1

d_10: 72.6 nm — Table 1

d_10: 69.9 nm — Table 1

d_50: 90.0 nm — Table 1

d_50: 105.8 nm — Table 1

d_50: 88.1 nm — Table 1

d_50: 84.3 nm — Table 1

d_90: 101.1 nm — Table 1

d_90: 114.8 nm — Table 1

d_90: 98.8 nm — Table 1

d_90: 93.4 nm — Table 1

U: 0.32 — Table 1

U: 0.23 — Table 1

U: 0.30 — Table 1

U: 0.28 — Table 1

Mersolat H95 charge: 6.29 g — Agglomerating Copolymer C-1

Demineralized water charge: 1177.2 g — Agglomerating Copolymer C-1

Potassium persulfate charge: 4.87 g — Agglomerating Copolymer C-1

Demineralized water charge: 209.2 g — Agglomerating Copolymer C-1

Ethyl acrylate charge: 211.2 g — Agglomerating Copolymer C-1

Temperature increase: 60° C. to 80° C. — Agglomerating Copolymer C-1

Ethyl acrylate feed: 1691.3 g — Agglomerating Copolymer C-1

Potassium persulfate feed: 3.98 g — Agglomerating Copolymer C-1

Demineralized water feed: 170.9 g — Agglomerating Copolymer C-1

Mersolat H95 feed: 32.95 g — Agglomerating Copolymer C-1

Methacrylamide feed: 90.6 g — Agglomerating Copolymer C-1

Demineralized water feed: 1248.8 g — Agglomerating Copolymer C-1

Feed time: 405 minutes — Agglomerating Copolymer C-1

Mersolat H95 charge: 17.83 g — Comparative Example C-2

Demineralized water charge: 1177.2 g — Comparative Example C-2

Potassium persulfate charge: 4.87 g — Comparative Example C-2

Demineralized water charge: 209.2 g — Comparative Example C-2

Ethyl acrylate charge: 211.2 g — Comparative Example C-2

Temperature increase: 60° C. to 80° C. — Comparative Example C-2

Ethyl acrylate feed: 1691.3 g — Comparative Example C-2

Potassium persulfate feed: 3.98 g — Comparative Example C-2

Demineralized water feed: 170.9 g — Comparative Example C-2

Mersolat H95 feed: 21.38 g — Comparative Example C-2

Methacrylamide feed: 90.6 g — Comparative Example C-2

Demineralized water feed: 1248.8 g — Comparative Example C-2

Feed time: 405 minutes — Comparative Example C-2

Solids content: 40.0 wt % — Comparative Example C-2

Agglomeration yield: 65.8 wt % — Example 1

Agglomeration yield: 65.7 wt % — Example 2

Agglomeration yield: 64.3 wt % — Example 3

Agglomeration yield: 67.8 wt % — Example 4

Agglomeration yield: 61.8 wt % — Example 5

Agglomeration yield: 65.0 wt % — Example 6

Agglomeration yield: 67.6 wt % — Example 7

Agglomeration yield: 70.9 wt % — Example 8

d_50 value: 386 nm — Example 1

d_50 value: 293 nm — Example 2

d_50 value: 390 nm — Example 3

d_50 value: 290 nm — Example 4

d_50 value: 385 nm — Example 5

d_50 value: 289 nm — Example 6

d_50 value: 380 nm — Example 7

d_50 value: 291 nm — Example 8

SAN ratio: 75:25 styrene to acrylonitrile — Thermoplastic Copolymer a

Viscosity number: 64 ml/g — Thermoplastic Copolymer a

Concentration: 5 g/l in dimethylformamide — Thermoplastic Copolymer a

Measurement temperature: 20° C. — Thermoplastic Copolymer a

Melt flow rate MVR: 64 ml/10 min — Thermoplastic Copolymer a

Melt flow measurement temperature: 220° C. — Thermoplastic Copolymer a

Load: 10 kg — Thermoplastic Copolymer a

Extrusion temperature: 200° C. to 250° C. — Thermoplastic Molding Compounds

Extruder speed: 700 rpm — Thermoplastic Molding Compounds

Batch size: 4 kg — Thermoplastic Molding Compounds

Medium & Water Role: The core reaction medium is an aqueous emulsion latex system for the graft substrate and agglomerating copolymer. Water is also used later for dilution and latex handling, and the examples include demineralized water additions and aqueous latex processing.

low acrylonitrile content: 10 to 30 wt % of acrylonitrile and/or methyl methacrylate in the graft sheath (B2)

#### Medium & Water Role

The core reaction medium is an aqueous emulsion latex system for the graft substrate and agglomerating copolymer. Water is also used later for dilution and latex handling, and the examples include demineralized water additions and aqueous latex processing.

#### low acrylonitrile content

10 to 30 wt % of acrylonitrile and/or methyl methacrylate in the graft sheath (B2)

#### Relevant Experimental Evidence

Example B1-1: Demonstrated aqueous emulsion polymerization of a butadiene/styrene graft substrate at 67° C. with 95% conversion.

Examples B1-2 to B1-4: Showed that increasing total styrene content from 14 to 28 wt % changes particle-size and gel metrics.

Agglomerating Copolymer C-1: Demonstrated emulsion polymerization of ethyl acrylate/methacrylamide copolymer in water for agglomeration.

Comparative Example C-2: Showed a similar agglomerating copolymer made with a different emulsifier loading and produced a 40.0 wt % latex solids product.

Example table data: Showed agglomerated graft substrates with d50 values around 289-390 nm and agglomeration yields around 61.8-70.9 wt %.

#### Technical Relevance

This patent is directly relevant because it discloses a butadiene-rich rubber substrate made by aqueous emulsion polymerization and a graft sheath containing acrylonitrile, which is the key compositional motif for low-acrylonitrile NBR-related materials. The staged feed strategy, water-rich medium, and control of styrene/butadiene ratio provide practical levers for tuning rubber composition and morphology.

### Patent Comparison Table

| Patent | Applicant | Medium & Water Role | low acrylonitrile content |
| --- | --- | --- | --- |
| US7592409B2 | Not available from source | The core reaction medium is an aqueous emulsion/microemulsion latex system. Water is explicitly used as the aqueous phase in emulsifier formation and polymerization, and the examples repeatedly describe water charges and latex formation. | Not disclosed in extracted evidence |
| US9624333B2 | Not available from source | The core reaction medium is an aqueous emulsion latex system for the graft substrate and agglomerating copolymer. Water is also used later for dilution and latex handling, and the examples include demineralized water additions and aqueous latex processing. | 10 to 30 wt % of acrylonitrile and/or methyl methacrylate in the graft sheath (B2) |

## 3. Cross-Patent Comparison & Synthesis Trends

US7592409B2 focuses on controlled aqueous emulsion/microemulsion polymerization with in-situ emulsifier formation and explicitly includes acrylonitrile-containing rubber blocks, whereas US9624333B2 uses conventional aqueous emulsion polymerization of a butadiene/styrene graft substrate followed by grafting with an acrylonitrile-containing sheath.

US7592409B2 discloses block-copolymer architecture (A-B-A triblock) and controlled radical methods (RAFT/NMP-type conditions), while US9624333B2 discloses graft copolymer architecture with agglomerated rubber substrate and SAN-type sheath.

Both patents rely on water as the polymerization medium, but US7592409B2 emphasizes microemulsion/latex formation from latent surfactant systems, while US9624333B2 emphasizes staged monomer feed, potassium stearate emulsification, and agglomeration of rubber particles.

For acrylonitrile content, US7592409B2 only states that the B block may comprise acrylonitrile and methacrylonitrile with 1,3-butadiene or isoprene, without a numeric ACN range; US9624333B2 explicitly sets the graft sheath at 10 to 30 wt % acrylonitrile and/or methyl methacrylate.

US9624333B2 provides the more direct low-ACN compositional guidance for NBR-related materials, while US7592409B2 is more of an enabling process patent for aqueous controlled polymerization of nitrile-rubber-containing blocks.

## 4. Conclusion

The evidence indicates that low-acrylonitrile NBR-related synthesis is most strongly supported by aqueous emulsion routes with staged monomer addition and surfactant/initiator control. US9624333B2 is the most compositionally relevant patent because it explicitly discloses an acrylonitrile-containing sheath at 10 to 30 wt % and a butadiene-rich emulsion-prepared rubber substrate, while US7592409B2 contributes a controlled microemulsion/block-copolymer methodology that can accommodate acrylonitrile/butadiene segments. Based on the extracted evidence, the most defensible synthesis direction for low-ACN NBR is water-based emulsion polymerization with controlled feed strategy, potassium persulfate initiation, and careful surfactant/soap stabilization; however, the exact low-ACN rubber grade range is not directly quantified in US7592409B2 and is only indirectly supported in US9624333B2 through the acrylonitrile-containing graft sheath.

## 5. References

US7592409B2 | Styrene acrylonitrile isoprene triblock copolymer | Not disclosed | US | 2009 | https://patents.google.com/patent/US7592409B2/en

US9624333B2 | Thermoplastic moulding materials based on acrylonitrile, styrene and butadiene | Not disclosed | US | 2017 | https://patents.google.com/patent/US9624333B2/en