# Low Styrene SBR Patent Landscape: Solution-Phase Styrene-Butadiene Rubber with Tin-Modified Continuous Polymerization

## 1. Abstract

This report synthesizes the patent evidence for low-styrene styrene-butadiene rubber (SBR) with emphasis on polymerization route, monomer feed, and process control. The selected patent landscape in the provided manifest is narrow and centers on a single primary patent, US6313232B1, which discloses continuous solution polymerization of a conjugated diene monomer or a diene/vinyl aromatic copolymer in hydrocarbon solvent using an organolithium initiator. Although the patent is not explicitly framed as a low-styrene invention, it is directly relevant because it covers butadiene/styrene copolymerization, the core chemistry used to make SBR, and it provides process conditions that influence copolymer architecture and downstream tire performance.

The disclosed synthesis approach is a continuous hydrocarbon-solution process with staged tin-compound addition during polymerization and again after withdrawal of the polymerization mixture. The patent emphasizes that adding tin compounds at 25–80% conversion, preferably 50–80%, and then again inline after reactor discharge improves hysteresis-related properties, including reduced Payne effect and lower tan delta at 50 °C. The evidence also identifies the use of organolithium initiators, hydrocarbon solvents such as hexane, and tin compounds including tin tetrachloride, dibutyltin dichloride, and tributyltin chloride. The examples show post-reaction termination with isopropanol, solvent removal by drum drying, and compounding with carbon black and conventional tire additives.

From a low-styrene SBR perspective, the patent is most useful as a process-control reference rather than a composition-specific low-styrene disclosure. It demonstrates how continuous solution polymerization and post-polymerization tin treatment can be used to tailor rubber performance in butadiene/styrene systems, which is relevant to industrial SBR grades where styrene content is adjusted to meet rolling resistance and wet traction targets.

## 2. Methodology

### Primary Patent Evidence

### Patent 1: US6313232B1 — Continuous addition of tin halides to solution SBR

| Patent Number | US6313232B1 |
| --- | --- |
| Title | Continuous addition of tin halides to solution SBR |
| Assignee | Bridgestone Corporation |
| Jurisdiction | US |
| Publication Year | 2001 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: The patent discloses continuous solution polymerization of a conjugated diene monomer or a mixture of a conjugated diene monomer and a vinyl aromatic hydrocarbon monomer in a hydrocarbon solvent using an organolithium initiator. A tin compound is added during polymerization at a specified conversion window and then added again after the polymerization mixture is withdrawn from the reactor, producing diene polymers with improved hysteresis-related properties.

Conversion at first tin addition: between 25% and 80% — Claims / synthesis passages

Preferred conversion at first tin addition: between 50% and 80% — Claims / synthesis passages

Polymerization medium: hydrocarbon solvent — Abstract / claims

Initiator: organolithium compound — Abstract / claims

Tin compound examples: tin tetrachloride, dibutyltin dichloride, tributyltin chloride — Claim 3 / synthesis passages

Polymer cement withdrawal: approximately 300-400 g portions — Comparative Example

Tin compound solution concentration: 10% by weight in hexane — Comparative Example

Tin addition amount: equivalent to 0.04 g active lithium per 100 g monomer — Comparative Example

Mixing time after tin addition: 15-30 minutes — Comparative Example

Compounding temperature: 90 °C — Comparative Example

Compounding temperature: 105 °C — Comparative Example

Dynastat test temperature: 50 °C — Comparative Example

Strain sweep test temperature: 25 °C — Comparative Example

Strain sweep start strain: 0.25% — Comparative Example

Strain sweep increment: 0.25% strain — Comparative Example

Strain sweep endpoint: 14.7% strain — Comparative Example

Sample dimensions: 9.3 mm diameter × 15.5 mm high — Comparative Example

Polymer molecular weight: greater than about 100,000 — synthesis passages

Medium & Water Role: Hydrocarbon-solution polymerization is the core reaction medium. No water-related process step disclosed in the extracted evidence.

styrene content below conventional SBR grades: Not disclosed in extracted evidence

#### Medium & Water Role

Hydrocarbon-solution polymerization is the core reaction medium. No water-related process step disclosed in the extracted evidence.

#### styrene content below conventional SBR grades

Not disclosed in extracted evidence

#### Relevant Experimental Evidence

Comparative Example: Post-withdrawal addition of Bu3SnCl or SnCl4 to polymer cement improved Dynastat and Payne-effect results versus control.

Comparative Example: Drum drying removed solvents before compounding.

Comparative Example: Repetition with other tin compounds reportedly gave substantially similar results.

#### Technical Relevance

This patent is relevant because it directly covers solution-polymerized butadiene/styrene copolymers, the standard SBR platform, and shows how staged tin treatment can improve tire-relevant properties. It does not explicitly define a low-styrene grade, but it provides a process route that can be applied to SBR compositions with reduced styrene content.

### Patent Comparison Table

| Patent | Applicant | Medium & Water Role | styrene content below conventional SBR grades |
| --- | --- | --- | --- |
| US6313232B1 | Bridgestone Corporation | Hydrocarbon-solution polymerization is the core reaction medium. No water-related process step disclosed in the extracted evidence. | Not disclosed in extracted evidence |

## 3. Cross-Patent Comparison & Synthesis Trends

Fewer than two selected primary patents were available, so cross-patent quantitative trends were not generated.

## 4. Conclusion

The manifest contains one primary patent, US6313232B1, which is a solution-polymerization process patent for butadiene/styrene copolymers rather than an explicit low-styrene composition patent. Its main contribution to the low-styrene SBR topic is process control: continuous hydrocarbon-solution polymerization with organolithium initiation and staged tin-compound addition to improve hysteresis, Payne effect, and rolling resistance in SBR-type elastomers.

## 5. References

US6313232B1 | Continuous addition of tin halides to solution SBR | Bridgestone Corporation | US | 2001 | https://patents.google.com/patent/US6313232B1/en