# PATENT RESEARCH REPORT

## 1. Abstract

The synthesis and formulation of low-to-medium acrylonitrile carboxylated nitrile butadiene rubber (XNBR) latexes are designed to mimic the physical properties of natural rubber—specifically high elongation, low modulus, and high tensile strength—for thin-walled elastomeric articles such as medical examination gloves. The patent landscape, represented by US9926439B2, US8470422B2, and EP2010602B1, establishes a core technology based on blending two distinct XNBR terpolymers to achieve synergistic mechanical and processing performance. The primary polymerization and formulation approach involves blending a first XNBR terpolymer (which provides a lower elastic modulus and softness) with a second XNBR terpolymer (which exhibits superior film-forming capabilities) in a compositional ratio ranging from 60:40 to 40:60, with a 50:50 ratio being preferred. The resulting blended polymer composition features a low-to-medium acrylonitrile content between 17% and 45% by weight, a methacrylic acid content of less than 15% by weight, and the remaining balance being butadiene. To achieve the desired elastomeric properties, a dual-crosslinking system is employed. Ionic crosslinking of the carboxylic acid groups is controlled using 0.5 to 1.5 parts of a metallic oxide (typically zinc oxide) combined with 0 to 1.5 parts of an alkali agent providing monovalent ions. Covalent crosslinking of the butadiene segments is achieved using 0.5 to 1.5 parts sulfur and 0.5 to 1.5 parts of a rubber accelerator system, specifically exemplified by a combination of 0.5 phr diphenyl guanidine (DPG), 0.25 phr zinc mercaptobenzothiazole (ZMBT), and 0.25 phr zinc diethyldithiocarbamate (ZDEC). Process trends highlight the control of glove thickness to a thin range of 0.05 to 0.11 mm to minimize the force required for stretching. Furthermore, EP2010602B1 introduces a post-polymerization surface modification involving an exterior coating of silicone emulsion, silicone oil, or glycerin, alongside a controlled drying temperature profile of 80°C to under 100°C to optimize surface release and tactile properties.

## 2. Primary Patent Evidence

### Patent 1: US9926439B2 — Nitrile rubber article having natural rubber characteristics

| Patent Number | US9926439B2 |
| --- | --- |
| Title | Nitrile rubber article having natural rubber characteristics |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2018-03-27 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Elongation: 400 % (400 % of Elongation)

Dpg: 0.5 phr (0.5 phr of Dpg)

Zmbt: 0.25 phr (0.25 phr of Zmbt)

Zdec: 0.25 phr (0.25 phr of Zdec)

#### Relevant Experimental Evidence

Example EXAMPLE 12: Elongation: 400 %, Dpg: 0.5 phr, Zmbt: 0.25 phr, Zdec: 0.25 phr

#### Technical Relevance

Selected via deterministic pipeline scoring.

### Patent 2: US8470422B2 — Nitrile rubber article having natural rubber characteristics

| Patent Number | US8470422B2 |
| --- | --- |
| Title | Nitrile rubber article having natural rubber characteristics |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2013-06-25 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Elongation: 400 % (400 % of Elongation)

Dpg: 0.5 phr (0.5 phr of Dpg)

Zmbt: 0.25 phr (0.25 phr of Zmbt)

Zdec: 0.25 phr (0.25 phr of Zdec)

#### Relevant Experimental Evidence

Example EXAMPLE 12: Elongation: 400 %, Dpg: 0.5 phr, Zmbt: 0.25 phr, Zdec: 0.25 phr

#### Technical Relevance

Selected via deterministic pipeline scoring.

### Patent 3: EP2010602B1 — Exterior-coated nitrile rubber article having natural rubber characteristics

| Patent Number | EP2010602B1 |
| --- | --- |
| Title | Exterior-coated nitrile rubber article having natural rubber characteristics |
| Assignee | Not available from source |
| Jurisdiction | EP |
| Publication Year | 2016-11-02 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Temperature: 80 °C (temperature ... 80 °C)

Elongation: 400 % (400 % of Elongation)

Dpg: 0.5 phr (0.5 phr of Dpg)

Zmbt: 0.25 phr (0.25 phr of Zmbt)

Zdec: 0.25 phr (0.25 phr of Zdec)

Modulus: 300 % (300 % of Modulus)

Strain: 300 % (300 % of Strain)

Extension: 400 % (400 % of Extension)

#### Relevant Experimental Evidence

Example EXAMPLE 12: Elongation: 400 %, Temperature: 80 °C, Dpg: 0.5 phr, Zmbt: 0.25 phr, Zdec: 0.25 phr, Modulus: 300 %, Strain: 300 %, Extension: 400 %

#### Technical Relevance

Selected via deterministic pipeline scoring.

## 3. Cross-Patent Comparison & Synthesis Trends

Monomer Content and Ratios: All three patents (US9926439B2, US8470422B2, and EP2010602B1) specify a carboxylated nitrile-butadiene rubber (XNBR) blend with an acrylonitrile (AN) content of 17% to 45% by weight and a methacrylic acid (MAA) content of less than 15% by weight, with butadiene making up the remainder.

Terpolymer Blending Strategy: The patents consistently employ a blend of two distinct XNBR terpolymers in a compositional ratio ranging from 60:40 to 40:60 (optimally 50:50). The first terpolymer is characterized by a lower elastic modulus to impart softness, while the second terpolymer exhibits superior film-forming properties to facilitate dip-processing.

Crosslinking and Vulcanization Systems: The formulation chemistry is identical across the documents, utilizing a dual-crosslinking system: ionic crosslinking via 0.5 to 1.5 parts of a metallic oxide (such as zinc oxide) combined with 0 to 1.5 parts of an alkali agent (total combined > 1.0 part), and covalent crosslinking via 0.5 to 1.5 parts sulfur and 0.5 to 1.5 parts of a multi-component accelerator system.

Specific Accelerator Package: The examples in all three patents specify a highly defined accelerator package consisting of 0.5 phr diphenyl guanidine (DPG), 0.25 phr zinc mercaptobenzothiazole (ZMBT), and 0.25 phr zinc diethyldithiocarbamate (ZDEC) to achieve optimal vulcanization kinetics and physical properties.

Key Distinctions and Process Innovations: While US9926439B2 and US8470422B2 focus on the core latex blend and glove article properties, EP2010602B1 introduces a critical post-processing step. It characterizes the elastomeric glove by an exterior coating of a silicone emulsion, silicone oil, glycerin solution, or fluorocarbon release agent, and specifies a drying temperature profile of 80°C to below 100°C for the gelled glove on the mold.

Physical Performance Targets: All three patents target a force-strain profile mimicking natural rubber, specifically achieving a low force at 400% elongation (typically 1.5 to 1.7 N compared to 1.3 N for natural rubber) and high tensile strength (30 to 58 MPa) at reduced glove thicknesses (0.05 to 0.11 mm).

## 4. Conclusion

The synthesis of low-acrylonitrile carboxylated nitrile butadiene rubber (XNBR) with natural rubber-like characteristics is successfully realized through a synergistic blending strategy. By combining a low-modulus XNBR terpolymer with a high-film-forming XNBR terpolymer in a 50:50 ratio, manufacturers can overcome the traditional trade-off between softness and processability. Recommended synthesis and formulation parameters derived from the patent evidence include maintaining an overall acrylonitrile content of 17-45 wt%, methacrylic acid content below 15 wt%, and utilizing a dual-crosslinking system comprising 0.5-1.5 phr zinc oxide, 0.5-1.5 phr sulfur, and a balanced accelerator package of 0.5 phr DPG, 0.25 phr ZMBT, and 0.25 phr ZDEC. Additionally, incorporating an exterior silicone or glycerin coating and maintaining drying temperatures between 80°C and 100°C optimizes the surface properties and structural integrity of the resulting thin-walled (0.05-0.11 mm) elastomeric articles.

## 5. References

US9926439B2 | Nitrile rubber article having natural rubber characteristics | Not disclosed | US | 2018 | https://patents.google.com/patent/US9926439B2/en

US8470422B2 | Nitrile rubber article having natural rubber characteristics | Not disclosed | US | 2013 | https://patents.google.com/patent/US8470422B2/en

EP2010602B1 | Exterior-coated nitrile rubber article having natural rubber characteristics | Not disclosed | EP | 2016 | https://patents.google.com/patent/EP2010602B1/en