# Low Acrylonitrile NBR Patent Landscape Report

## 1. Abstract

This report evaluates patent evidence relevant to low acrylonitrile nitrile butadiene rubber (NBR), with emphasis on composition control, monomer feed strategy, and emulsion polymerization process design. The target material is a butadiene-acrylonitrile copolymer with reduced acrylonitrile fraction relative to conventional NBR grades, typically achieved by controlling acrylonitrile feed, conversion profile, and reactor staging. In the provided manifest, only one primary patent was identified: US10208151B2. Although the patent is not directed to standalone low-ACN NBR, it is highly relevant because it discloses a diene-based rubber latex prepared by staged emulsion polymerization of 1,3-butadiene with controlled addition of emulsifier, initiator, electrolyte, molecular weight regulator, and cross-linking agent, followed by grafting with acrylonitrile/styrene to form ABS. The disclosed process demonstrates how rubber-phase latex properties can be tuned through monomer charge, cross-linker type, addition timing, temperature staging, and conversion endpoints. Key process trends include two-step polymerization, nitrogen-substituted reactor operation, use of potassium rosinate/potassium oleate emulsification, potassium persulfate initiation, tertiary dodecyl mercaptan molecular-weight control, and termination at high conversion (90%+). The examples show that changing the cross-linking agent from propylene glycol diacrylate n=7 to n=13 and adjusting addition timing changes gel content and particle size while preserving large latex particle size (~3100 Å). For low-ACN NBR synthesis, the patent is useful as a process-control reference for emulsion copolymerization and latex property management, even though it does not explicitly disclose low acrylonitrile NBR compositions.

## 2. Primary Patent Evidence

### Patent 1: US10208151B2 — Method for preparing large-size diene-based rubber latex and acrylonitrile- …

| Patent Number | US10208151B2 |
| --- | --- |
| Title | Method for preparing large-size diene-based rubber latex and acrylonitrile- … |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2019 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: The patent discloses a two-stage emulsion polymerization route to prepare large-size diene-based rubber latex from 1,3-butadiene, using staged monomer/emulsifier addition, potassium persulfate initiation, tertiary dodecyl mercaptan molecular-weight control, and a cross-linking agent of (propylene glycol)n diacrylate. The resulting latex is then used as the rubber phase for grafting acrylonitrile and styrene to make ABS copolymer powder and thermoplastic resin.

Ion exchanged water: 65 parts by weight — Example 1

1,3-butadiene: 75 parts by weight — Example 1

Potassium rosinate: 1 part by weight — Example 1

Potassium oleate: 1.5 parts by weight — Example 1

Potassium carbonate (K2CO3): 0.3 part by weight — Example 1

Tertiary dodecyl mercaptan (TDDM): 0.3 part by weight — Example 1

Potassium persulfate (K2S2O8): 0.3 part by weight — Example 1

(Propylene glycol)7 diacrylate: 0.2 part by weight — Example 1

Reaction temperature: 70° C — Example 1

First polymerization conversion rate: 40% — Example 1

Reaction temperature: 82° C — Example 1

Second polymerization conversion rate: 75% — Example 1

Final polymerization conversion rate: 93% — Example 1

Gel content: 78% — Example 1

Particle size: 3100 Å — Example 1

Diene-based rubber polymer: 60 parts by weight — Example 1

Ion exchanged water: 100 parts by weight — Example 1

Acrylonitrile: 10 parts by weight — Example 1

Styrene: 30 parts by weight — Example 1

Ion exchanged water: 25 parts by weight — Example 1

t-Butyl hydroperoxide: 0.12 part by weight — Example 1

Potassium rosinate: 1.0 part by weight — Example 1

Tertiary dodecyl mercaptan (TDDM): 0.3 part by weight — Example 1

Dextrose: 0.054 part by weight — Example 1

Sodium pyrophosphate: 0.004 part by weight — Example 1

Ferrous sulfate: 0.002 part by weight — Example 1

Reaction temperature: 70° C — Example 1 (ABS grafting)

Addition time: 3 hours — Example 1

Dextrose: 0.05 part by weight — Example 1

Sodium pyrophosphate: 0.03 part by weight — Example 1

Ferrous sulfate: 0.001 part by weight — Example 1

t-Butyl hydroperoxide: 0.05 part by weight — Example 1

Reaction temperature: 80° C — Example 1

Polymerization conversion rate: 97% — Example 1

Graft rate: 41% — Example 1

Coagulates content: 0.3% — Example 1

(Propylene glycol)13 diacrylate: 0.2 part by weight — Example 2

Gel content: 76% — Example 2

Particle size: 3100 Å — Example 2

(Propylene glycol)13 diacrylate: 0.2 part by weight — Example 3

(Propylene glycol)13 diacrylate: 0.1 part by weight — Example 3

Reaction temperature: 70° C — Example 3

First polymerization conversion rate: 40% — Example 3

Reaction temperature: 82° C — Example 3

Final polymerization conversion rate: 93% — Example 3

Gel content: 70% — Example 3

Particle size: 3100 Å — Example 3

Diene-based rubber latex: 40 wt% to 70 wt% — Claims

Aromatic vinyl compound: 20 wt% to 50 wt% — Claims

Vinyl cyanide compound: 10 wt% to 40 wt% — Claims

Conjugated diene-based monomer: 50 parts by weight to 75 parts by weight — Claims

Emulsifier: 1 part by weight to 3 parts by weight — Claims

Polymerization initiator: 0.1 part by weight to 0.4 part by weight — Claims

Electrolyte: 0.1 part by weight to 3 parts by weight — Claims

Molecular weight control agent: 0.1 part by weight to 0.5 part by weight — Claims

Ion exchanged water: 65 parts by weight to 100 parts by weight — Claims

Cross-linking agent: 0.05 part by weight to 0.3 part by weight — Claims

Balance monomer addition: 0 to 0.1 parts by weight emulsifier — Claims

Balance cross-linking agent: 0 to 0.2 parts by weight — Claims

Step 1 conversion point: 45% to 60% — Description

Step 3 termination conversion: 90% to 95% or higher — Description

Average particle diameter: 2,500 Å to 4,000 Å — Description

Gel content: 60% to 80% — Description

#### Relevant Experimental Evidence

Example 1: Produced large-size rubber latex with 78% gel content and 3100 Å particle size using (propylene glycol)7 diacrylate, then grafted acrylonitrile/styrene to ABS latex with 97% conversion and 41% graft rate.

Example 2: Replacing the cross-linker with (propylene glycol)13 diacrylate lowered gel content to 76% while maintaining 3100 Å particle size.

Example 3: Using (propylene glycol)13 diacrylate in a split-addition mode further reduced gel content to 70% while preserving 3100 Å particle size.

Comparative Example 1: A non-crosslinked latex was prepared for comparison and then used in ABS grafting.

Comparative Example 2: Adding polypropylene glycol diacrylate (Mn=6,000) at 0.2 part by weight produced a large-size latex of 3100 Å for comparison.

#### Technical Relevance

This patent is relevant because it provides a detailed emulsion-polymerization framework for controlling diene rubber latex morphology, conversion, and grafting behavior, all of which are important when designing low-ACN NBR or related nitrile rubber systems. While it does not explicitly claim low acrylonitrile NBR, its staged addition strategy and composition control principles are directly transferable to acrylonitrile/butadiene copolymer synthesis.

## 3. Cross-Patent Comparison & Synthesis Trends

No qualifying primary patents were identified under the configured target material relevance criteria. Cross-patent quantitative trends were therefore not generated.

## 4. Conclusion

The evidence base contains one primary patent, US10208151B2, which is not a direct low-acrylonitrile NBR disclosure but is technically useful for nitrile-rubber process design. The strongest transferable lessons are staged emulsion polymerization, controlled monomer and emulsifier addition, use of a molecular-weight regulator, and conversion-based termination to manage latex size and gel content. For low-ACN NBR synthesis, the most relevant evidence-supported process direction is careful feed-ratio control in emulsion polymerization, with staged addition and temperature management to maintain composition uniformity and polymer properties. However, no patent in the provided manifest explicitly discloses a low-acrylonitrile NBR composition, so any low-ACN target specification must be inferred from broader nitrile-rubber process principles rather than directly claimed composition data.

## 5. References

US10208151B2 | Method for preparing large-size diene-based rubber latex and acrylonitrile- … | Not disclosed | US | 2019 | https://patents.google.com/patent/US10208151B2/en