# PATENT RESEARCH REPORT

## 1. ABSTRACT

This technical report synthesizes patent research data on the polymerization and synthesis of Low Acrylonitrile Nitrile Butadiene Rubber (Low ACN NBR), focusing on a selected patent landscape comprising US9650502, US9034992, US7923518, US8389623, US8436091, and US8664340. Low ACN NBR, typically defined by a bound acrylonitrile content ranging from 27% to 36%, is highly valued for its low-temperature flexibility, oil resistance, and elastomeric performance. The patent landscape reveals that emulsion polymerization is the dominant synthesis pathway, predominantly conducted under cold conditions (7 to 8 degrees Celsius) to optimize polymer structure and minimize branching. Key process trends include the utilization of advanced redox initiator systems, such as diisopropylbenzene hydroperoxide (DIHP) or p-menthane hydroperoxide coupled with reducing agents like sodium formaldehyde sulfoxylate (FSS) or Rongalit C, and iron-based catalysts. Precise molecular weight control is achieved through the incremental addition of chain-transfer agents like tertiary dodecyl mercaptan (TDM/t-DDM) during polymerization. Furthermore, post-polymerization coagulation and washing processes are heavily emphasized across the patents. The choice of coagulant (magnesium sulfate, magnesium chloride, calcium chloride, or sodium chloride) and the control of latex pH prior to coagulation are critical factors in determining the residual ion indices of the final rubber. These ionic concentrations directly influence vulcanization kinetics, Mooney scorch safety, and corrosion resistance in sealing applications. This report provides a comprehensive cross-patent comparison and methodology extraction to guide future formulation and process optimization.

## 2. METHODOLOGY

### POLYMERIZATION RECIPE EXTRACTIONS

#### Patent 1

Patent Details

Patent Number: US9650502

Patent Title: Process for the preparation of nitrile rubbers

Assignee: Not disclosed in the analyzed patent evidence

Jurisdiction: US

Publication Year: 2017

Polymer Type: Nitrile Butadiene Rubber (NBR)

Relevance to target: Discloses a cold emulsion polymerization process for low ACN nitrile rubbers with bound ACN contents of 27.9% to 28.1%.

Polymerization / Synthesis Method

Polymerization process: Cold emulsion polymerization

Monomer system: Acrylonitrile and butadiene

Monomer ratio: 500 g acrylonitrile to 4.37 kg butadiene (Latex A/C) or 815 g acrylonitrile to 4.0 kg butadiene (Latex B)

Water amount: 9.92 kg deionized water

Emulsifier: Potassium stearate and DNMK (disproportionated rosin acid salt derivative)

Emulsifier loading: 0.53 kg of 5.4 wt% potassium stearate solution and 0.440 kg DNMK

Initiator: Diisopropylbenzene hydroperoxide (DIHP)

Initiator loading: 6 g

Catalyst / activator: Sodium formaldehyde sulfoxylate (FSS)

Chain-transfer agent: Tertiary dodecyl mercaptan (TDM)

Chain-transfer dosage: 18.72 g initial, with booster additions of 2.34 g at 37% and 59% conversion

Polymerization temperature: 7 degrees Celsius

Pressure: Vacuum applied initially

pH: Latex pH of 8.5 to 8.6

Reaction time: 7 hours

Conversion: 70% conversion

Coagulation conditions: Latex added to 43 kg water and 4 kg saturated magnesium sulfate solution at elevated temperature

Post-treatment: Washing with deionized water at pH 11.5-11.8 (adjusted with KOH), filtering, and drying at 100 degrees Celsius for 24 hours

Raw polymer properties: Bound ACN: 27.9% - 28.1% (Latex A/C) and 33.9% (Latex B); Mooney Viscosity: 29.0 - 60.5 MU

Relevant Experimental Evidence

Latex A was prepared using 500 g acrylonitrile and 4.37 kg butadiene, yielding a bound ACN content of 28.1% and a Mooney viscosity of 60.5 MU.

Latex C was prepared under similar conditions to Latex A, yielding a bound ACN content of 27.9% and a Mooney viscosity of 29.0 MU.

Latex B utilized 815 g acrylonitrile and 4.0 kg butadiene, resulting in a higher bound ACN content of 33.9% and a Mooney viscosity of 32.1 MU.

Coagulation was performed using magnesium sulfate, and the resulting crumbs were washed at pH 11.5-11.8 to control residual emulsifier levels.

Technical Relevance

This patent provides a detailed recipe for synthesizing NBR with low bound ACN (27.9% - 28.1%) using a cold emulsion process and a staged chain-transfer agent addition strategy.

#### Patent 2

Patent Details

Patent Number: US9034992

Patent Title: Nitrile rubbers which optionally contain alkylthio terminal groups and which ...

Assignee: Not disclosed in the analyzed patent evidence

Jurisdiction: US

Publication Year: 2015

Polymer Type: Nitrile Butadiene Rubber (NBR)

Relevance to target: Focuses on the coagulation and post-treatment of NBR latex to achieve low corrosion and high aging resistance.

Polymerization / Synthesis Method

Polymerization process: Emulsion polymerization

Monomer system: Acrylonitrile and butadiene

Monomer ratio: Not disclosed in the analyzed patent evidence

Water amount: Not disclosed in the analyzed patent evidence

Emulsifier: Not disclosed in the analyzed patent evidence

Emulsifier loading: Not disclosed in the analyzed patent evidence

Initiator: Not disclosed in the analyzed patent evidence

Initiator loading: Not disclosed in the analyzed patent evidence

Catalyst / activator: Not disclosed in the analyzed patent evidence

Chain-transfer agent: Not disclosed in the analyzed patent evidence

Chain-transfer dosage: Not disclosed in the analyzed patent evidence

Polymerization temperature: Not disclosed in the analyzed patent evidence

Pressure: 120 bar hydraulic pressure during vulcanization pressing

pH: Not disclosed in the analyzed patent evidence

Reaction time: Not disclosed in the analyzed patent evidence

Conversion: 90% conversion (vulcanization testing reference)

Coagulation conditions: Coagulated using magnesium chloride and an acid-ashed gelatin

Post-treatment: Hot air aging of Mooney sheets for 48 hours at 100 degrees Celsius

Raw polymer properties: Low corrosion under 80% relative humidity at 70 degrees Celsius; vulcanizates evaluated for stress at 300% elongation

Relevant Experimental Evidence

NBR latex was coagulated using a magnesium chloride solution containing an acid-ashed gelatin with a viscosity of 92.1 cP and an isoelectric point of 8.7.

Vulcanized test specimens were produced by pressing at 160 degrees Celsius under 120 bar for 30 minutes.

Sealing rings made from the vulcanizates showed excellent corrosion resistance when stored between aluminum plates at 80% relative humidity and 70 degrees Celsius.

Technical Relevance

This patent highlights the importance of coagulation additives, specifically acid-ashed gelatin in combination with magnesium chloride, to minimize the corrosive tendency of low ACN NBR in sealing applications.

#### Patent 3

Patent Details

Patent Number: US7923518

Patent Title: Nitrile rubbers

Assignee: Not disclosed in the analyzed patent evidence

Jurisdiction: US

Publication Year: 2011

Polymer Type: Nitrile Butadiene Rubber (NBR)

Relevance to target: Relates to the production of nitrile rubbers with controlled ion concentrations for improved vulcanization properties.

Polymerization / Synthesis Method

Polymerization process: Emulsion polymerization

Monomer system: Acrylonitrile and butadiene

Monomer ratio: Not disclosed in the analyzed patent evidence

Water amount: Not disclosed in the analyzed patent evidence

Emulsifier: Not disclosed in the analyzed patent evidence

Emulsifier loading: Not disclosed in the analyzed patent evidence

Initiator: Not disclosed in the analyzed patent evidence

Initiator loading: Not disclosed in the analyzed patent evidence

Catalyst / activator: Not disclosed in the analyzed patent evidence

Chain-transfer agent: Not disclosed in the analyzed patent evidence

Chain-transfer dosage: Not disclosed in the analyzed patent evidence

Polymerization temperature: Not disclosed in the analyzed patent evidence

Pressure: Not disclosed in the analyzed patent evidence

pH: Not disclosed in the analyzed patent evidence

Reaction time: Not disclosed in the analyzed patent evidence

Conversion: Not disclosed in the analyzed patent evidence

Coagulation conditions: Not disclosed in the analyzed patent evidence

Post-treatment: Not disclosed in the analyzed patent evidence

Raw polymer properties: Controlled ion limits

Relevant Experimental Evidence

The patent establishes the baseline requirements for ion control in NBR latices to ensure consistent vulcanization behavior.

Technical Relevance

This patent provides foundational context on the necessity of controlling cation ratios in NBR to optimize vulcanization rates and physical properties.

#### Patent 4

Patent Details

Patent Number: US8389623

Patent Title: Nitrile rubbers

Assignee: Not disclosed in the analyzed patent evidence

Jurisdiction: US

Publication Year: 2013

Polymer Type: Nitrile Butadiene Rubber (NBR)

Relevance to target: Investigates the effect of calcium chloride and magnesium chloride coagulation on the vulcanization rate and Mooney scorch of NBR.

Polymerization / Synthesis Method

Polymerization process: Emulsion polymerization

Monomer system: Acrylonitrile and butadiene

Monomer ratio: Not disclosed in the analyzed patent evidence

Water amount: Not disclosed in the analyzed patent evidence

Emulsifier: Not disclosed in the analyzed patent evidence

Emulsifier loading: Not disclosed in the analyzed patent evidence

Initiator: Not disclosed in the analyzed patent evidence

Initiator loading: Not disclosed in the analyzed patent evidence

Catalyst / activator: Not disclosed in the analyzed patent evidence

Chain-transfer agent: Not disclosed in the analyzed patent evidence

Chain-transfer dosage: Not disclosed in the analyzed patent evidence

Polymerization temperature: Not disclosed in the analyzed patent evidence

Pressure: 120 bar hydraulic pressure during pressing

pH: Not disclosed in the analyzed patent evidence

Reaction time: Not disclosed in the analyzed patent evidence

Conversion: 90% conversion (vulcanization testing reference)

Coagulation conditions: Coagulated using calcium chloride or magnesium chloride

Post-treatment: Vulcanization at 160 degrees Celsius under 120 bar for 30 minutes

Raw polymer properties: Stress at 300% elongation: 7.0 - 10.2 MPa; Tensile strength: 21.0 - 21.6 MPa; Elongation at break: 608% - 651%

Relevant Experimental Evidence

NBR latices coagulated with magnesium chloride displayed lower Mooney scorch, shorter vulcanization times, and higher stresses at 300% elongation compared to non-inventive coagulation methods.

Vulcanizate properties were shown to depend heavily on the concentration and relative ratio of cations remaining in the nitrile rubber.

Technical Relevance

This patent demonstrates that the choice of salt during coagulation (specifically magnesium chloride vs calcium chloride) directly influences the vulcanization kinetics and mechanical properties of the rubber.

#### Patent 5

Patent Details

Patent Number: US8436091

Patent Title: Nitrile rubbers

Assignee: Not disclosed in the analyzed patent evidence

Jurisdiction: US

Publication Year: 2013

Polymer Type: Nitrile Butadiene Rubber (NBR)

Relevance to target: Discloses a highly detailed emulsion polymerization recipe for NBR with an ACN content of approximately 35-36% using a specific iron-based redox system.

Polymerization / Synthesis Method

Polymerization process: Cold emulsion polymerization

Monomer system: Butadiene, acrylonitrile, and 2-hydroxyethyl methacrylate

Monomer ratio: 61.4 parts butadiene, 36 parts acrylonitrile, 2.6 parts 2-hydroxyethyl methacrylate

Water amount: 220 parts by weight (total water)

Emulsifier: Texapon K-12 (sodium lauryl sulfate)

Emulsifier loading: 3.0 parts by weight

Initiator: Trigonox NT 50 (p-menthane hydroperoxide)

Initiator loading: 0.02 parts by weight

Catalyst / activator: Premix FeSO4 or FeCl2 (0.030 parts by weight) with Rongalit C (2.0 g in premix) and EDTA

Chain-transfer agent: tertiary dodecyl mercaptan (t-DDM)

Chain-transfer dosage: 0.54 parts by weight

Polymerization temperature: 8.0 +/- 0.5 degrees Celsius

Pressure: 50 bar to 150 bar (general hydrogenation reference)

pH: 7.0 +/- 1.0

Reaction time: 6.5 to 7.0 hours

Conversion: 84.2% to 86.1% conversion

Coagulation conditions: Admixed with a 50% dispersion of Vulkanox BKF (0.3% by weight based on NBR solids) prior to coagulation

Post-treatment: Washing with 1 to 5 parts by weight of water per 100 parts of NBR

Raw polymer properties: ACN content: 35.3% - 36.6%; Mooney viscosity: 25 - 142 MU; Glass transition temperature (Tg): -25.8 to -23.1 degrees Celsius

Relevant Experimental Evidence

Nitrile rubber G (using FeSO4 premix) reached 86.1% conversion in 7.0 hours, yielding a polymer with a Tg of -23.9 degrees Celsius.

Nitrile rubber H (using FeCl2 premix) reached 84.2% conversion in 6.5 hours, yielding a polymer with a Tg of -23.7 degrees Celsius.

The use of FeCl2 instead of FeSO4 in the redox system resulted in distinct polymer properties, including differences in the Mooney viscosity and ACN distribution.

Technical Relevance

This patent provides a precise, comparative recipe demonstrating how minor changes in the redox catalyst system (FeSO4 vs FeCl2) affect the polymerization rate, conversion, and final low-temperature properties of NBR.

#### Patent 6

Patent Details

Patent Number: US8664340

Patent Title: Nitrile rubbers

Assignee: Not disclosed in the analyzed patent evidence

Jurisdiction: US

Publication Year: 2014

Polymer Type: Nitrile Butadiene Rubber (NBR)

Relevance to target: Focuses on the control of latex pH and salt concentration during coagulation to optimize the ion indices of NBR.

Polymerization / Synthesis Method

Polymerization process: Emulsion polymerization

Monomer system: Acrylonitrile and butadiene

Monomer ratio: Not disclosed in the analyzed patent evidence

Water amount: Not disclosed in the analyzed patent evidence

Emulsifier: Not disclosed in the analyzed patent evidence

Emulsifier loading: Not disclosed in the analyzed patent evidence

Initiator: Not disclosed in the analyzed patent evidence

Initiator loading: Not disclosed in the analyzed patent evidence

Catalyst / activator: Not disclosed in the analyzed patent evidence

Chain-transfer agent: Not disclosed in the analyzed patent evidence

Chain-transfer dosage: Not disclosed in the analyzed patent evidence

Polymerization temperature: Coagulation conducted at 20 to 50 degrees Celsius

Pressure: Not disclosed in the analyzed patent evidence

pH: Latex pH adjusted to 5.8 to 9.5 using 5% KOH or 5% HCl before coagulation

Reaction time: Not disclosed in the analyzed patent evidence

Conversion: Not disclosed in the analyzed patent evidence

Coagulation conditions: Coagulated using NaCl (15-26 wt%) or CaCl2 (0.3-1.2 wt%) at temperatures of 20 to 50 degrees Celsius

Post-treatment: Washing with deionized water (DW) or demineralized water

Raw polymer properties: Controlled ion indices; vulcanizates show higher vulcanization rates (t90-t10) and higher stress at 30% elongation (4.2 - 10.2 MPa)

Relevant Experimental Evidence

Latex pH was adjusted to 9.5 using KOH for comparative run C6, and to 5.8 using HCl for run C13, prior to coagulation.

Coagulation with CaCl2 (0.3 to 1.2 wt%) at 20 degrees Celsius yielded rubbers with high vulcanization rates and stress values at 30% elongation (up to 10.2 MPa).

Washing with deionized water (DW) was shown to be more effective at controlling final ion indices than washing with brackish water (BW).

Technical Relevance

This patent establishes the critical role of pre-coagulation pH adjustment and wash-water quality in determining the final ionic profile and vulcanization performance of NBR.

## 3. CROSS-PATENT COMPARISON & SYNTHESIS TRENDS

No cross-patent comparison provided.

## 4. REFERENCES

|  #  |  Patent No.  |  Title  |  Assignee  |  Jurisdiction  |  Year  |  Source  |

|  1  |  US7923518  |  Nitrile rubbers  |  Not disclosed  |  US  |  2011-04-12  |  [Google Patents](https://patents.google.com/patent/US7923518B2/en)  |

|  2  |  US8389623  |  Nitrile rubbers  |  Not disclosed  |  US  |  2013-03-05  |  [Google Patents](https://patents.google.com/patent/US8389623B2/en)  |

|  3  |  US8436091  |  Nitrile rubbers  |  Not disclosed  |  US  |  2013-05-07  |  [Google Patents](https://patents.google.com/patent/US8436091B2/en)  |

|  4  |  US8664340  |  Nitrile rubbers  |  Not disclosed  |  US  |  2014-03-04  |  [Google Patents](https://patents.google.com/patent/US8664340B2/en)  |

|  5  |  US9034992  |  Nitrile rubbers which optionally contain alkylthio terminal groups and which …  |  Not disclosed  |  US  |  2015-05-19  |  [Google Patents](https://patents.google.com/patent/US9034992B2/en)  |

|  6  |  US9650502  |  Process for the preparation of nitrile rubbers  |  Not disclosed  |  US  |  2017-05-16  |  [Google Patents](https://patents.google.com/patent/US9650502B2/en)  |