# LOW ACRYLONITRILE NBR

## 1. ABSTRACT

This report provides a technical summary of the research scope, definition of Low Acrylonitrile NBR, selected patent landscape, major polymerization approaches, and major formulation/process trends. The target compound, Low Acrylonitrile NBR, is a type of nitrile rubber with a low acrylonitrile content. The selected patent landscape includes patents related to the synthesis and properties of Low Acrylonitrile NBR. The major polymerization approaches include emulsion polymerization and metathesis reactions. The major formulation/process trends include the use of catalysts, solvents, and co-olefins to control the polymerization process and properties of the resulting polymer.

## 2. METHODOLOGY

### POLYMERIZATION RECIPE EXTRACTIONS

#### Patent 1

Patent Details

Patent Number: US7105606

Patent Title: Polymer blends comprising low molecular weight nitrile rubber

Assignee: Not disclosed

Jurisdiction: US

Publication Year: 2006-09-12

Polymer Type: Nitrile rubber

Relevance to target: The patent is relevant to Low Acrylonitrile NBR as it describes the synthesis and properties of low molecular weight nitrile rubber, which is a type of Low Acrylonitrile NBR.

Polymerization / Synthesis Method

Polymerization process: Metathesis reactions

Monomer system: Butadiene-acrylonitrile terpolymer

Monomer ratio: Butadiene content of 47 mol %, an acrylonitrile content of 21 mol %, a butylacrylate content of 32 mol %

Water amount: Not disclosed in the analyzed patent evidence

Emulsifier: Not disclosed in the analyzed patent evidence

Emulsifier loading: Not disclosed in the analyzed patent evidence

Initiator: Wilkinson's catalyst

Initiator loading: 0.08 phr

Catalyst / activator: Triphenylphosphine

Chain-transfer agent: Not disclosed in the analyzed patent evidence

Chain-transfer dosage: Not disclosed in the analyzed patent evidence

Polymerization temperature: 80° C

Pressure: 500 psi

pH: Not disclosed in the analyzed patent evidence

Reaction time: 30 minutes

Conversion: Not disclosed in the analyzed patent evidence

Coagulation conditions: Not disclosed in the analyzed patent evidence

Post-treatment: Degassed 3 times with H2 (100 psi) under full agitation

Raw polymer properties: Mooney viscosity of 55 (ML 1+4 @ 100° C.) and a RDB of 18%

Relevant Experimental Evidence

Viscosity: 18 %

Bht: 0.025 %

Time: 30 minutes

Co-ol: 6 %

Sol: 0.5 phr

Cements: 6 %

Viscosity: 6 %

Triphenylphosphine: 0.08 phr

Sol: 1 phr

All: 99.6 %

Alternatively: 99.3 %

Solid Content: 6 %

Technical Relevance

This patent is relevant to Low Acrylonitrile NBR as it describes the synthesis and properties of low molecular weight nitrile rubber, which is a type of Low Acrylonitrile NBR. The patent provides information on the monomer system, polymerization process, and properties of the resulting polymer, which can be used to inform the development of Low Acrylonitrile NBR.

## 3. CROSS-PATENT COMPARISON & SYNTHESIS TRENDS

The selected patent (US7105606) describes the synthesis and properties of low molecular weight nitrile rubber, which is a type of Low Acrylonitrile NBR.

The patent uses metathesis reactions to synthesize the polymer, with a butadiene content of 47 mol %, an acrylonitrile content of 21 mol %, and a butylacrylate content of 32 mol %.

The polymerization process involves the use of Wilkinson's catalyst and triphenylphosphine, with a reaction time of 30 minutes and a temperature of 80° C.

The resulting polymer has a Mooney viscosity of 55 (ML 1+4 @ 100° C.) and a RDB of 18%.

## 4. REFERENCES

[US7105606](https://patents.google.com/patent/US7105606)