# Low Acrylonitrile NBR

## POLYMERIZATION / SYNTHESIS PATENT RESEARCH REPORT

### Abstract

The patent landscape for Low Acrylonitrile NBR (nitrile butadiene rubber) synthesis reveals a focus on emulsion polymerization processes. The majority of patents disclose the use of acrylonitrile, butadiene, and optionally methacrylic acid as monomers. Initiator systems, such as redox systems, are employed to facilitate polymerization. Emulsifier selection and loading are critical factors, with anionic surfactants being commonly used. The monomer ratio, particularly the acrylonitrile content, is carefully controlled to achieve desired properties. Coagulation and post-treatment conditions, including the use of coagulants and adjustment of total solids content, are also important considerations. The resulting Low Acrylonitrile NBR polymers exhibit a range of properties, including solid content, Mooney viscosity, and tensile properties. Overall, the patents demonstrate a trend towards developing Low Acrylonitrile NBR with improved performance and versatility.

### Methodology

#### EP2316860 - Nitrile rubbers

Process: emulsion polymerization

Monomers: at least one alpha,beta-unsaturated nitrile, at least one conjugated diene and optionally at least one further copolymerizable monomer

Monomer ratio: Not disclosed

Initiator: redox system, which comprises (a) at least one peroxo compound as an oxidizing agent, (b) at least a reducing agent and (c) iron(II)chloride

Emulsifier: Not disclosed

Catalyst: Not disclosed

Chain transfer agent: Not disclosed

Coagulation: Not disclosed

Water amount: Not disclosed

#### US9926439 - Nitrile rubber article having natural rubber characteristics

Process: emulsion

Monomers: acrylonitrile, butadiene, methacrylic acid

Monomer ratio: acrylonitrile content between 17 and 45% by weight, methacrylic acid content less than 15% by weight, remaining balance butadiene

Initiator: Not disclosed

Emulsifier: anionic surfactant

Catalyst: zinc oxide

Chain transfer agent: Not disclosed

Coagulation: Not disclosed

Water amount: Not disclosed

#### EP2507313 - Elastomeric rubber and rubber products without the use of vulcanizing …

Process: emulsion

Monomers: carboxylated acrylonitrile butadiene

Monomer ratio: Not disclosed

Initiator: Not disclosed

Emulsifier: Not disclosed

Catalyst: Not disclosed

Chain transfer agent: Not disclosed

Coagulation: coagulant dipping process

Water amount: adjust to TSC 20-21%

### Cross-Patent Comparison & Synthesis Trends

#### Emulsifier Selection and Loading

Anionic surfactants are commonly used as emulsifiers in Low Acrylonitrile NBR synthesis. However, the specific emulsifier selection and loading are not consistently disclosed across the patents.

#### Initiator and Chain Transfer Agent Strategies

Redox systems, comprising peroxo compounds, reducing agents, and iron(II)chloride, are employed as initiators. Chain transfer agents are not consistently disclosed.

#### Monomer Ratio and Reaction Control

The monomer ratio, particularly the acrylonitrile content, is critical in achieving desired properties. Acrylonitrile content is controlled between 17 and 45% by weight in some patents.

#### Coagulation and Post-Treatment Conditions

Coagulation conditions, including the use of coagulants and adjustment of total solids content, are important considerations. The coagulant dipping process is used in one patent, while others adjust the total solids content to specific ranges.

### References

|  Patent Number  |  Patent Title  |  Assignee  |  Jurisdiction  |  Publication Year  |  Google Patents URL  |

| --- | --- | --- | --- | --- | --- |

|  EP2316860  |  Nitrile rubbers  |  Not disclosed  |  EP  |  2012  |  [https://patents.google.com/patent/EP2316860B1/en](https://patents.google.com/patent/EP2316860B1/en)  |

|  US9926439  |  Nitrile rubber article having natural rubber characteristics  |  Not disclosed  |  US  |  2018  |  [https://patents.google.com/patent/US9926439B2/en](https://patents.google.com/patent/US9926439B2/en)  |

|  EP2507313  |  Elastomeric rubber and rubber products without the use of vulcanizing …  |  Not disclosed  |  EP  |  2018  |  [https://patents.google.com/patent/EP2507313B1/en](https://patents.google.com/patent/EP2507313B1/en)  |