# Low Acrylonitrile NBR Patent Report: Evidence from US11347156B2

## 1. Abstract

This report synthesizes the patent evidence available in the required manifest for low acrylonitrile NBR, with the manifest containing a single primary patent: US11347156B2. The patent is not directed to NBR synthesis or monomer-feed control; instead, it concerns an electro-conductive member for electrophotography that uses a matrix-domain rubber architecture. Within that architecture, acrylonitrile-butadiene rubber (NBR) appears as one of the candidate diene-based rubbers for either the matrix or the domains, paired with styrene-butadiene rubber (SBR) in the complementary phase. The extracted evidence includes explicit nitrile-content values for several commercial NBR grades used as reference materials in the examples, ranging from 15% to 41.5%, which provides context for low- versus higher-acrylonitrile grades, but these values are not disclosed as properties of the claimed target material itself. The patent’s core technical contribution is phase-separated rubber design: a first rubber composition forms the matrix, a second rubber composition forms conductive domains, and the two rubbers are selected to differ in monomer units and to have controlled solubility-parameter separation and viscoelastic matching. The examples emphasize formulation-driven performance rather than polymerization chemistry, using NBR, SBR, IR, BR, EPDM, CR, and hydrin as raw rubbers, along with carbon black, sulfur, and vulcanization accelerators. Water is not part of the polymerization process because no polymerization is disclosed; the evidence instead shows dry compounding, molding, and evaluation of electro-conductive members. Overall, the patent is only indirectly relevant to low acrylonitrile NBR because it documents NBR grades and their use in a functional rubber composition, but it does not disclose NBR preparation, acrylonitrile feed control, or synthesis conditions for low-acrylonitrile NBR.

## 2. Methodology

### Primary Patent Evidence

### Patent 1: US11347156B2 — Electro-conductive member for electrophotography, process cartridge for …

| Patent Number | US11347156B2 |
| --- | --- |
| Title | Electro-conductive member for electrophotography, process cartridge for … |
| Assignee | Canon Kabushiki Kaisha |
| Jurisdiction | US |
| Publication Year | 2022 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: This patent does not disclose NBR synthesis or polymerization; it discloses fabrication of an electro-conductive member by compounding rubber compositions into a matrix-domain structure and molding them onto an electro-conductive support. NBR is used as one of the rubber materials in the examples and claims, paired with SBR in the complementary phase.

Nitrile content: 15% — Example section, NBR (1) JSR NBR N260S

SP value: 17.2 (J/cm3)0.5 — Example section, NBR (1) JSR NBR N260S

Nitrile content: 41.5% — Example section, NBR (2) JSR NBR N220S

SP value: 20.6 (J/cm3)0.5 — Example section, NBR (2) JSR NBR N220S

Nitrile content: 27.5% — Example section, NBR (3) Nipol DN302

SP value: 18.8 (J/cm3)0.5 — Example section, NBR (3) Nipol DN302

Nitrile content: 18.0% — Example section, NBR (4) Nipol DN401LL

SP value: 17.4 (J/cm3)0.5 — Example section, NBR (4) Nipol DN401LL

Nitrile content: 35% — Example section, NBR (5) Nipol N230S

SP value: 20.0 (J/cm3)0.5 — Example section, NBR (5) Nipol N230S

Nitrile content: 40.0% — Example section, NBR (6) JSR NBR N202S

SP value: 20.4 (J/cm3)0.5 — Example section, NBR (6) JSR NBR N202S

Raw rubber: NBR 100 parts by mass — Example 1, Table 1

Raw rubber: Unvulcanized domain composition 30 parts by mass — Example 1, Table 2

Raw rubber: Polyisoprene 70 parts by mass — Example 1, Table 2

Filler: Calcium carbonate 40 parts by mass — Example 1, Table 2

Vulcanization accelerating aid: Zinc oxide 5 parts by mass — Example 1, Table 2

Processing aid: Zinc stearate 2 parts by mass — Example 1, Table 2

Vulcanizing agent: Dispersive sulfur 3 parts by mass — Example 1, Table 3

Vulcanization accelerator (1): Di-2-benzothiazolyl disulfide 2 parts by mass — Example 1, Table 3

Vulcanization accelerator (2): Tetramethylthiuram disulfide 0.5 parts by mass — Example 1, Table 3

Electro-conductive particles in domains: 50 to 150 parts by mass per 100 parts by mass of the second rubber — Claim 1

Difference of absolute values of SP values: 0.2 to 4.0 (J/cm3)0.5 — Claim 1

tan δ1/tan δ2: 0.45 to 2.00 — Claim 1

Temperature: 23° C. — claim/evaluation context

Relative humidity: 50% — claim/evaluation context

Frequency: 80 Hz — claim/evaluation context

Domain volume fraction: 28.7 vol% — Table 5-1, Example 1

tanδ1/tanδ2 (A): 0.57 — Table 5-1, Example 1

tanδ1/tanδ2 (B): 0.23 — Table 5-1, Example 1

Domain volume fraction: 29.1 vol% — Table 5-1, Example 2

tanδ1/tanδ2 (A): 0.46 — Table 5-1, Example 2

tanδ1/tanδ2 (B): 0.17 — Table 5-1, Example 2

Domain volume fraction: 28.9 vol% — Table 5-1, Example 3

tanδ1/tanδ2 (A): 0.50 — Table 5-1, Example 3

tanδ1/tanδ2 (B): 0.21 — Table 5-1, Example 3

Domain volume fraction: 20.6 vol% — Table 5-1, Example 22

tanδ1/tanδ2 (A): 1.00 — Table 5-1, Example 22

tanδ1/tanδ2 (B): 1.38 — Table 5-1, Example 22

Domain volume fraction: 30.6 vol% — Table 5-1, Example 26

tanδ1/tanδ2 (A): 0.67 — Table 5-1, Example 26

tanδ1/tanδ2 (B): 0.52 — Table 5-1, Example 26

Domain volume fraction: 19.4 vol% — Table 5-1, Example 30

tanδ1/tanδ2 (A): 0.96 — Table 5-1, Example 30

tanδ1/tanδ2 (B): 1.87 — Table 5-1, Example 30

Temperature: 23° C. — Example 40 evaluation

Relative humidity: 50% — Example 40 evaluation

Abutting pressure: 1250 gf (12.26 N) — Example 40 evaluation

Output speed: 370 mm/sec — Example 40 evaluation

Image resolution: 1,200 dpi — Example 40 evaluation

Printing rate: 1.0% — Example 40 evaluation

Continuous output: 20000 sheets — Example 40 evaluation

Rest time: 12 hours — Example 40 evaluation

Conditioning time: 48 hours — Example 40 evaluation

Medium & Water Role: No polymerization medium is disclosed. Water is not used in synthesis, but the evaluation conditions explicitly include 23° C. and 50% relative humidity; no aqueous polymerization, coagulation, washing, or latex step is disclosed in the extracted evidence.

low acrylonitrile content: Not disclosed in extracted evidence

#### Medium & Water Role

No polymerization medium is disclosed. Water is not used in synthesis, but the evaluation conditions explicitly include 23° C. and 50% relative humidity; no aqueous polymerization, coagulation, washing, or latex step is disclosed in the extracted evidence.

#### low acrylonitrile content

Not disclosed in extracted evidence

#### Relevant Experimental Evidence

Comparative Example 3: NBR was used as the matrix rubber with EPDM as the domain rubber, showing poor discharge-related performance due to large SP mismatch.

Comparative Example 5: NBR was used as the matrix rubber with SBR as the domain rubber, but the accelerator choice led to an unfavorable tan δ1/tan δ2 balance.

Comparative Example 6: NBR was used for both domain and matrix, and the matrix-domain structure could not be confirmed.

Example 1: NBR was used as the raw rubber in the domain composition, and the member was fabricated by kneading, molding, and evaluation.

Examples 2 to 39: multiple rubber pairings were compared, including NBR/SBR combinations, to correlate SP difference and viscoelasticity with image performance.

#### Technical Relevance

This patent is relevant only as an application-side reference because it explicitly includes NBR grades and shows how NBR can be formulated in a phase-separated rubber structure. It does not disclose low-acrylonitrile NBR synthesis, but it provides composition context for NBR materials with nitrile contents as low as 15% in the example set.

### Patent Comparison Table

| Patent | Applicant | Medium & Water Role | low acrylonitrile content |
| --- | --- | --- | --- |
| US11347156B2 | Canon Kabushiki Kaisha | No polymerization medium is disclosed. Water is not used in synthesis, but the evaluation conditions explicitly include 23° C. and 50% relative humidity; no aqueous polymerization, coagulation, washing, or latex step is disclosed in the extracted evidence. | Not disclosed in extracted evidence |

## 3. Cross-Patent Comparison & Synthesis Trends

Fewer than two selected primary patents were available, so cross-patent quantitative trends were not generated.

## 4. Conclusion

The single primary patent in the manifest, US11347156B2, is not a synthesis patent for low-acrylonitrile NBR; it is a formulation and device patent that uses NBR as one of several rubber materials in a matrix-domain electro-conductive member. The evidence provides useful compositional context, including explicit nitrile contents for several commercial NBR grades, but it does not disclose preparation conditions, monomer feed ratios, or polymerization routes for low-acrylonitrile NBR.

## 5. References

US11347156B2 | Electro-conductive member for electrophotography, process cartridge for … | Canon Kabushiki Kaisha | US | 2022 | https://patents.google.com/patent/US11347156B2/en