# Low Acrylonitrile NBR

## POLYMERIZATION / SYNTHESIS PATENT RESEARCH REPORT

### Abstract

The patent landscape for Low Acrylonitrile NBR (Nitrile Butadiene Rubber) synthesis reveals a focus on emulsion polymerization processes. The majority of patents disclose the use of specific emulsifiers, initiators, and chain transfer agents to control the polymerization reaction. The acrylonitrile content in the resulting polymer is typically in the range of 18-46 wt%. Recurring chemistry includes the use of rosin acid or soap as emulsifiers, di-isopropylbenzene hydroperoxide as initiators, and tert-dodecyl mercaptan as chain transfer agents. Trends in the patent landscape indicate a focus on optimizing reaction conditions, such as temperature and reaction time, to achieve high conversion rates and desirable polymer properties. However, some parameters, such as monomer ratio and coagulation conditions, are not consistently disclosed across patents.

### Methodology

#### Patent 1: Not disclosed

Polymerization process: emulsion polymerization

Acrylonitrile content: 18-46 wt%

Monomer ratio: Not disclosed

Water amount: Not disclosed

Emulsifier: RA rosin acid or/and soap

Initiator: di-isopropylbenzene hydroperoxide, iron edta sodium salt or secondary reduction agent rongalite

Chain transfer agent: tert-dodecyl mercaptan, uncle's ten carbon mercaptan, uncle's 14 carbon mercaptan, uncle's 16 carbon mercaptan

Temperature: 5-30 ℃

Reaction time: 7-12 hours

Conversion: 65-80%

Coagulation: Not disclosed

Polymer properties: Mooney viscosity: 30-95, tensile strength: 10-22 Mpa

Experimental notes: cold process discontinuous emulsion polymerization, nitrogen pressure testing, nitrogen replacement, cold water cooling, temperature-reducing coil

### Cross-Patent Comparison & Synthesis Trends

#### Emulsifier Selection and Loading

The use of RA rosin acid or/and soap as emulsifiers is a common trend in the patent landscape.

#### Initiator and Chain Transfer Agent Strategies

Di-isopropylbenzene hydroperoxide is used as an initiator, while tert-dodecyl mercaptan and other mercaptans are used as chain transfer agents.

#### Monomer Ratio and Reaction Control

The monomer ratio is not disclosed in the provided patent, making it difficult to identify trends in this area.

#### Coagulation and Post-Treatment Conditions

Coagulation conditions are not disclosed in the provided patent, making it challenging to identify trends in this area.

### References

|  Patent Number  |  Patent Title  |  Assignee  |  Jurisdiction  |  Publication Year  |

| --- | --- | --- | --- | --- |

|  Not disclosed  |  Not disclosed  |  Not disclosed  |  Not disclosed  |  Not disclosed  |