# Low Styrene SBR Patent Landscape: Emulsion, Solution, and Functionalized Styrene-Butadiene Copolymer Routes

## 1. Abstract

This report synthesizes ten primary patents relevant to styrene-butadiene rubber (SBR) preparation, with emphasis on low-styrene embodiments and process routes that control styrene incorporation while preserving processability and tire performance. The selected patents span aqueous emulsion polymerization, organic-solvent solution polymerization, and post-polymerization functionalization/oil-extension strategies. Across the landscape, the target material is consistently a styrene-butadiene copolymer or elastomer, but the disclosed styrene levels vary widely: some patents explicitly use styrene in the 10–50 wt% range or around 25 wt%, while others disclose lower or moderate styrene fractions in solution SBR feeds (e.g., 30–40 wt% styrene in monomer charge) and functionalized emulsion SBRs with styrene around 21 wt% in the final polymer. Several patents focus less on lowering styrene per se and more on improving silica affinity, wet traction, rolling resistance, or processability through reactive emulsifiers, reactive polyols, epoxy-acrylate comonomers, silane modifiers, or oil extension. The dominant emulsion routes use water as the polymerization medium with rosin/fatty-acid emulsifier systems, redox or peroxide initiators, mercaptan chain-transfer agents, and low-temperature batch operation near 7–10 °C. The solution routes use hydrocarbon solvents such as hexane or cyclohexane, organolithium initiation, polar modifiers, and in some cases branching or coupling chemistry, followed by solvent removal and oil extension. Downstream water use is common in emulsion patents for coagulation, washing, and drying, while solution patents use water mainly for steam stripping or solvent removal. Overall, the patent set shows that low-styrene SBR development is not limited to a single synthesis platform; rather, it is achieved through careful monomer feed design and by integrating functional comonomers or post-modification steps that compensate for reduced styrene content with improved filler interaction and tire-relevant performance.

## 2. Methodology

### Primary Patent Evidence

### Patent 1: US8530017B2 — …  copolymer using reactive emulsifier and styrene-butadiene copolymer prepared by …

| Patent Number | US8530017B2 |
| --- | --- |
| Title | … copolymer using reactive emulsifier and styrene-butadiene copolymer prepared by … |
| Assignee | Korea Kumho Petrochemical Co., Ltd. |
| Jurisdiction | US |
| Publication Year | 2013 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: The patent discloses radical emulsion polymerization of styrene and 1,3-butadiene in water using a reactive emulsifier that participates in the polymerization and remains in the copolymer. The process is aimed at producing styrene-butadiene copolymers with improved silica affinity and tire tread performance, including variants containing reactive emulsifier-derived functionality.

Water: 1600 mL — Example 1

Potassium rosinate: 11 g — Example 1

Fatty acid potassium salt: 18 g — Example 1

Potassium chloride: 1.5 g — Example 1

Styrene: 260 g — Example 1

Methylcarboxylate methacrylate: 30 g — Example 1

1,3-Butadiene: 710 g — Example 1

EDTA: 0.5 g — Example 1

Sodium hydrosulfite: 0.3 g — Example 1

Ferrous sulfate: 0.1 g — Example 1

Sodium formaldehyde sulfonate: 0.4 g — Example 1

n-Dodecyl mercaptan: 1.0 g — Example 1

Methane hydroperoxide: 0.6 g — Example 1

Reactor volume: 5 L — Example 1

Polymerization time: 8 hours — Example 1

Polymerization temperature: 10 °C — Example 1

Diethylhydroxyamine: 1.0 g — Example 1

Weight average molecular weight: 860,000 g/mol — Example 1

Styrene monomer amount: 10-50 wt % — Claims

Butadiene monomer amount: 45-85 wt % — Claims

Polymerization temperature: 0-80 °C — Synthesis passages

Polymerization time: 1-48 hours — Synthesis passages

Weight average molecular weight: 100,000-3,000,000 g/mol — Synthesis passages

Medium & Water Role: Water is the polymerization medium in the emulsion SBR synthesis, and later water is also used in downstream coagulation/stripping and washing steps. The examples explicitly charge water to the reactor and later describe stripping and drying after polymerization.

low styrene content: Styrene monomer amount: 10-50 wt % — Claims

#### Medium & Water Role

Water is the polymerization medium in the emulsion SBR synthesis, and later water is also used in downstream coagulation/stripping and washing steps. The examples explicitly charge water to the reactor and later describe stripping and drying after polymerization.

#### low styrene content

Styrene monomer amount: 10-50 wt % — Claims

#### Relevant Experimental Evidence

Example 1: Reactive emulsifier-containing SBR was prepared with 260 g styrene and 710 g butadiene, giving Mw 860,000 g/mol.

Example 2: Increasing styrene to 280 g with polyoxyethylene phosphate methacrylate gave Mw 820,000 g/mol.

Example 3: Higher reactive emulsifier loading (30 g) still produced a high-Mw SBR (824,000 g/mol).

Example 4: Allyl alcohol ethoxylate comonomer yielded a copolymer with Mw 850,000 g/mol.

Example 7: Polyoxypropylene glycol phosphate acrylate comonomer produced Mw 845,000 g/mol.

#### Technical Relevance

This patent is directly relevant because it is an SBR emulsion polymerization platform and explicitly discloses styrene/butadiene feed ratios in the low-to-moderate SBR range. It also shows how reactive emulsifiers can be used to tune silica affinity without abandoning the SBR backbone.

### Patent 2: US6858683B2 — Process for the preparation of SBR rubbers with an improved processability and …

| Patent Number | US6858683B2 |
| --- | --- |
| Title | Process for the preparation of SBR rubbers with an improved processability and … |
| Assignee | Polimeri Europa S.P.A. |
| Jurisdiction | US |
| Publication Year | 2005 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: The patent discloses anionic solution polymerization of styrene and butadiene in hydrocarbon solvent, followed by termination, oil extension, solvent stripping, and drying. It focuses on improving processability and rolling resistance through control of microstructure, branching, and reactor configuration rather than emulsion chemistry.

Cyclohexane: 15 liters (11.7 kg) — Comparative Example 1

Tetrahydrofurfuryl ethyl ether (THFA): 2.4 g (200 ppm) — Comparative Example 1

Butadiene: 1.14 kg — Comparative Example 1

Styrene: 0.38 kg — Comparative Example 1

Temperature: 30 °C — Comparative Example 1

Li n-butyl: 2.05 g of a 5 wt% solution — Comparative Example 1

Reaction time: 20 minutes — Comparative Example 1

Temperature: 80 °C — Comparative Example 1

Ethyl alcohol: 0.15 g — Comparative Example 1

Highly aromatic oil: 0.560 kg — Comparative Example 1

Water: present in solvent-removal vessel — Comparative Example 1

Vapour temperature: 100 °C — Comparative Example 1

Vacuum oven temperature: 60 °C — Comparative Example 1

Drying time: 24 hours — Comparative Example 1

CSTR volume: 100 liters each — Comparative Example 2

Operating pressure: 3 bars — Comparative Example 2

Residence time: 30 minutes — Comparative Example 2

Butadiene: 9 wt % — Comparative Example 2

Styrene: 3 wt % — Comparative Example 2

Randomizing agent/vinyl promoter: 250 ppm — Comparative Example 2

Temperature: 57 °C — Comparative Example 2

Conversion: 74% — Comparative Example 2

Temperature: 66 °C — Comparative Example 2

Overall conversion: 99% — Comparative Example 2

Vinyl unit content: 67% — Comparative Example 2

Weight average molecular weight: 540,000 — Comparative Example 2

Mooney viscosity: 51 — Comparative Example 2

Cyclohexane: 15 liters (11.7 kg) — Comparative Example 3

THFA: 4.9 g (400 ppm) — Comparative Example 3

Butadiene: 1.14 kg — Comparative Example 3

Styrene: 0.38 kg — Comparative Example 3

Li n-butyl: 3 g of a 5 wt% solution — Comparative Example 3

SiCl4: 1.59 g of a 5 wt% solution in cyclohexane — Comparative Example 3

Temperature: 80 °C — Comparative Example 3

Highly aromatic oil: 0.560 kg — Comparative Example 3

Water: present in solvent-removal vessel — Comparative Example 3

Vacuum oven temperature: 60 °C — Comparative Example 3

Drying time: 24 hours — Comparative Example 3

Weight average molecular weight: 649,000 — Comparative Example 3

1,2 content: 65% — Comparative Example 3

Mooney viscosity: 49 — Comparative Example 3

Residence time: 30 minutes — Comparative Example 4

Butadiene: 9 wt % — Comparative Example 4

Styrene: 3 wt % — Comparative Example 4

Randomizing agent/vinyl promoter: 350 ppm — Comparative Example 4

Temperature: 53 °C — Comparative Example 4

Conversion: 59% — Comparative Example 4

Temperature: 61 °C — Comparative Example 4

Overall conversion: 90% — Comparative Example 4

Temperature: 66 °C — Comparative Example 4

Final conversion: 98% — Comparative Example 4

SiCl4: 40% of lithium fed — Comparative Example 4

Highly aromatic oil: 27% — Comparative Example 4

Weight average molecular weight: 720,000 — Comparative Example 4

Vinyl unit content: 66% — Comparative Example 4

Mooney viscosity: 50 — Comparative Example 4

DVB: total quantity equal to lithium fed — Comparative Example 10

Gel content: 5% — Comparative Example 10

DVB: 75% to first reactor and 25% to second reactor — Comparative Example 11

Insoluble product: 22% — Comparative Example 11

Medium & Water Role: The polymerization itself is carried out in cyclohexane solution, not in water. Water appears later only in the solvent-removal step, where the polymer solution is fed to a stirred reactor containing water heated by steam to eliminate solvent, followed by filtration and drying.

low styrene content: Styrene: 3 wt % — Comparative Example 2; Styrene: 3 wt % — Comparative Example 4

#### Medium & Water Role

The polymerization itself is carried out in cyclohexane solution, not in water. Water appears later only in the solvent-removal step, where the polymer solution is fed to a stirred reactor containing water heated by steam to eliminate solvent, followed by filtration and drying.

#### low styrene content

Styrene: 3 wt % — Comparative Example 2; Styrene: 3 wt % — Comparative Example 4

#### Relevant Experimental Evidence

Comparative Example 1: Batch solution SBR was made in cyclohexane and finished by steam stripping and drying.

Comparative Example 2: Continuous solution SBR with 9 wt% butadiene and 3 wt% styrene gave 99% overall conversion and Mw 540,000.

Comparative Example 3: Radial batch SBR using SiCl4 coupling produced Mw 649,000 and 1,2 content 65%.

Comparative Example 4: Continuous radial SBR with SiCl4 coupling reached 98% final conversion and Mw 720,000.

Comparative Example 9: Branched continuous SBR using DVB showed no gel and Mw 650,000.

#### Technical Relevance

This patent is relevant because it is a core SBR manufacturing disclosure, albeit in solution rather than emulsion form. It provides a low-styrene feed example in continuous operation and shows how reactor design and branching/coupling affect processability.

### Patent 3: US9328176B2 — Functional styrene-butadiene copolymer

| Patent Number | US9328176B2 |
| --- | --- |
| Title | Functional styrene-butadiene copolymer |
| Assignee | Korea Kumho Petrochemical Co., Ltd. |
| Jurisdiction | US |
| Publication Year | 2016 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: The patent discloses emulsion polymerization of styrene-butadiene copolymers and functionalized variants in water, followed by ring-opening of epoxy groups using acidic or alkaline aqueous solutions. The process is designed to improve silica affinity and tire performance by introducing hydroxyl functionality into the SBR backbone.

Water: 1,500 mL — Example 1

Sodium rosinate: 25 g — Example 1

Sodium salt of fatty acid: 35 g — Example 1

Styrene: 380 g — Example 1

Glycidyl methyl methacrylate: 50 g — Example 1

1,3-Butadiene: 570 g — Example 1

EDTA: 0.6 g — Example 1

Ferrous sulfate: 0.1 g — Example 1

n-Dodecylmercaptan: 1.5 g — Example 1

p-Menthane hydroperoxide: 0.6 g — Example 1

Reactor volume: 5 L — Example 1

Temperature: 10 °C — Example 1

Reaction time: 24 hours — Example 1

Diethylhydroxylamine: 1.0 g — Example 1

Sulfuric acid: 20% aqueous solution, 100 g — Example 1

Average molecular weight: 908,000 g/mol — Example 1

NaOH: 20% aqueous solution, 100 g — Example 4

Average molecular weight: 740,000 g/mol — Example 4

KOH: 20% aqueous solution, 100 g — Example 5

Average molecular weight: 791,000 g/mol — Example 5

Water: 1,500 mL — Comparative Example 1

Styrene: 400 g — Comparative Example 1

1,3-Butadiene: 600 g — Comparative Example 1

Average molecular weight: 843,000 g/mol — Comparative Example 1

Water: 1,500 mL — Comparative Example 2

Styrene: 380 g — Comparative Example 2

1,3-Butadiene: 570 g — Comparative Example 2

Methyl methacrylic acid: 50 g — Comparative Example 2

Average molecular weight: 795,000 g/mol — Comparative Example 2

Styrene monomer amount: 10-50 wt % — Synthesis passages

Butadiene monomer amount: 45-85 wt % — Synthesis passages

Epoxy acrylate monomer amount: 0.1-10 wt % — Synthesis passages

Radical initiator amount: 0.05-3 parts by weight per 100 parts monomers — Synthesis passages

Polymerization temperature: 0-80 °C — Synthesis passages

Medium & Water Role: Water is part of the emulsion polymerization medium and is also used later in aqueous ring-opening chemistry and downstream latex handling. The examples explicitly charge water to the reactor and use 20% aqueous sulfuric acid, NaOH, or KOH for post-polymerization ring opening.

low styrene content: Styrene monomer amount: 10-50 wt % — Synthesis passages

#### Medium & Water Role

Water is part of the emulsion polymerization medium and is also used later in aqueous ring-opening chemistry and downstream latex handling. The examples explicitly charge water to the reactor and use 20% aqueous sulfuric acid, NaOH, or KOH for post-polymerization ring opening.

#### low styrene content

Styrene monomer amount: 10-50 wt % — Synthesis passages

#### Relevant Experimental Evidence

Example 1: GMA-containing SBR was prepared in water and ring-opened with 20% sulfuric acid to give hydroxyl-functional copolymer.

Example 4: NaOH ring-opening produced a hydroxyl-functional SBR with Mw 740,000.

Example 5: KOH ring-opening produced a hydroxyl-functional SBR with Mw 791,000.

Comparative Example 1: Unfunctionalized SBR was prepared under similar emulsion conditions.

Comparative Example 2: Methyl methacrylic acid comonomer gave a different copolymer with Mw 795,000.

#### Technical Relevance

This patent is relevant because it is an SBR emulsion process with explicit styrene/butadiene feed levels and a functional comonomer strategy that preserves SBR identity while improving silica compatibility. It is useful for low-styrene SBR research because it shows how monomer balance and post-ring-opening functionality can be combined in aqueous SBR synthesis.

### Patent 4: US8455600B2 — …  butadiene copolymer highly functionalized with reactive polyol and manufacturing …

| Patent Number | US8455600B2 |
| --- | --- |
| Title | … butadiene copolymer highly functionalized with reactive polyol and manufacturing … |
| Assignee | Korea Kumho Petrochemical Co., Ltd. |
| Jurisdiction | US |
| Publication Year | 2013 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: The patent discloses emulsion polymerization of styrene and butadiene in water using reactive polyol monomers, followed by preparation of functionalized SBR latex and downstream compounding. The reactive polyol is introduced during polymerization to improve silica affinity and blending behavior.

Water: 1600 mL — Example 1

Potassium rosinate: 23 g — Example 1

Fatty acid potassium salt: 37 g — Example 1

Potassium chloride: 3.5 g — Example 1

Styrene: 480 g — Example 1

Reactive polyol (Chemical Formula 4): 30 g, molecular weight 400 — Example 1

1,3-Butadiene: 490 g — Example 1

EDTA: 0.5 g — Example 1

Sodium hydrosulfite: 0.3 g — Example 1

Ferrous sulfate: 0.1 g — Example 1

Sodium formaldehyde sulfonate: 0.4 g — Example 1

Dodecanethiol: 1.0 g — Example 1

Methane hydroperoxide: 0.6 g — Example 1

Reactor volume: 5 L — Example 1

Reaction time: 8 hours — Example 1

Temperature: 10 °C — Example 1

Diethylhydroxyamine: 1.0 g — Example 1

Average molecular weight: 1,010,000 g/mol — Example 1

Reactive polyol molecular weight: 3000 — Example 2

Average molecular weight: 950,000 g/mol — Example 2

Reactive polyol molecular weight: 9000 — Example 3

Average molecular weight: 975,000 g/mol — Example 3

Styrene: 450 g — Example 4

Acrylonitrile: 30 g — Example 4

Average molecular weight: 920,000 g/mol — Example 4

Styrene: 430 g — Example 5

Acrylonitrile: 50 g — Example 5

Average molecular weight: 930,000 g/mol — Example 5

Bound styrene content: 21.0 wt% — Example 6

cis-1,4 content: 9.5 wt% — Example 6

trans-1,4 content: 76.3 wt% — Example 6

vinyl 1,2 content: 14.2 wt% — Example 6

Mooney viscosity (ML 1+4, 100°C): 45.8 — Example 6

Average molecular weight: 356,000 g/mol — Example 6

Medium & Water Role: Water is the polymerization medium for the SBR latex synthesis, and later water is also used in latex handling and compounding-related steps. The examples explicitly charge water to the reactor and describe the latex as the product form before oil blending and compounding.

low styrene content: Bound styrene content: 21.0 wt% — Example 6

#### Medium & Water Role

Water is the polymerization medium for the SBR latex synthesis, and later water is also used in latex handling and compounding-related steps. The examples explicitly charge water to the reactor and describe the latex as the product form before oil blending and compounding.

#### low styrene content

Bound styrene content: 21.0 wt% — Example 6

#### Relevant Experimental Evidence

Example 1: Reactive polyol was incorporated during emulsion polymerization to give a styrene-butadiene-reactive polyol copolymer.

Example 2: Higher-molecular-weight reactive polyol was used, yielding Mw 950,000 g/mol.

Example 3: Sorbitol-derived reactive polyol gave Mw 975,000 g/mol.

Example 4: Acrylonitrile-containing functional copolymer was prepared with Mw 920,000 g/mol.

Example 6: Oil-extended functionalized SBR showed 21.0 wt% bound styrene and Mw 356,000 g/mol.

#### Technical Relevance

This patent is relevant because it is an emulsion SBR platform with explicit styrene/butadiene feed levels and a functional monomer strategy that improves silica affinity. It also provides a concrete low-to-moderate styrene final polymer composition in a functionalized SBR embodiment.

### Patent 5: US20140256858A1 — Solution polymerization prepared styrene/butadiene elastomer containing liquid …

| Patent Number | US20140256858A1 |
| --- | --- |
| Title | Solution polymerization prepared styrene/butadiene elastomer containing liquid … |
| Assignee | Robert Anthony Bethea |
| Jurisdiction | US |
| Publication Year | 2014 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: The patent discloses anionically initiated solution polymerization of styrene and 1,3-butadiene in hexane to make a high-molecular-weight SSBR cement, followed by blending with liquid styrene-butadiene polymer or petroleum oil and solvent removal. The focus is on extending the cement before recovery to improve processability.

Reactor volume: 2000 liters — Example I

Temperature: 60-70 °C — Example I

Internal pressure: 350-450 kPa — Example I

Total monomers in hexane: 15 wt% — Example I

1,3-Butadiene: 60 wt% of total monomers — Example I

Styrene: 40 wt% of total monomers — Example I

TMEDA: 0.12 pphm — Example I

n-BuLi: 0.039 pphm — Example I

Conversion: 90-99% — Example I

Polymerization termination agent: Polystay K and isopropyl alcohol, 1.0 and 0.5 pphm — Example I

Liquid styrene/butadiene polymer number average molecular weight: 1,000-50,000 g/mol — Claims

H-SSBR number average molecular weight: 200,000-1,000,000 g/mol — Claims

Triglyceride vegetable oil: 5-60 phr — Claims

Mooney viscosity: 50-180 — Claims

Mooney viscosity: 80-120 — Claims

Medium & Water Role: The polymerization is carried out in hexane solution, not in water. Water appears later only in steam-stripping/solvent-removal operations used to recover the oil-extended SSBR composite.

low styrene content: Not disclosed in extracted evidence

#### Medium & Water Role

The polymerization is carried out in hexane solution, not in water. Water appears later only in steam-stripping/solvent-removal operations used to recover the oil-extended SSBR composite.

#### low styrene content

Not disclosed in extracted evidence

#### Relevant Experimental Evidence

Example I: A hexane solution with 60 wt% butadiene and 40 wt% styrene was anionically polymerized to high conversion.

Example I: The recovered H-SSBR had bound styrene 38.9 wt% and Mooney viscosity about 121.

Example I: Petroleum oil extension reduced Mooney viscosity to about 52.8.

Example I: Soybean oil extension reduced Mooney viscosity further to about 40.

#### Technical Relevance

This patent is relevant as a solution-polymerized SSBR route that explicitly controls styrene/butadiene feed ratio and demonstrates post-polymerization extension strategies. Although not a low-styrene patent, it is important for understanding solution SBR manufacturing and processability control.

### Patent 6: US10174133B2 — Modified styrene-butadiene copolymer, preparation method thereof, and rubber …

| Patent Number | US10174133B2 |
| --- | --- |
| Title | Modified styrene-butadiene copolymer, preparation method thereof, and rubber … |
| Assignee | Lg Chem, Ltd. |
| Jurisdiction | US |
| Publication Year | 2019 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Medium & Water Role: No water-related process step disclosed in the extracted evidence.

low styrene content: Not disclosed in extracted evidence

#### Medium & Water Role

No water-related process step disclosed in the extracted evidence.

#### low styrene content

Not disclosed in extracted evidence

#### Relevant Experimental Evidence

Comparative Example: Comparative Example

Example 1:: Example 1:

Example 2: Example 2

Experimental Example 1: Experimental Example 1

Example 1: Example 1

Example: Example

#### Technical Relevance

Selected via deterministic pipeline scoring.

### Patent 7: EP2657262B1 — Triglyceride containing solution polymerization prepared styrene/butadiene …

| Patent Number | EP2657262B1 |
| --- | --- |
| Title | Triglyceride containing solution polymerization prepared styrene/butadiene … |
| Assignee | The Goodyear Tire & Rubber Company |
| Jurisdiction | EP |
| Publication Year | 2014 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: The patent discloses anionically initiated solution polymerization of styrene and butadiene in hexane to form SSBR cement, followed by extension with triglyceride vegetable oil or petroleum oil and solvent removal. The examples compare petroleum oil and soybean oil extension effects on processability and Mooney viscosity.

Reactor volume: 2000 liters — Example I

Temperature: 63-71 °C — Example I

Internal pressure: 97-186 kPa — Example I

Total monomers in hexane: 12 wt% — Example I

1,3-Butadiene: 70 wt% of total monomers — Example I

Styrene: 30 wt% of total monomers — Example I

TMEDA: 0.12 pphm — Example I

SMT: 0.0035 pphm — Example I

n-BuLi: 0.025 pphm — Example I

Conversion: 90-95% — Example I

Polystay K: 0.5 pphm — Example I

Bound styrene: 31.7 wt% — Example I

Vinyl content: 63.5% — Example I

cis content: 21.4% — Example I

trans content: 15.1% — Example I

Mooney viscosity: 107 — Example I

Soybean oil extension: 36.9 pphr — Example I

Petroleum oil extension: 36.8 pphr — Example I

Mooney viscosity after petroleum oil extension: 52.8 — Example I

Mooney viscosity after soybean oil extension: 40 — Example I

Triglyceride vegetable oil: 5-60 phr — Claims

H-SSBR Mooney viscosity: 50-180 — Claims

H-SSBR Mooney viscosity: 80-120 — Claims

Medium & Water Role: The polymerization is conducted in hexane solution, while water is used later in steam stripping to remove solvent from the SSBR/oil blend. No aqueous polymerization medium is disclosed.

low styrene content: Not disclosed in extracted evidence

#### Medium & Water Role

The polymerization is conducted in hexane solution, while water is used later in steam stripping to remove solvent from the SSBR/oil blend. No aqueous polymerization medium is disclosed.

#### low styrene content

Not disclosed in extracted evidence

#### Relevant Experimental Evidence

Example I: Base SSBR was prepared from 70 wt% butadiene and 30 wt% styrene in hexane.

Example I: The recovered SSBR had bound styrene 31.7 wt% and Mooney viscosity 107.

Example I: Petroleum oil extension reduced Mooney viscosity to 52.8.

Example I: Soybean oil extension reduced Mooney viscosity further to 40.

#### Technical Relevance

This patent is relevant because it is a solution SBR process with a relatively lower styrene feed than many conventional grades and explicit control of polymer properties through oil extension. It is especially useful for understanding how solution SBR can be processed and extended without changing the SBR backbone chemistry.

### Patent 8: EP2424740B1 — Elastomer compositions modified by silanes

| Patent Number | EP2424740B1 |
| --- | --- |
| Title | Elastomer compositions modified by silanes |
| Assignee | Dow Corning Corporation |
| Jurisdiction | EP |
| Publication Year | 2013 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: The patent discloses modification of diene elastomers with olefinically unsaturated silanes in the absence of free-radical initiator, primarily as a compounding/modification route rather than SBR synthesis. The examples shown are natural rubber-based rubber compositions, so the patent is only indirectly relevant to SBR processing and silica coupling concepts.

Silica: 50.0 parts — Example 1 and 2

Silane 1: 5.5 parts — Example 2

Silane 2: 5.3 parts — Example 1

Carbon black N234: 45.0 parts — Comparative example C1

ACST: 2.5 parts — Example 1 and 2

ZnO: 3.0 parts — Example 1 and 2

6PPD: 2.0 parts — Example 1 and 2

Carbon black N330: 3.0 parts — Example 1 and 2

S: 1.5 parts — Example 1 and 2

CBS: 1.8 parts — Example 1 and 2

Mixing temperature: 80 °C — Table 2

Mixing temperature: 90 °C — Table 2

Mixing temperature: 100 °C — Table 2

Mixing temperature: 120 °C — Table 2

Mixing temperature: 150-160 °C — Table 2

Milling temperature: about 70 °C — Table 3

Rheometry temperature: 160 °C — Table 4

Medium & Water Role: No water-related process step disclosed in the extracted evidence.

low styrene content: Not disclosed in extracted evidence

#### Medium & Water Role

No water-related process step disclosed in the extracted evidence.

#### low styrene content

Not disclosed in extracted evidence

#### Relevant Experimental Evidence

Examples 1 and 2: Natural rubber was modified with unsaturated silanes in silica-filled formulations.

Example 1: Acryloxypropyltrimethoxysilane-based silane 2 was used.

Example 2: Comparative silane 1 was used for comparison.

Examples 3 and 4: Alternative silanes were evaluated for silica dispersion and rolling resistance.

Example 5: Bis(triethoxysilylpropyl)-tetrasulfane and related silanes were compared.

#### Technical Relevance

This patent is only indirectly relevant to low-styrene SBR because it addresses silane coupling and silica-filled elastomer compounding rather than SBR synthesis. It is useful as a downstream formulation reference for silica interaction, but it does not disclose SBR preparation.

### Patent 9: EP2986647B1 — Oil extended functionalized styrene-butadiene copolymer

| Patent Number | EP2986647B1 |
| --- | --- |
| Title | Oil extended functionalized styrene-butadiene copolymer |
| Assignee | ARLANXEO Deutschland GmbH |
| Jurisdiction | EP |
| Publication Year | 2017 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: The patent discloses emulsion polymerization of styrene-butadiene latex, followed by blending with vegetable-oil emulsions and coagulation/washing to obtain oil-extended functionalized SBR. A functionalized latex embodiment is prepared by incorporating glycidyl methacrylate at the start of polymerization and then ring-opening the epoxy group.

Water: 8,700 g — Example 1

Emulsifier batch with potassium salt of fatty and rosin acids: 2,330 g — Example 1

1,3-Butadiene: 3,830 g — Example 1

Styrene: 1,486 g — Example 1

Pinane hydroperoxide: 2.5 g — Example 1

Activator batch: 390 g — Example 1

t-Dodecyl mercaptan: 10 g — Example 1

Temperature: 7 °C — Example 1

Conversion: 60% — Example 1

Duration: about 7 hours — Example 1

Oil in dry rubber: 37.5 phr — Example 1

Water: 8,500 g — Example 4

Emulsifier batch with potassium salt of fatty and rosin acids: 2,330 g — Example 4

Buffering system pH: 8.7 — Example 4

1,3-Butadiene: 3,830 g — Example 4

Styrene: 1,242 g — Example 4

GMA/styrene blend: 106/133 g — Example 4

Pinane hydroperoxide: 2.5 g — Example 4

Activator batch: 390 g — Example 4

t-Dodecyl mercaptan: 10 g — Example 4

Temperature: 7 °C — Example 4

Conversion: 60% — Example 4

Duration: about 5 hours — Example 4

Final latex pH: 9.2 — Example 4

Oil in dry rubber: 37.5 phr — Example 4

Bound styrene content: 21.0 wt% — Example 6

cis-1,4 content: 9.5 wt% — Example 6

trans-1,4 content: 76.3 wt% — Example 6

vinyl 1,2 content: 14.2 wt% — Example 6

Mooney viscosity (ML 1+4, 100°C): 45.8 — Example 6

Average molecular weight: 356,000 g/mol — Example 6

Styrene content: 15 to 50 wt% — Claims

Butadiene content: 42 to 80 wt% — Claims

Functional monomer content: 5 to 43 wt% — Claims

Functional monomer content: 0.3 to 10 wt% — Claims

Mooney viscosity: 35 to 65 — Claims

Average molecular weight: 100,000 to 2,200,000 g/mol — Claims

Medium & Water Role: Water is the emulsion polymerization medium and is also used later for latex/oil blending, coagulation, and washing of crumbs. The examples explicitly charge water to the reactor and wash the coagulated crumbs with demineralized water.

low styrene content: Bound styrene content: 21.0 wt% — Example 6

#### Medium & Water Role

Water is the emulsion polymerization medium and is also used later for latex/oil blending, coagulation, and washing of crumbs. The examples explicitly charge water to the reactor and wash the coagulated crumbs with demineralized water.

#### low styrene content

Bound styrene content: 21.0 wt% — Example 6

#### Relevant Experimental Evidence

Example 1: Standard SBR latex was prepared by emulsion polymerization and extended with oil emulsion.

Example 4: GMA was introduced at the start of polymerization to make functionalized SBR latex.

Example 4: The final latex had pH 9.2 and was oil-extended with 37.5 phr oil.

Example 6: Functionalized SBR extended with epoxidized soybean oil showed bound styrene 21.0 wt% and Mw 356,000 g/mol.

#### Technical Relevance

This patent is highly relevant because it is an emulsion SBR platform with explicit styrene/butadiene composition ranges and a functional monomer strategy that yields a low-to-moderate styrene functionalized SBR. It also demonstrates vegetable-oil extension and latex coagulation/washing, both important for practical SBR manufacture.

### Patent 10: US20170260340A1 — Styrene-butadiene rubber (sbr)-nanocarbon filled masterbatches and uses thereof

| Patent Number | US20170260340A1 |
| --- | --- |
| Title | Styrene-butadiene rubber (sbr)-nanocarbon filled masterbatches and uses thereof |
| Assignee | Amril Ag |
| Jurisdiction | US |
| Publication Year | 2017 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: The patent discloses preparation of nanocarbon-reinforced SBR masterbatches by dispersing carbon nanotubes in water with surfactant, combining the aqueous nanocarbon dispersion with SBR latex, and then coagulating the latex to recover a filled rubber masterbatch. It is a compounding and dispersion patent rather than an SBR synthesis patent.

Nanocarbon dispersion: 3% — Example 1.1

Nanocarbon: 15 g — Example 1.1

Surfactant: 75 g — Example 1.1

Distilled water: 410 g — Example 1.1

Stirring speed: 80 rpm — Example 1.1

Stirring time: about 10 minutes — Example 1.1

Ball milling time: 24 hours — Example 1.1

pH of CNT dispersion: 8.0 to 10.0 — Example 1.1

SBR latex concentration: 45% — Example 1.2

SBR latex dilution: 30% — Example 1.2

Surfactant level: about 5 pphr — Example 1.2

3 pphr CNT-SBR masterbatch — Example 1.2

Mixing time: 60 minutes — Example 1.2

Stirring speed: 80 to 100 rpm — Example 1.2

Temperature: 23 to 30 °C — Example 1.2

Calcium chloride: 500 ml of 20% w/w — Example 1.2

CNT length: less than 50 μm — Examples

CNT outer diameter: less than 20 nm — Examples

CNT C-purity: greater than 85% — Examples

Medium & Water Role: Water is central to the nanocarbon dispersion and the SBR latex masterbatch preparation. The patent does not disclose SBR polymerization; instead, it uses water for dispersion, latex blending, and coagulation of the filled latex.

low styrene content: Not disclosed in extracted evidence

#### Medium & Water Role

Water is central to the nanocarbon dispersion and the SBR latex masterbatch preparation. The patent does not disclose SBR polymerization; instead, it uses water for dispersion, latex blending, and coagulation of the filled latex.

#### low styrene content

Not disclosed in extracted evidence

#### Relevant Experimental Evidence

Example 1.1: A 3% CNT dispersion was prepared in water with surfactant and ball milling.

Example 1.2: CNT dispersion was combined with SBR latex to make a 3 pphr CNT-SBR masterbatch.

Example 1.2: The filled latex was coagulated with calcium chloride.

Example 2.2: CNT-filled SBR showed much lower electrical resistivity than virgin SBR.

Example 3.1: CNT addition increased Mooney viscosity, and mechanical peptizer reduced it.

#### Technical Relevance

This patent is relevant to SBR processing and formulation, but not to SBR synthesis. It demonstrates how SBR latex can be combined with aqueous nanocarbon dispersions and coagulated, which is useful for downstream handling of SBR-based materials.

### Patent Comparison Table

| Patent | Applicant | Medium & Water Role | low styrene content |
| --- | --- | --- | --- |
| US8530017B2 | Korea Kumho Petrochemical Co., Ltd. | Water is the polymerization medium in the emulsion SBR synthesis, and later water is also used in downstream coagulation/stripping and washing steps. The examples explicitly charge water to the reactor and later describe stripping and drying after polymerization. | Styrene monomer amount: 10-50 wt % — Claims |
| US6858683B2 | Polimeri Europa S.P.A. | The polymerization itself is carried out in cyclohexane solution, not in water. Water appears later only in the solvent-removal step, where the polymer solution is fed to a stirred reactor containing water heated by steam to eliminate solvent, followed by filtration and drying. | Styrene: 3 wt % — Comparative Example 2; Styrene: 3 wt % — Comparative Example 4 |
| US9328176B2 | Korea Kumho Petrochemical Co., Ltd. | Water is part of the emulsion polymerization medium and is also used later in aqueous ring-opening chemistry and downstream latex handling. The examples explicitly charge water to the reactor and use 20% aqueous sulfuric acid, NaOH, or KOH for post-polymerization ring opening. | Styrene monomer amount: 10-50 wt % — Synthesis passages |
| US8455600B2 | Korea Kumho Petrochemical Co., Ltd. | Water is the polymerization medium for the SBR latex synthesis, and later water is also used in latex handling and compounding-related steps. The examples explicitly charge water to the reactor and describe the latex as the product form before oil blending and compounding. | Bound styrene content: 21.0 wt% — Example 6 |
| US20140256858A1 | Robert Anthony Bethea | The polymerization is carried out in hexane solution, not in water. Water appears later only in steam-stripping/solvent-removal operations used to recover the oil-extended SSBR composite. | Not disclosed in extracted evidence |
| US10174133B2 | Lg Chem, Ltd. | No water-related process step disclosed in the extracted evidence. | Not disclosed in extracted evidence |
| EP2657262B1 | The Goodyear Tire & Rubber Company | The polymerization is conducted in hexane solution, while water is used later in steam stripping to remove solvent from the SSBR/oil blend. No aqueous polymerization medium is disclosed. | Not disclosed in extracted evidence |
| EP2424740B1 | Dow Corning Corporation | No water-related process step disclosed in the extracted evidence. | Not disclosed in extracted evidence |
| EP2986647B1 | ARLANXEO Deutschland GmbH | Water is the emulsion polymerization medium and is also used later for latex/oil blending, coagulation, and washing of crumbs. The examples explicitly charge water to the reactor and wash the coagulated crumbs with demineralized water. | Bound styrene content: 21.0 wt% — Example 6 |
| US20170260340A1 | Amril Ag | Water is central to the nanocarbon dispersion and the SBR latex masterbatch preparation. The patent does not disclose SBR polymerization; instead, it uses water for dispersion, latex blending, and coagulation of the filled latex. | Not disclosed in extracted evidence |

## 3. Cross-Patent Comparison & Synthesis Trends

Emulsion-route patents (US8530017B2, US9328176B2, US8455600B2, EP2986647B1) all use water as the polymerization medium and typically rely on rosin/fatty-acid emulsifiers, peroxide/redox initiators, mercaptan chain-transfer agents, and low temperatures around 7-10 °C.

Solution-route patents (US6858683B2, US20140256858A1, EP2657262B1) use hydrocarbon solvents such as cyclohexane or hexane, organolithium initiation, and solvent stripping; water appears only in downstream stripping/workup.

The explicitly low-styrene feed disclosure among the primary SBR synthesis patents is strongest in US6858683B2, where a continuous solution example uses 3 wt% styrene in the feed; EP2657262B1 uses 30 wt% styrene feed and US20140256858A1 uses 40 wt% styrene feed.

Functionalization strategies differ: US8530017B2 uses reactive emulsifiers, US9328176B2 uses epoxy-acrylate monomer plus aqueous ring-opening, US8455600B2 uses reactive polyols, and EP2986647B1 uses GMA plus vegetable-oil extension.

US20170260340A1 and EP2424740B1 are downstream compounding/masterbatch or silane-modification patents rather than SBR synthesis patents; they are relevant to processing and filler interaction but do not define low-styrene SBR synthesis conditions.

## 4. Conclusion

Across the selected primary patents, low-styrene SBR is realized mainly through emulsion or solution polymerization of styrene and butadiene with careful feed control, then enhanced by functional comonomers, reactive emulsifiers, or post-polymerization extension to recover performance lost by reducing styrene. The most explicit low-styrene feed disclosure appears in the solution-process patent US6858683B2, while the emulsion patents emphasize silica affinity and tire performance through functionalization rather than extreme styrene reduction. Water is central in the emulsion patents and appears only as a downstream stripping/workup medium in the solution patents.

## 5. References

US8530017B2 | … copolymer using reactive emulsifier and styrene-butadiene copolymer prepared by … | Korea Kumho Petrochemical Co., Ltd. | US | 2013 | https://patents.google.com/patent/US8530017B2/en

US6858683B2 | Process for the preparation of SBR rubbers with an improved processability and … | Polimeri Europa S.P.A. | US | 2005 | https://patents.google.com/patent/US6858683B2/en

US9328176B2 | Functional styrene-butadiene copolymer | Korea Kumho Petrochemical Co., Ltd. | US | 2016 | https://patents.google.com/patent/US9328176B2/en

US8455600B2 | … butadiene copolymer highly functionalized with reactive polyol and manufacturing … | Korea Kumho Petrochemical Co., Ltd. | US | 2013 | https://patents.google.com/patent/US8455600B2/en

US20140256858A1 | Solution polymerization prepared styrene/butadiene elastomer containing liquid … | Robert Anthony Bethea | US | 2014 | https://patents.google.com/patent/US20140256858A1/en

US10174133B2 | Modified styrene-butadiene copolymer, preparation method thereof, and rubber … | Lg Chem, Ltd. | US | 2019 | https://patents.google.com/patent/US10174133B2/en

EP2657262B1 | Triglyceride containing solution polymerization prepared styrene/butadiene … | The Goodyear Tire & Rubber Company | EP | 2014 | https://patents.google.com/patent/EP2657262B1/en

EP2424740B1 | Elastomer compositions modified by silanes | Dow Corning Corporation | EP | 2013 | https://patents.google.com/patent/EP2424740B1/en

EP2986647B1 | Oil extended functionalized styrene-butadiene copolymer | ARLANXEO Deutschland GmbH | EP | 2017 | https://patents.google.com/patent/EP2986647B1/en

US20170260340A1 | Styrene-butadiene rubber (sbr)-nanocarbon filled masterbatches and uses thereof | Amril Ag | US | 2017 | https://patents.google.com/patent/US20170260340A1/en