# PATENT RESEARCH REPORT

## 1. Abstract

This technical report synthesizes patent literature regarding the synthesis, compounding, and application of Low Acrylonitrile Nitrile Butadiene Rubber (Low Acrylonitrile NBR). The research scope encompasses the polymerization methodologies, structural modifications, and formulation trends of diene-based elastomers containing low levels of acrylonitrile (typically under 30% by mass). Low Acrylonitrile NBR is highly valued for its low-temperature flexibility, oil resistance, and compatibility with polar fillers like silica. The selected patent landscape reveals three primary polymerization and modification approaches: cold emulsion polymerization, anionic solution copolymerization, and olefin metathesis-driven segment interchange. Emulsion polymerization remains the dominant industrial method, utilizing rosin/fatty acid emulsifiers, mercaptan chain transfer agents, and organic peroxide initiators at low temperatures (e.g., 10°C) to achieve random monomer distribution and narrow glass transition widths. Anionic solution polymerization, initiated by functionalized lithium amides, is utilized to introduce tertiary amine or pyrrolidine groups, significantly enhancing filler-elastomer interactions and reducing hysteresis. Olefin metathesis, utilizing Grubbs-type catalysts, offers a route to novel block copolymers via segment interchange of hydrogenated NBR (HNBR). In terms of application, Low Acrylonitrile NBR is heavily featured in electro-conductive matrix-domain structures for electrophotographic members, where its specific volume resistivity and compatibility with epichlorohydrin or other polar rubbers prevent transfer defects and image fogging. This report provides a comprehensive analysis of these synthetic methodologies and compounding formulations to guide the development of high-performance Low Acrylonitrile NBR materials.

## 2. Primary Patent Evidence

### Patent 1: EP3715957B1 — Electro-conductive member, process cartridge image forming apparatus and a …

| Patent Number | EP3715957B1 |
| --- | --- |
| Title | Electro-conductive member, process cartridge image forming apparatus and a … |
| Assignee | Not disclosed in the available patent text. |
| Jurisdiction | EP |
| Publication Year | 2022 |
| Priority Date | Not available from source |
| Legal Status | Not available from source |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Mentions matrix-domain structures using rubbers, potentially low acrylonitrile NBR as a component in electro-conductive members. |

#### Polymerization / Synthesis Method

Monomers: Value not specified.

Polymerization Temperature: Value not specified.

Initiator: Value not specified.

Coagulation Method: Value not specified.

#### Relevant Experimental Evidence

No specific experimental examples disclosed in the supplied evidence.

#### Technical Relevance

Contributes to understanding the application of NBR/rubber blends in electro-conductive layers with matrix-domain structures for electrophotographic members.

### Patent 2: US11340553B2 — Process cartridge and electrophotographic apparatus

| Patent Number | US11340553B2 |
| --- | --- |
| Title | Process cartridge and electrophotographic apparatus |
| Assignee | Not disclosed in the available patent text. |
| Jurisdiction | US |
| Publication Year | 2022 |
| Priority Date | Not available from source |
| Legal Status | Not available from source |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Uses NBR and other rubbers in matrix-domain electro-conductive layers. |

#### Polymerization / Synthesis Method

Solid Content: 23 % (hydroxygallium phthalocyanine pigment)

Solid Content: 88 %

Solid Content: 98 %

Orthophthalonitrile: 5.46 parts

Gallium trichloride: 3.75 parts

Reaction Time: 4.5 hours

Concentrated sulfuric acid: 139.5 parts

Ice: 620 parts

Aqueous ammonia: 2 %

Hydrochloric acid: 200 parts (35 mass %)

Ion-exchanged water: 1000 parts

Chlorogallium phthalocyanine pigment yield: 71 %

Hydroxygallium phthalocyanine pigment yield: 97 %

Stearic acid: 1.33 parts (MRC 9)

Stearic acid: 0.91 parts (MRC 13)

Stearic acid: 1.54 parts (MRC 14)

Zinc oxide: 4.62 parts (MRC 14)

Epichlorohydrin-ethylene oxide-allyl glycidyl ether terpolymer: 90 parts

Liquid NBR: 10 parts

#### Relevant Experimental Evidence

Preparation 1: Synthesis of chlorogallium phthalocyanine pigment using 5.46 parts orthophthalonitrile, 45 parts alpha-chloronaphthalene, and 3.75 parts gallium trichloride heated to 30°C under nitrogen flow for 4.5 hours, yielding 71%.

Preparation 2: Dissolution of 4.65 parts chlorogallium phthalocyanine in 139.5 parts concentrated sulfuric acid, dropwise addition to 620 parts ice water, dispersion in 2% aqueous ammonia, yielding 97% hydrous hydroxygallium phthalocyanine (23% solid content).

Preparation 4: Mixing 10 parts hydroxygallium phthalocyanine with 200 parts 35% hydrochloric acid, adding to 1000 parts ice-cooled ion-exchanged water to obtain 9 parts chlorogallium phthalocyanine.

MRC Production Examples: Formulation of rubber compositions (SBR, EPDM, Butyl, NBR) with fillers and electroconducting agents, including a mixture of 90 parts epichlorohydrin terpolymer and 10 parts liquid NBR.

#### Technical Relevance

Provides detailed preparation methods for phthalocyanine pigments and rubber formulations containing NBR as a blend component for electro-conductive layers.

### Patent 3: US20230015442A1 — Method for separating and recovering lignin and meltable flowable biolignin …

| Patent Number | US20230015442A1 |
| --- | --- |
| Title | Method for separating and recovering lignin and meltable flowable biolignin … |
| Assignee | Not disclosed in the available patent text. |
| Jurisdiction | US |
| Publication Year | 2023 |
| Priority Date | Not available from source |
| Legal Status | Not available from source |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Mentions lignin nitrile rubber compositions using dry lignin powder with nitrile rubber or acrylonitrile butadiene (NBR) where lignin acts as a nano-filler. |

#### Polymerization / Synthesis Method

Biomass: Value not specified.

Lignin solvent: n-butanol, butyl acetate, butyl ester, furfural

Carrier fluid: Value not specified.

#### Relevant Experimental Evidence

No specific experimental examples disclosed in the supplied evidence.

#### Technical Relevance

Discusses the integration of lignin with nitrile rubber (acrylonitrile butadiene) to form composites, highlighting the limitations of conventional dry lignin powder as a filler.

### Patent 4: US10869391B2 — Garment-type electronic device and method for producing same

| Patent Number | US10869391B2 |
| --- | --- |
| Title | Garment-type electronic device and method for producing same |
| Assignee | Not disclosed in the available patent text. |
| Jurisdiction | US |
| Publication Year | 2020 |
| Priority Date | Not available from source |
| Legal Status | Not available from source |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Uses stretchable conductor compositions containing synthetic rubbers (which can include NBR) for garment-type electronic devices. |

#### Polymerization / Synthesis Method

Curing Temperature: Room temperature

Curing Time: 24 hours

Silicone resin thickness: 5 mm

Stretching: 10 %

#### Relevant Experimental Evidence

Example 5: Two-component curable silicone resin poured into a screen to a thickness of 5 mm and cured at room temperature over 24 hours, evaluated for electrical conductivity maintenance under 10% stretching.

Example 1: Evaluated level difference at the boundary between the electrode portion and wiring portion, and electrical conductivity maintenance under 10% stretching.

#### Technical Relevance

Demonstrates the formulation of stretchable conductive inks/pastes using synthetic rubbers and resins for flexible electronics.

### Patent 5: US12486386B2 — Process for regenerating a monolithic, macro-structural, inter-penetrating …

| Patent Number | US12486386B2 |
| --- | --- |
| Title | Process for regenerating a monolithic, macro-structural, inter-penetrating … |
| Assignee | Not disclosed in the available patent text. |
| Jurisdiction | US |
| Publication Year | 2025 |
| Priority Date | Not available from source |
| Legal Status | Not available from source |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Employs sulfidic metathesis to regenerate vulcanized rubbers, which can include NBR or other diene-based elastomers. |

#### Polymerization / Synthesis Method

Organometallic compound ratio: 0.1 to 5.0 parts per hundred parts vulcanized rubber particles

Reaction Temperature: 100-150 °C

Particle Size: 30 mesh (ground tire rubber particles)

Particle Size: greater than 200 mesh

#### Relevant Experimental Evidence

No specific experimental examples disclosed in the supplied evidence.

#### Technical Relevance

Discloses a method for preparing modified rubbers via sulfidic metathesis of vulcanized rubber particles using organometallic compounds, useful for recycling diene elastomers.

### Patent 6: US11971683B2 — Electrophotographic electro-conductive member, process cartridge, and …

| Patent Number | US11971683B2 |
| --- | --- |
| Title | Electrophotographic electro-conductive member, process cartridge, and … |
| Assignee | Not disclosed in the available patent text. |
| Jurisdiction | US |
| Publication Year | 2024 |
| Priority Date | Not available from source |
| Legal Status | Not available from source |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Uses low-acrylonitrile NBR (such as N215SL, which is a low-acrylonitrile NBR grade) for domain formation in electro-conductive layers. |

#### Polymerization / Synthesis Method

Kneader capacity: 6 L

Kneader filling rate: 70 vol %

Blade rotation speed: 30 rpm

Mixing Time 1: 16 minutes

Mixing Time 2: 18 minutes

Relative Humidity 1: 50 %

Relative Humidity 2: 80 %

Conditioning Time: 48 hours

Acrylic polyol solution: 1000 parts (solid content: 100 parts)

Caprolactone-modified acrylic polyol solution: 100 parts (solid content: 70 mass %)

Drying Temperature: 90 °C

Drying Time: 30 minutes

Second rubber type: BR (150B), IR (IR2200L), NBR (N215SL)

#### Relevant Experimental Evidence

Example 1: Preparation of Carbon Masterbatch (CMB) for domain formation using a 6 L pressurized kneader at 70 vol% filling rate and 30 rpm blade speed, mixing for 16 and 18 minutes. Second rubber includes NBR (N215SL) with Mooney viscosity of 45.

Example 2: Preparation of a coating solution using 1000 parts acrylic polyol solution (100 parts solid content) and caprolactone-modified acrylic polyol, coated and dried at room temperature for 30 minutes, then at 90°C.

Comparative Examples 8 and 9: Observed matrix-domain structures with 0% of domains satisfying specific structural requirements (B1) and (B2).

#### Technical Relevance

Discloses the use of specific NBR grades (e.g., N215SL, a low-acrylonitrile NBR) in matrix-domain electro-conductive layers to suppress image fogging.

### Patent 7: US8557921B2 — Production of meta-block copolymers by polymer segment interchange

| Patent Number | US8557921B2 |
| --- | --- |
| Title | Production of meta-block copolymers by polymer segment interchange |
| Assignee | Not disclosed in the available patent text. |
| Jurisdiction | US |
| Publication Year | 2013 |
| Priority Date | Not available from source |
| Legal Status | Not available from source |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Uses HNBR (hydrogenated nitrile butadiene rubber) in cross-metathesis reactions to prepare block copolymers. |

#### Polymerization / Synthesis Method

HPBD: 0.25 g

HNBR: 0.25 g

Reaction Temperature 1: 95 °C

Reaction Temperature 2: 105 °C

Grubbs II catalyst: 8 mg

Grubbs II catalyst: 9 mg

Fumaryl-modified polycarbonate: 0.25 g

Poly(ethylene-co-octene-co-butadiene): 0.25 g

Poly(ethylene-co-butadiene): 0.10 g

Poly(ethylene-co-octene-co-butadiene): 0.40 g

Tetrahydrofuran: 30 ml

Tetrahydrofuran: 50 ml

Recovered polymer product: 0.45 g

Recovered polymer product: 0.47 g

Recovered polymer product: 0.71 g

#### Relevant Experimental Evidence

Example 1: A toluene solution of 0.25 g HPBD and 0.25 g HNBR warmed to 95°C, reacted with 8 mg Grubbs II metathesis catalyst, yielding 0.45 g of recovered block copolymer after removing volatiles under reduced pressure.

Example 6: A toluene solution of 0.25 g fumaryl-modified polycarbonate and 0.25 g poly(ethylene-co-octene-co-butadiene) warmed to 105°C, reacted with 9 mg Grubbs II catalyst, yielding 0.47 g polymer.

Example 7: A toluene solution of 0.10 g poly(ethylene-co-butadiene) and 0.40 g poly(ethylene-co-octene-co-butadiene) warmed to 105°C, yielding 0.47 g recovered polymer analyzed by CRYSTAF.

Example 10: Metathesis product treated with 50 ml THF overnight to extract non-metathesized components, yielding 0.71 g recovered polymer.

#### Technical Relevance

Demonstrates polymer segment interchange via olefin metathesis using HNBR to synthesize novel block copolymers with tailored Tg and solubility parameters.

### Patent 8: US11137716B2 — Process cartridge and electrophotographic apparatus

| Patent Number | US11137716B2 |
| --- | --- |
| Title | Process cartridge and electrophotographic apparatus |
| Assignee | Not disclosed in the available patent text. |
| Jurisdiction | US |
| Publication Year | 2021 |
| Priority Date | Not available from source |
| Legal Status | Not available from source |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Uses Nipol DN401LL (which is a low-acrylonitrile NBR grade, ~18% AN content) in electro-conductive rubber compositions. |

#### Polymerization / Synthesis Method

Acrylonitrile butadiene rubber (Nipol DN401LL): 70 parts

Epichlorohydrin/ethylene oxide/allyl glycidyl ether terpolymer: 30 parts

Kneader capacity: 6 L

Kneader filling rate: 70 vol %

Blade rotation speed: 30 rpm

Mixing Time 1: 16 minutes

Mixing Time 2: 20 minutes

Butyl rubber (JSR Butyl 065): 100 parts

Calcium carbonate (Nanox #30): 70 parts

Zinc oxide: 7 parts

Zinc stearate: 2.8 parts

CMB 1: 25 parts

MRC 1: 85 parts

Sulfur: 3 parts

Tetramethylthiuram disulfide: 1 part

Epichlorohydrin rubber (EPICHLOMER CG102): 100 parts

Adekacizer LV70: 3 parts

Calcium carbonate: 60 parts

Zinc oxide: 5 parts

Sulfur: 1.8 parts

Carbon black (ASAHI #35G): 40 parts

Zinc stearate: 3.0 parts

Kneader capacity: 7 L

Dibenzothiazyl disulfide: 2.5 parts

Tetraethylthiuram disulfide: 2.0 parts

Sulfur: 3.0 parts

Foaming Time: 15 minutes

#### Relevant Experimental Evidence

Example: Mixing 70 parts NBR (Nipol DN401LL) and 30 parts epichlorohydrin terpolymer using a 6 L pressure kneader at 70 vol% filling rate and 30 rpm for 16 minutes.

Example: Compounding 100 parts butyl rubber with 70 parts calcium carbonate, 7 parts zinc oxide, and 2.8 parts zinc stearate.

Example: Mixing 25 parts CMB 1 and 85 parts MRC1, followed by adding 3 parts sulfur and 1 part tetramethylthiuram disulfide, mixing for 20 minutes.

Example: Compounding 100 parts epichlorohydrin rubber with 3 parts Adekacizer LV70, 60 parts calcium carbonate, 5 parts zinc oxide, and 1.8 parts sulfur.

#### Technical Relevance

Provides detailed compounding recipes utilizing low-acrylonitrile NBR (Nipol DN401LL) in electro-conductive matrix-domain structures to prevent transfer black spots.

### Patent 9: US11286376B2 — Process for regenerating a monolithic, macro-structural, inter-penetrating …

| Patent Number | US11286376B2 |
| --- | --- |
| Title | Process for regenerating a monolithic, macro-structural, inter-penetrating … |
| Assignee | Not disclosed in the available patent text. |
| Jurisdiction | US |
| Publication Year | 2022 |
| Priority Date | Not available from source |
| Legal Status | Not available from source |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Relates to sulfidic metathesis of vulcanized rubbers (which can include NBR) to form interpenetrating networks. |

#### Polymerization / Synthesis Method

Organometallic compound ratio: 0.1 to 5.0 parts per hundred parts vulcanized rubber particles

Reaction Temperature: 100-150 °C

Laminate spacing: 10 nm to 5 microns

Anisotropy ratio: 1.1:1 to 3:1

#### Relevant Experimental Evidence

No specific experimental examples disclosed in the supplied evidence.

#### Technical Relevance

Describes the creation of a rubber-based heterogeneous matrix with an interpenetrating network of elastomers (e.g., SBR, NR, GTR) via sulfidic metathesis.

### Patent 10: US6693160B1 — Functionalized monomers for synthesis of rubbery polymers

| Patent Number | US6693160B1 |
| --- | --- |
| Title | Functionalized monomers for synthesis of rubbery polymers |
| Assignee | Not disclosed in the available patent text. |
| Jurisdiction | US |
| Publication Year | 2004 |
| Priority Date | Not available from source |
| Legal Status | Not available from source |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Synthesizes amine-functionalized monomers that can be copolymerized with conjugated diolefins (like butadiene and acrylonitrile) to produce functionalized rubbery polymers (including NBR). |

#### Polymerization / Synthesis Method

Butadiene ratio: 80 %

Styrene ratio: 19 %

PES ratio: 1 %

PES in hexane: 101.4 g (93% purity)

Butadiene in hexane: 20.27 %

Monomer weight: 100 g

n-Butyllithium: 155.9 mmoles (2.5% of 6329 mmoles)

Monomer conversion: 96 %

DVB conversion: 73 %

DVB conversion: 80 %

Polymerization Time: 100 minutes

Hexane elution time: 5.7 minutes

CSTR retention time 1: 1 hour

CSTR retention time 2: 0.5 hours

Uncured viscosity strain: 15 %

Piperidine: 1 mole

Aqueous sodium hydroxide: 20-35 %

Divinylbenzene: 1030 g (80% active, 824 g pure)

Pyrrolidine: 450 g (528 ml)

TMEDA: 0.48 ml

n-BuLi: 1.5 ml (1.6 M)

TMEDA: 0.52 ml

n-BuLi: 2.0 ml (1.6 M)

Tin coupled PES-styrene-butadiene: 0.25, 0.5, 2.0, 5.0 % PES

Silica coupling agent: 0 to 5 phs

Silica: 55 phr

Processing oil: 10 phr

Zinc oxide: 3 phr

Stearic acid: 2 phr

Antioxidant: 1.5 phr

Sulfenamide accelerator: 1.5 phr

Sulfur: 1.4 phr

#### Relevant Experimental Evidence

Examples 103-105: Linear polymerization of 1% PES / 19% Styrene / 80% Butadiene. Premix prepared with 101.4 g of 93% PES in hexane added to 20.27% butadiene in hexane. Total monomer conversion reached 96%.

Example 33: Synthesis of functionalized monomer by reacting 1030 g of 80% divinylbenzene (824 g pure) with 450 g dry pyrrolidine under nitrogen, followed by addition of n-butyllithium at 2.5% molar ratio, achieving 73-80% DVB conversion.

Example 14: Preparation of 25/75 SBR containing 0.5 wt% 2-(N-hexamethyleneimino)-methyl 1,3-butadiene, with polymerization times of 90 and 100 minutes.

Example 22: Preparation of high trans 10/90 SBR containing 0.5% pyrrolidine functional groups, showing 74.5% trans-1,4-polybutadiene units and 7.6% polystyrene.

#### Technical Relevance

Discloses synthesis of amine-functionalized monomers and their copolymerization with dienes to produce functionalized elastomers with low hysteresis and high filler affinity.

### Patent 11: US7041761B2 — Functionalized monomers for synthesis of rubbery polymers

| Patent Number | US7041761B2 |
| --- | --- |
| Title | Functionalized monomers for synthesis of rubbery polymers |
| Assignee | Not disclosed in the available patent text. |
| Jurisdiction | US |
| Publication Year | 2006 |
| Priority Date | Not available from source |
| Legal Status | Not available from source |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Copolymerization of dienes with functionalized monomers to produce rubbery polymers with low hysteresis. |

#### Polymerization / Synthesis Method

Butadiene ratio: 80 %

Styrene ratio: 19 %

PES ratio: 1 %

PES in hexane: 101.4 g (93% purity)

Butadiene in hexane: 20.27 %

Divinylbenzene: 1030 g (80% active, 824 g pure)

n-Butyllithium: 155.9 mmoles

Pinane hydroperoxide: 1.82 g (44% active)

Monomer conversion: 96 %

Shortstop conversion: 65 %

Polymerization Time: 100 minutes

CSTR retention time 1: 1 hour

CSTR retention time 2: 0.5 hours

Sodium naphthalenesulfonate-formaldehyde dispersant: 4.76 g (47.5% active)

Tripotassium phosphate: 7.2 g

Disproportionated rosin acid: 140 g (20% solution)

Unsaturated fatty acids: 532 g (10% solution)

Aqueous potassium hydroxide: 10 %

Styrene: 580 g

PES: 22.5 g (92% purity)

tert-Dodecylmercaptan: 4.5 g

Latex solid content: 24.7 %

Bound styrene: 24.0 %

Bound PES: 0.9 %

Daxad 14B: 33 g (47.5% active)

Potassium chloride: 25.5 g

Disproportionated rosin acid: 767 g

Styrene: 3245 g

PES: 59.8 g (92% purity)

tert-Dodecylmercaptan: 16.0 g

Pinane hydroperoxide: 10 g (55% active)

Isopropylhydroxylamine: 44 g (15% active)

Sulfuric acid: 10 % wt.

PAMS: 20 g (100% purity)

Isopropylhydroxylamine: 8 g (15% active)

#### Relevant Experimental Evidence

Example 122: Emulsion polymerization of styrene (580 g), butadiene, and PES (22.5 g, 92% purity) using Daxad 14B (4.76 g), disproportionated rosin acid (140 g), and unsaturated fatty acids (532 g). Initiated with pinane hydroperoxide (1.82 g) at 10°C, shortstopped at 65% conversion, yielding a latex with 24.7% solids. Bound styrene was 24.0%, bound PES was 0.9%.

Example 124: Large-scale emulsion polymerization using 3245 g styrene, 59.8 g PES, 16.0 g tert-dodecylmercaptan, and 10 g pinane hydroperoxide (55% active). Shortstopped at 65% conversion with isopropylhydroxylamine, coagulated with 10% sulfuric acid at pH 3-4.

Example 125: Emulsion polymerization of styrene (580 g), butadiene, and PAMS (20 g, 100% purity) using 4.4 g tert-dodecylmercaptan, initiated with pinane hydroperoxide at 10°C, shortstopped at 65% conversion with isopropylhydroxylamine.

#### Technical Relevance

Provides detailed emulsion polymerization recipes for functionalized diene-based rubbers, demonstrating control over conversion, molecular weight, and functional monomer incorporation.

### Patent 12: US5567815A — Teritary amine containing antonic initiators used in preparing polymers and …

| Patent Number | US5567815A |
| --- | --- |
| Title | Teritary amine containing antonic initiators used in preparing polymers and … |
| Assignee | Not disclosed in the available patent text. |
| Jurisdiction | US |
| Publication Year | 1996 |
| Priority Date | Not available from source |
| Legal Status | Not available from source |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Anionic polymerization of dienes using tertiary amine-containing initiators to produce elastomers with reduced hysteresis. |

#### Polymerization / Synthesis Method

1,3-Butadiene: 500 g

Hexane: 2000 g

n-Butyl lithium: 10 mmoles

Polybutadiene molecular weight: 140,700

Mw/Mn: 1.31

Cis-1,4 units: 36.5 %

Trans-1,4 units: 52.7 %

Vinyl units: 10.8 %

#### Relevant Experimental Evidence

Example 1: Polymerization of 500 g 1,3-butadiene in 2000 g hexane initiated with an anionic initiator system (formed by reacting DIPB, a secondary amine, and n-butyl lithium). The recovered polybutadiene had a molecular weight of 140,700, Mw/Mn of 1.31, and a microstructure of 36.5% cis-1,4, 52.7% trans-1,4, and 10.8% vinyl units.

#### Technical Relevance

Discloses a method for preparing tertiary amine-functionalized anionic initiators and using them to synthesize diene elastomers with improved filler interaction and reduced hysteresis.

### Patent 13: US6995224B2 — Functionalized monomers for synthesis of rubbery polymers

| Patent Number | US6995224B2 |
| --- | --- |
| Title | Functionalized monomers for synthesis of rubbery polymers |
| Assignee | Not disclosed in the available patent text. |
| Jurisdiction | US |
| Publication Year | 2006 |
| Priority Date | Not available from source |
| Legal Status | Not available from source |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Copolymerization of dienes with functionalized monomers to produce rubbery polymers with low hysteresis. |

#### Polymerization / Synthesis Method

Butadiene ratio: 80 %

Styrene ratio: 19.5 %

Pyr-AMS ratio: 0.5 %

Butadiene in hexane: 20.27 %

PAMS in hexane: 101.4 g (93% purity)

Monomer weight: 100 g

n-Butyllithium: 155.9 mmoles

Monomer conversion: 96 %

DVB conversion: 73 %

DVB conversion: 80 %

Polymerization Time: 100 minutes

CSTR retention time 1: 1 hour

CSTR retention time 2: 0.5 hours

Pyr-AMS consumption: 26 % (at 2 hours)

SiCl4 residence time: 90 minutes

Sodium hydroxide: 30 %

2,3-dibromopropane: 0.1 mol

Hexamethyleneimine: 0.4 mol

Pyr-AMS: 44.2 g (100% purity)

1,3-butadiene in hexane: 19.64 %

Styrene in hexane: 20.27 %

Isopropylalcohol: 10 %

Silica: 55 phr

Processing oil: 10 phr

Zinc oxide: 3 phr

Stearic acid: 2 phr

Antioxidant: 1.5 phr

Sulfenamide accelerator: 1.2 phr

Sulfur: 1.4 phr

#### Relevant Experimental Evidence

Example 123: Synthesis of a linear 0.5% Pyr-AMS / 19.5% Styrene / 80% Butadiene SSBR copolymer. Monomer premix prepared by adding 44.2 g of 100% Pyr-AMS to 36,000 g of 19.64% 1,3-butadiene in hexane. Copolymerized with styrene in hexane and coupled with silicon tetrachloride.

Example: Synthesis of functionalized monomer by reacting 0.1 mol 2,3-dibromopropane with 0.4 mol hexamethyleneimine in 30% aqueous NaOH at 60°C.

Example: Continuous polymerization in two CSTRs with a total residence time of 90 minutes, followed by coupling with SiCl4, shortstopped with isopropyl alcohol.

#### Technical Relevance

Details the synthesis of pyrrolidine- and amine-functionalized styrene-butadiene-diene terpolymers, demonstrating improved silica and carbon black dispersion.

### Patent 14: US6562929B2 — Conjugated diene-based rubber and method of producing the same, oil extended …

| Patent Number | US6562929B2 |
| --- | --- |
| Title | Conjugated diene-based rubber and method of producing the same, oil extended … |
| Assignee | Not disclosed in the available patent text. |
| Jurisdiction | US |
| Publication Year | 2003 |
| Priority Date | Not available from source |
| Legal Status | Not available from source |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Synthesizes a low-acrylonitrile NBR-like terpolymer containing 9 to 30% by mass of an olefinically unsaturated nitrile monomer (acrylonitrile), 10 to 50% by mass of an aromatic vinyl monomer (styrene), and 20 to 81% by mass of a conjugated diene monomer (butadiene). |

#### Polymerization / Synthesis Method

Olefinically unsaturated nitrile monomer (acrylonitrile): 9 to 30 % by mass

Aromatic vinyl monomer (styrene): 10 to 50 % by mass

Conjugated diene monomer (butadiene): 20 to 81 % by mass

Mooney viscosity [ML1+4 (100°C)]: 20 to 200

Glass transition point: -60 to 0 °C

Glass transition width: 20 °C or less

Extending oil: 10 to 60 parts by mass per 100 parts rubber

#### Relevant Experimental Evidence

Example 1: Copolymerization of monomers containing 9-30% acrylonitrile, 10-50% styrene, and 20-81% butadiene. Acrylonitrile is added portionwise to the polymerization system containing styrene and butadiene, and the remainder is added intermittently to maintain random distribution and a narrow glass transition width (20°C or less). Mooney viscosity of the resulting rubber was in the range of 20 to 200.

#### Technical Relevance

Directly addresses the synthesis of low-acrylonitrile NBR terpolymers with highly randomized monomer distribution, narrow glass transition width, and excellent compatibility with silica fillers.

## 3. Cross-Patent Comparison & Synthesis Trends

Monomer Content Ranges: US6562929B2 specifies a highly randomized terpolymer containing 9 to 30% by mass of acrylonitrile, 10 to 50% styrene, and 20 to 81% butadiene. US11137716B2 utilizes Nipol DN401LL, a commercial low-acrylonitrile NBR grade (~18% acrylonitrile), while US11971683B2 utilizes N215SL, another low-acrylonitrile NBR grade.

Polymerization Processes: Emulsion polymerization is detailed in US7041761B2 for functionalized diene rubbers. Anionic solution polymerization is utilized in US5567815A, US6693160B1, and US6995224B2 to prepare functionalized diene elastomers. US8557921B2 introduces a distinct metathesis-driven segment interchange process in solution to form block copolymers from HNBR.

Emulsifier and Initiator Systems: US7041761B2 details a cold emulsion system (10°C) using disproportionated rosin acid and unsaturated fatty acid potassium salts as emulsifiers, initiated by pinane hydroperoxide. In contrast, the anionic solution systems (US5567815A, US6693160B1) utilize n-butyllithium or functionalized lithium amides in hydrocarbon solvents at elevated temperatures.

Chain-Transfer and Coagulation: US7041761B2 utilizes tert-dodecylmercaptan as a chain-transfer agent to control molecular weight and coagulates the latex using 10% sulfuric acid at pH 3-4. The solution polymerization patents typically terminate reactions with alcohols (e.g., isopropyl alcohol) and recover the polymer by vacuum stripping or solvent precipitation.

Compounding and Applications: US11137716B2 and US11971683B2 focus on compounding low-acrylonitrile NBR into matrix-domain electro-conductive layers with epichlorohydrin rubbers, utilizing sulfur vulcanization systems with zinc oxide and stearic acid to control electrical impedance and physical properties.

## 4. Conclusion

The synthesis of high-performance Low Acrylonitrile NBR requires precise control over monomer randomness, molecular weight distribution, and functionalization. Based on the patent evidence, cold emulsion polymerization at 10°C using disproportionated rosin acid emulsifiers and tert-dodecylmercaptan chain transfer agents is recommended for producing highly randomized terpolymers with narrow glass transition widths (<20°C) and Mooney viscosities of 20-200. For applications requiring low hysteresis and high filler interaction, anionic solution copolymerization with amine-functionalized monomers (such as PES or PAMS) initiated by functionalized lithium amides is highly effective. Compounding low-acrylonitrile grades (such as Nipol DN401LL or N215SL) into matrix-domain structures with epichlorohydrin rubbers provides optimal electro-conductive properties for specialized engineering applications. Future research should focus on optimizing metathesis-driven segment interchange to create thermoplastic NBR elastomers with tailored block architectures.

## 5. References

EP3715957B1 | Electro-conductive member, process cartridge image forming apparatus and a … | Not disclosed in the available patent text. | EP | 2022 | https://patents.google.com/patent/EP3715957B1/en

US11340553B2 | Process cartridge and electrophotographic apparatus | Not disclosed in the available patent text. | US | 2022 | https://patents.google.com/patent/US11340553B2/en

US20230015442A1 | Method for separating and recovering lignin and meltable flowable biolignin … | Not disclosed in the available patent text. | US | 2023 | https://patents.google.com/patent/US20230015442A1/en

US10869391B2 | Garment-type electronic device and method for producing same | Not disclosed in the available patent text. | US | 2020 | https://patents.google.com/patent/US10869391B2/en

US12486386B2 | Process for regenerating a monolithic, macro-structural, inter-penetrating … | Not disclosed in the available patent text. | US | 2025 | https://patents.google.com/patent/US12486386B2/en

US11971683B2 | Electrophotographic electro-conductive member, process cartridge, and … | Not disclosed in the available patent text. | US | 2024 | https://patents.google.com/patent/US11971683B2/en

US8557921B2 | Production of meta-block copolymers by polymer segment interchange | Not disclosed in the available patent text. | US | 2013 | https://patents.google.com/patent/US8557921B2/en

US11137716B2 | Process cartridge and electrophotographic apparatus | Not disclosed in the available patent text. | US | 2021 | https://patents.google.com/patent/US11137716B2/en

US11286376B2 | Process for regenerating a monolithic, macro-structural, inter-penetrating … | Not disclosed in the available patent text. | US | 2022 | https://patents.google.com/patent/US11286376B2/en

US6693160B1 | Functionalized monomers for synthesis of rubbery polymers | Not disclosed in the available patent text. | US | 2004 | https://patents.google.com/patent/US6693160B1/en

US7041761B2 | Functionalized monomers for synthesis of rubbery polymers | Not disclosed in the available patent text. | US | 2006 | https://patents.google.com/patent/US7041761B2/en

US5567815A | Teritary amine containing antonic initiators used in preparing polymers and … | Not disclosed in the available patent text. | US | 1996 | https://patents.google.com/patent/US5567815A/en

US6995224B2 | Functionalized monomers for synthesis of rubbery polymers | Not disclosed in the available patent text. | US | 2006 | https://patents.google.com/patent/US6995224B2/en

US6562929B2 | Conjugated diene-based rubber and method of producing the same, oil extended … | Not disclosed in the available patent text. | US | 2003 | https://patents.google.com/patent/US6562929B2/en