# Patent Landscape for High-Acrylonitrile NBR Synthesis and Controlled Emulsion/Organic-Solvent Polymerization

## 1. Abstract

This report synthesizes two primary patents relevant to high-acrylonitrile nitrile butadiene rubber (NBR) synthesis and process control. The target material is a butadiene–acrylonitrile copolymer enriched in acrylonitrile, typically requiring careful monomer feed control, polymerization temperature management, and molecular-weight regulation to achieve the desired high-ACN grade while maintaining processability. EP2478021B1 focuses directly on nitrile rubber production in organic solvents using free-radical polymerization of a conjugated diene, an α,β-unsaturated nitrile, and optional comonomers in the presence of a modifier; the patent emphasizes solution-phase synthesis, RAFT-like control chemistry, and examples using acrylonitrile/butadiene feeds at 37/63 phm under 3 bar and 100°C. It also discloses terpolymer variants incorporating hydroxyethyl acrylate or HDODA and post-polymerization isolation by ethanol precipitation. US7592409B2 is not an NBR manufacturing patent per se, but it is highly relevant because it discloses controlled emulsion polymerization technology that explicitly includes block polymers containing acrylonitrile/methacrylonitrile and conjugated diolefin segments, including acrylonitrile/butadiene-based B blocks. The patent’s core contribution is in-situ emulsifier formation from latent surfactant/surfactant activator pairs, enabling controlled emulsion polymerization with conventional aqueous media, rapid initiation, and stable latex formation. Across the two patents, the main process trends are: solution polymerization in organic solvent with modifier-mediated control for direct NBR synthesis, and controlled emulsion polymerization with in-situ emulsification for architecturally complex acrylonitrile-containing block copolymers. The evidence supports high-ACN NBR synthesis strategies centered on monomer ratio selection, oxygen exclusion, controlled radical initiation, and solvent/emulsion process design rather than hydrogenation or post-modification routes.

## 2. Primary Patent Evidence

### Patent 1: EP2478021B1 — Nitrile rubbers and production of same in organic solvents

| Patent Number | EP2478021B1 |
| --- | --- |
| Title | Nitrile rubbers and production of same in organic solvents |
| Assignee | Not available from source |
| Jurisdiction | EP |
| Publication Year | 2015 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: The patent discloses free-radical preparation of nitrile rubbers in organic solvent, using at least one conjugated diene and at least one α,β-unsaturated nitrile in the presence of a modifier. The examples show solution polymerization in dimethylacetamide with acrylonitrile and 1,3-butadiene, followed by precipitation in ethanol and vacuum drying; some examples also introduce termonomers such as hydroxyethyl acrylate or HDODA.

Vazo® 88: 284.9 mg — Example 1

Vazo® 88: 1.17 mmol — Example 1

Vazo® 88: 0.31 phm — Example 1

DoPAT: 204 mg — Example 1

DoPAT: 0.583 mmol — Example 1

DoPAT: 0.22 phm — Example 1

Dimethylacetamide: 50 ml — Example 1

Dimethylacetamide: 51 phm — Example 1

Acrylonitrile: 43 ml — Example 1

Acrylonitrile: 653.3 mmol — Example 1

Acrylonitrile: 37 phm — Example 1

1,3-Butadiene: 90 ml — Example 1

1,3-Butadiene: 1077 mmol — Example 1

1,3-Butadiene: 63 phm — Example 1

Pressure: 3 bar — Example 1

Reaction temperature: 100°C — Example 1

Polymerization time: 9 hours — Example 1

Hydroxyethyl acrylate (HEA): added to solvent prior to argon degassing — Example 6

Reaction time: 6 hours — Example 6

Final conversion: 39% — Example 6

Regulator amount: 2.22 phm — Example 7

Reaction time: 9 h — Example 7

Final conversion: 48% — Example 7

Styrene: 2.79 g — Example 8

Styrene: 26.8 mmol — Example 8

Styrene: 50 phm — Example 8

Temperature: 100°C — Example 8

Reaction time: 13 hours — Example 8

Final conversion: 9.2% — Example 8

Vazo® 88: amount shown in Table 7 — Examples 17-23

DoPAT: amount shown in Table 7 — Examples 17-23

DMAc: volume shown in Table 7 — Examples 17-23

Acrylonitrile: amount shown in Table 7 — Examples 17-23

HDODA: added in Examples 17-21 — Examples 17-23

HEA: additionally added in Example 21 — Examples 17-23

1,3-Butadiene: amount shown in Table 7 — Examples 17-23

Pressure: 3 bar — Examples 17-23

Reaction temperature: 100°C — Examples 17-23

Polymerization time: 9 hours — Examples 17-23

Vazo® 88 post-dose: 128 mg — Examples 18, 20, 23

Vazo® 88 post-dose: 0.523 mmol — Examples 18, 20, 23

Vazo® 88 post-dose: 0.15 phm — Examples 18, 20, 23

Post-dose solvent: 5 ml dimethylacetamide — Examples 18, 20, 23

#### Relevant Experimental Evidence

Example 1: Direct solution polymerization of acrylonitrile/butadiene in DMAc at 100°C and 3 bar produced NBR using Vazo® 88 and DoPAT.

Example 6: A terpolymer containing hydroxyethyl acrylate was prepared by the same solution route and stopped after 6 hours at 39% conversion.

Example 7: Lower regulator loading (2.22 phm) was used to deliberately obtain low-molecular-weight NBR, reaching 48% conversion after 9 hours.

Example 8: The low-Mn NBR from Example 7 was chain-extended with styrene to form an NBR-block-styrene terpolymer at 100°C.

Example 17: Acrylonitrile/butadiene polymerization was repeated with additional termonomers (HDODA and/or HEA) under the same 3 bar, 100°C solution conditions.

#### Technical Relevance

This patent is directly relevant because it discloses organic-solvent synthesis of nitrile rubbers from acrylonitrile and butadiene, with explicit control over monomer feed, regulator level, and temperature. The solution process is especially pertinent for high-acrylonitrile grades where composition control and controlled molecular weight are critical.

### Patent 2: US7592409B2 — Styrene acrylonitrile isoprene triblock copolymer

| Patent Number | US7592409B2 |
| --- | --- |
| Title | Styrene acrylonitrile isoprene triblock copolymer |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2009 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: The patent discloses controlled emulsion polymerization using an in-situ formed emulsifier generated from a latent surfactant and a surfactant activator in aqueous medium. Although many examples are styrene-based, the claims and abstract explicitly extend the method to block polymers containing acrylonitrile or methacrylonitrile with conjugated diolefin monomers such as isoprene and butadiene, enabling A-B-A triblock architectures.

Latent surfactant: ~0.2 grams — Example 1

Styrene: 5 milliliters — Example 1

Surfactant activator water phase: 5 milliliters — Example 1

Styrene: 1,000 grams — Example 2

Oleic acid: 60.0 grams — Example 2

Dibenzyltrithiocarbonate: 7.2 grams — Example 2

RO water: 4,000 grams — Example 2

Potassium persulfate: 40.0 grams — Example 2

Tripotassium phosphate: 40.0 grams — Example 2

Potassium hydroxide: 16.4 grams — Example 2

Reaction temperature: 65° C — Example 2

Complete conversion time: less than 1.5 hours — Example 2

Styrene: 1,000 grams — Example 3

Hexadecyl half ester of maleic acid: 60.0 grams — Example 3

Dibenzyltrithiocarbonate: 7.2 grams — Example 3

RO water: 4,000 grams — Example 3

Potassium persulfate: 40.0 grams — Example 3

Tripotassium phosphate: 40.0 grams — Example 3

Potassium hydroxide: 16.4 grams — Example 3

Reaction temperature: 65° C — Example 3

Complete conversion time: less than 3 hours — Example 3

0.6 phr K/Oleate soap solution: added prior to isolation — Example 3

RO water: 200 — Example 4

RO water: 241 — Example 5

RO water: 197.1 — Example 5

RO water: 84.7 — Example 5

Styrene: 1,000 grams — Example 6

Oleic acid: 60.0 grams — Example 6

PBN: 10.0 grams — Example 6

RO water: 4,000 grams — Example 6

Potassium persulfate: 40.0 grams — Example 6

Tripotassium phosphate: 40.0 grams — Example 6

Potassium hydroxide: 16.4 grams — Example 6

Reaction temperature: 75° C — Example 6

Complete conversion time: less than 2 hours — Example 6

Styrene: 50 grams (0.48 moles) — Example 8

Oleic acid: 3.0 grams (0.0106 moles) — Example 8

PBN: 0.44 grams (0.002485 moles) — Example 8

Distilled water: 200 grams — Example 8

Potassium persulfate: 2.06 grams (0.00762 moles) — Example 8

Tripotassium phosphate: 2.13 grams (0.01 moles) — Example 8

Potassium hydroxide: 0.9 grams (0.014 moles) — Example 8

Reaction temperature: 65° C — Example 8

Complete conversion time: about 7 hours — Example 8

Styrene: 200 grams (1.923 moles) — Example 10

Oleic acid: 12.0 grams (0.0424 moles) — Example 10

PBN: 2.0 grams (0.0113 moles) — Example 10

Distilled water: 500 grams — Example 10

Potassium persulfate: 8.0 grams (0.296 moles) — Example 10

Tripotassium phosphate: 8.0 grams (0.0377 moles) — Example 10

Potassium hydroxide: 3.6 grams (0.056 moles) — Example 10

Reaction temperature: 75° C — Example 10

Complete conversion time: about 3.5 hours — Example 10

Styrene: 50.0 grams (0.48 moles) — Example 11

PIN: equimolar amount — Example 11

Complete conversion time: about 7 hours — Example 11

Styrene: 100 grams of about 22% solids latex — Example 12

Potassium persulfate: 0.5 grams (0.00184 moles) — Example 12

Distilled water: 100 milliliters — Example 12

n-Butyl acrylate: 22.0 grams (0.171 moles) — Example 12

Reaction temperature: about 65° C — Example 12

Weak exotherm: about 70° C — Example 12

Complete conversion time: about 2 hours — Example 12

Styrene: 50.0 grams (0.48 moles) — Example 13

Benzaldehyde: 0.31 grams (0.00292 moles) — Example 13

N-isopropylhydroxylamine: 1.4 grams of a 15% aqueous solution — Example 13

Room temperature: 1 hour — Example 13

Distilled water: 200 grams — Example 13

Potassium persulfate: 2.06 grams (0.00762 moles) — Example 13

Tripotassium phosphate: 2.13 grams (0.01 moles) — Example 13

Potassium hydroxide: 0.9 grams (0.014 moles) — Example 13

Reaction temperature: 75° C — Example 13

Complete conversion time: about 4 hours — Example 13

Styrene: 50.0 grams (0.48 moles) — Example 14

Dodecylbenzenesulfonic acid: 3.0 grams (0.0092 moles) — Example 14

Water: 1 milliliter — Example 14

Sodium nitrite: 0.171 grams (0.002485 moles) — Example 14

Distilled water: 200 grams — Example 14

Potassium persulfate: 2.06 grams (0.00762 moles) — Example 14

Tripotassium phosphate: 2.13 grams (0.01 moles) — Example 14

Potassium hydroxide: 0.74 grams (0.0115 moles) — Example 14

Reaction temperature: 75° C — Example 14

Complete conversion time: about 3 hours — Example 14

Styrene: 50 grams (0.48 moles) — Example 15

Oleic acid: 3.0 grams (0.0106 moles) — Example 15

1,1-Diphenylethylene (DPE): 0.448 grams (0.002485 moles) — Example 15

Distilled water: 200 grams — Example 15

Potassium persulfate: 2.06 grams (0.00762 moles) — Example 15

Tripotassium phosphate: 2.13 grams (0.01 moles) — Example 15

Potassium hydroxide: 0.92 grams (0.0143 moles) — Example 15

Reaction temperature: 75° C — Example 15

Complete conversion time: about 2 hours — Example 15

Styrene: 2,240 grams — Example 16

Oleic acid: 134.4 grams — Example 16

Dibenzyltrithiocarbonate: 16.0 grams — Example 16

RO water: 3,808 grams — Example 16

Potassium persulfate: 13.44 grams — Example 16

Tripotassium phosphate: 89.6 grams — Example 16

Potassium hydroxide: 36.96 grams — Example 16

Reaction temperature: 65° C — Example 16

Complete conversion time: less than 3 hours — Example 16

Latex solids: 38.9% — Example 16

Sodium nitrite: 0.69 grams (0.01 moles) — Example 17

Oleic acid: 3.0 grams (0.0106 moles) — Example 17

Styrene: 50 grams (0.48 moles) — Example 17

Acetic acid: 1.0 grams (0.0167 moles) — Example 17

Water: 2 grams — Example 17

Distilled water: 160 grams — Example 17

Potassium persulfate: 2.0 grams (0.00739 moles) — Example 17

Tripotassium phosphate: 2.0 grams (0.01 moles) — Example 17

Potassium hydroxide: 2.35 grams (0.0367 moles) — Example 17

Reaction temperature: 75° C — Example 17

Complete conversion time: about 2.5 hours — Example 17

Latex solids: 26.1% — Example 17

Styrene: 50 grams (0.48 moles) — Example 18

Oleic acid: 3.0 grams (0.0106 moles) — Example 18

Crude 1-chloro-1,1-diphenylethane: approximately 0.01 moles — Example 18

Distilled water: 200 grams — Example 18

Potassium persulfate: 2.0 grams (0.0074 moles) — Example 18

Tripotassium phosphate: 2.0 grams (0.0094 moles) — Example 18

Potassium hydroxide: 1.55 grams (0.0242 moles) — Example 18

Reaction temperature: 75° C — Example 18

Complete conversion time: about 4 hours — Example 18

Latex solids: 22.7% — Example 18

Styrene: 1,300 grams (12.5 moles) — Example 19

Oleic acid: 78.0 grams (0.2756 moles) — Example 19

Crude 1-chloro-1,1-diphenylethane: 39.0 grams — Example 19

Deionized RO water: 2,470 grams — Example 19

Potassium persulfate: 50.7 grams (0.1875 moles) — Example 19

Tripotassium phosphate: 50.7 grams (0.2388 moles) — Example 19

Potassium hydroxide: 29.5 grams (0.602 moles) — Example 19

Reaction temperature: 75° C — Example 19

Complete conversion time: about 5.5 hours — Example 19

Latex solids: 38.6% — Example 19

1-hexene: 25 grams — Example 20

n-Butyl acrylate: 25 grams — Example 20

Dipyridyl: 0.38 grams — Example 20

Oleic acid: 4.0 grams — Example 20

Ethyl 2-bromoisobutyrate: 0.47 grams — Example 20

85% KOH: 1.7 grams — Example 20

Distilled water: 139 milliliters — Example 20

Copper sulfate pentahydrate solution: 60.9 grams of a 1% aqueous solution — Example 20

Hydrazine hydrate: 2 drops — Example 20

Reaction temperature: about 67° C — Example 20

Reaction time: 1.5 hours — Example 20

Latex solids: 10.9% — Example 20

1-hexene incorporation: 5.5 mole % — Example 20

#### Relevant Experimental Evidence

Example 1: Demonstrated in-situ emulsification from latent surfactant/activator pairs in styrene/water systems.

Example 2: Showed RAFT-controlled emulsion polymerization at 65°C with complete conversion in less than 1.5 hours.

Example 3: Showed in-situ generated polymerizable surfactant enabling rapid conversion and stable latex formation.

Example 12: Demonstrated seeded emulsion chain extension to a block copolymer with n-butyl acrylate at about 65°C.

Example 20: Demonstrated ATRP emulsion copolymerization with 1-hexene and n-butyl acrylate, confirming broader controlled-emulsion scope.

#### Technical Relevance

This patent is relevant because its claims explicitly cover block polymers containing acrylonitrile or methacrylonitrile with conjugated diolefins such as butadiene or isoprene. Its in-situ emulsifier strategy is important for controlled aqueous synthesis routes that could be adapted to high-acrylonitrile NBR-related block architectures and latex processing.

## 3. Cross-Patent Comparison & Synthesis Trends

EP2478021B1 is the more direct high-ACN NBR synthesis disclosure: it uses acrylonitrile/butadiene solution polymerization in organic solvent, with explicit monomer feed levels of 37 phm ACN and 63 phm butadiene in Example 1.

US7592409B2 is broader and more platform-oriented: it does not exemplify NBR synthesis directly, but its claims explicitly include acrylonitrile/methacrylonitrile plus conjugated diolefin blocks, making it relevant to NBR-based block copolymers rather than conventional random NBR.

EP2478021B1 uses organic-solvent free-radical polymerization with modifier/RAFT-like control chemistry (DoPAT) and initiator Vazo® 88, whereas US7592409B2 centers on controlled emulsion polymerization with in-situ emulsifier formation and controlled radical methods such as RAFT, NMP, ATRP, and DT.

EP2478021B1 operates at 100°C and 3 bar with polymerization times of 6-9 hours in the examples, while US7592409B2 commonly uses 65-75°C and reaches complete conversion in roughly 1.5-7 hours depending on the control system.

EP2478021B1 isolates polymer by ethanol precipitation and vacuum drying after solvent polymerization; US7592409B2 generally forms stable latexes and uses stripping/coagulation only in selected examples.

For high-acrylonitrile NBR, EP2478021B1 provides the clearest evidence for direct composition control, while US7592409B2 provides a useful emulsion-processing framework for acrylonitrile-containing block copolymers and latex-based manufacturing.

## 4. Conclusion

The evidence indicates two complementary synthesis directions for high-acrylonitrile NBR-related materials. The most directly relevant route is EP2478021B1, which discloses solution polymerization of acrylonitrile and 1,3-butadiene in DMAc with controlled radical chemistry, oxygen exclusion, 3 bar butadiene feed, and 100°C initiation; this is the strongest patent evidence for direct NBR manufacture with tunable acrylonitrile content. US7592409B2 contributes a broader controlled-emulsion platform that explicitly encompasses acrylonitrile/diolefin block polymers and demonstrates rapid, stable latex formation via in-situ emulsifier generation. Based on the evidence, the recommended synthesis parameters for high-ACN NBR are: acrylonitrile-rich monomer feed control, rigorous oxygen removal, controlled radical initiation, and either organic-solvent solution polymerization for direct NBR or controlled emulsion polymerization when block architecture or latex processing is desired.

## 5. References

EP2478021B1 | Nitrile rubbers and production of same in organic solvents | Not disclosed | EP | 2015 | https://patents.google.com/patent/EP2478021B1/en

US7592409B2 | Styrene acrylonitrile isoprene triblock copolymer | Not disclosed | US | 2009 | https://patents.google.com/patent/US7592409B2/en