# Low Acrylonitrile NBR

## POLYMERIZATION / SYNTHESIS PATENT RESEARCH REPORT

### Abstract

The patent landscape for Low Acrylonitrile NBR (Nitrile Butadiene Rubber) reveals a focus on emulsion and solution polymerization processes. The major synthesis approaches involve the use of various emulsifiers, initiators, and chain transfer agents to control the polymerization reaction. Recurring chemistry includes the use of acrylonitrile content between 18-46 wt% and the employment of di-isopropylbenzene hydroperoxide as an initiator. Trends in the patent landscape indicate a preference for cold process discontinuous emulsion polymerization and the use of nitrogen replacement and cold water cooling to control the reaction temperature. The resulting polymers exhibit a range of properties, including Mooney viscosity and tensile strength. The patent landscape also highlights the importance of temperature control, with reaction temperatures ranging from 5-30 ℃ and 20-60 ℃ for emulsion and solution polymerization, respectively.

### Methodology

#### Patent 1

Patent Number: Not disclosed

Patent Title: Not disclosed

Assignee: Not disclosed

Publication Year: Not disclosed

Jurisdiction: Not disclosed

Polymerization Process: emulsion polymerization

Acrylonitrile Content: 18-46 wt%

Monomer Ratio: Not disclosed

Water Amount: Not disclosed

Emulsifier: RA rosin acid or/and soap

Initiator: di-isopropylbenzene hydroperoxide, iron edta sodium salt or secondary reduction agent rongalite

Chain Transfer Agent: tert-dodecyl mercaptan, uncle's ten carbon mercaptan, uncle's 14 carbon mercaptan, uncle's 16 carbon mercaptan

Temperature: 5-30 ℃

Reaction Time: 7-12 hours

Conversion: 65-80%

Coagulation: Not disclosed

Polymer Properties: Mooney viscosity: 30-95, tensile strength: 10-22 Mpa

Experimental Notes: cold process discontinuous emulsion polymerization, nitrogen replacement, cold water cooling, temperature-reducing coil

#### Patent 2

Patent Number: US318330

Patent Title: SOLUTION POLYMERIZATION OF ACRYLONITRILE

Assignee: Not disclosed

Publication Year: 1952

Jurisdiction: US

Polymerization Process: solution polymerization

Acrylonitrile Content: at least 70 mole percent

Monomer Ratio: Not disclosed

Water Amount: Not disclosed

Emulsifier: Not disclosed

Initiator: 0.1 to 2.0% by weight based on the weight of the monomers of a free-radical-liberating catalyst

Chain Transfer Agent: Not disclosed

Temperature: between about 20 and 60 C

Reaction Time: 1 to 20 hours

Conversion: Not disclosed

Coagulation: Not disclosed

Polymer Properties: intrinsic viscosity of 1.8 and 2.6

Experimental Notes: carbon dioxide dissolved in the polymerization medium to exclude oxygen

### Cross-Patent Comparison & Synthesis Trends

#### Emulsifier Selection and Loading

The use of emulsifiers in Low Acrylonitrile NBR synthesis is evident, with Patent 1 employing RA rosin acid or/and soap. However, Patent 2 does not disclose the use of an emulsifier.

#### Initiator and Chain Transfer Agent Strategies

The initiators used in the patents include di-isopropylbenzene hydroperoxide and iron edta sodium salt (Patent 1) and a free-radical-liberating catalyst (Patent 2). Chain transfer agents, such as tert-dodecyl mercaptan, are used in Patent 1 to control the molecular weight of the polymer.

#### Monomer Ratio and Reaction Control

The monomer ratio is not disclosed in either patent, but the acrylonitrile content is specified as 18-46 wt% (Patent 1) and at least 70 mole percent (Patent 2).

#### Coagulation and Post-Treatment Conditions

The coagulation conditions are not disclosed in either patent, but Patent 1 mentions the use of a cold process discontinuous emulsion polymerization and nitrogen replacement.

### References

|  Patent Number  |  Patent Title  |  Assignee  |  Jurisdiction  |  Publication Year  |

| --- | --- | --- | --- | --- |

|  Not disclosed  |  Not disclosed  |  Not disclosed  |  Not disclosed  |  Not disclosed  |

|  US318330  |  SOLUTION POLYMERIZATION OF ACRYLONITRILE  |  Not disclosed  |  US  |  1952  |