# Patent Landscape Report for High-Acrylonitrile NBR-Related Disclosures

## 1. Abstract

This report synthesizes three primary patents retrieved under a high-acrylonitrile NBR search profile, with emphasis on how each disclosure relates to nitrile rubber composition control, degradation, or block-copolymer construction. The target material is high-acrylonitrile nitrile butadiene rubber (NBR), generally understood as a butadiene-acrylonitrile copolymer enriched in acrylonitrile to increase polarity, oil resistance, and gas-barrier performance relative to standard NBR. Among the selected patents, only US7875683B2 directly addresses nitrile rubber as the substrate and is therefore the most technically relevant to NBR processing; it discloses metathetic degradation of nitrile rubber using a metal-carbene metathesis catalyst combined with a transition-metal additive to reduce molecular weight before hydrogenation. US7592409B2 is relevant by composition and process analogy: it discloses controlled emulsion polymerization of block polymers containing an A block and a B block where the B block can include acrylonitrile and isoprene, and it provides detailed in-situ emulsification, RAFT/NMP-type control, and seed-latex strategies that are transferable to controlled nitrile-rubber architectures. US9296850B2 is only indirectly relevant, since it focuses on renewable isoprene production and polyisoprene/copolymer claims that merely list acrylonitrile among many possible comonomers; it does not disclose NBR synthesis. Across the landscape, the dominant process themes are controlled emulsion polymerization, in-situ surfactant generation, and metathesis-based molecular-weight reduction. The evidence suggests that high-ACN NBR development is most strongly supported by patents teaching precise monomer/comonomer control, aqueous emulsion processing, and post-polymerization molecular-weight tailoring rather than by direct high-ACN NBR examples.

## 2. Primary Patent Evidence

### Patent 1: US9296850B2 — Polymers of isoprene from renewable resources

| Patent Number | US9296850B2 |
| --- | --- |
| Title | Polymers of isoprene from renewable resources |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2016 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: This patent discloses microbial production of isoprene in engineered host cells, followed by recovery and polymerization of the isoprene into synthetic rubbers and other polymers. It also claims polyisoprene and isoprene copolymers, including copolymers where acrylonitrile is one of many optional comonomers, but it does not teach NBR-specific polymerization conditions.

Isoprene production threshold: more than about 0.002 percent of carbon available in the cell culture medium — Abstract

Polyisoprene delta-13C value: greater than -22% — Abstract

Polyisoprene delta-13C value: -30% to -28.5% — Detailed description

Polyisoprene delta-13C value: -34% to -24% — Detailed description

Liquid polyisoprene weight average molecular weight: 5,000 to 100,000 — Detailed description

Residual double bond content: 1 to 18% — Detailed description

Mooney viscosity: 55 to 120 ML 1+4 at 100°C — Background

Number average molecular weight: about 200,000 to 700,000 g/mol — Background

Lowest workable NBR feedstock Mooney viscosity: about 30 ML 1+4 at 100°C — Background

Hydrogenated nitrile rubber Mooney viscosity: in the order of 55 ML 1+4 at 100°C — Background

Hydrogenated nitrile rubber degree of hydrogenation: 50 to 100% — Background

#### Relevant Experimental Evidence

Example 1: Kudzu isoprene synthase was cloned and expressed in E. coli using pTrcHis2B, pET16b, and pCL1920-based constructs.

Example 4: Kudzu isoprene synthase was expressed in Bacillus subtilis using an aprE promoter-driven replicating plasmid.

Example 6: Yarrowia lipolytica expression vectors were constructed for kudzu and poplar isoprene synthase genes.

Example 11: Streptomyces albus expressing the codon-optimized isoprene synthase produced isoprene above control levels.

Example 12: E. coli strains using fatty acid or palm oil carbon sources produced mevalonate and isoprene.

#### Technical Relevance

This patent is only indirectly relevant because it contains broad copolymer claims that list acrylonitrile as a possible comonomer, but the actual disclosure is centered on renewable isoprene biosynthesis. It does not provide a practical route to high-acrylonitrile NBR synthesis or composition control.

### Patent 2: US7875683B2 — Process for the metathetic degradation of nitrile rubber

| Patent Number | US7875683B2 |
| --- | --- |
| Title | Process for the metathetic degradation of nitrile rubber |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2011 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: This patent discloses reduction of nitrile rubber molecular weight by metathesis using a catalyst based on a transition-group 6 or 8 metal-carbene complex together with a transition-metal additive of formula M(OZ)m. The process is intended to generate lower-molecular-weight nitrile rubber feedstocks that can subsequently be hydrogenated to HNBR with improved processability.

Transition metal additive formula: M(OZ)m — Claim 1

Transition group for M in additive: 4, 5 or 6 — Claim 1

m value: 4, 5 or 6 — Claim 1

Z radical carbon atoms: 1-32 carbon atoms — Claim 1

Z heteroatoms: 1 to 15 heteroatoms — Claim 1

HNBR degree of hydrogenation: 50 to 100% — Background

HNBR Mooney viscosity: 55 to 120 ML 1+4 at 100°C — Background

HNBR number average molecular weight: about 200,000 to 700,000 g/mol — Background

Residual double bond content: 1 to 18% — Background

Lowest workable NBR feedstock Mooney viscosity: about 30 ML 1+4 at 100°C — Background

Hydrogenated nitrile rubber Mooney viscosity from such feedstock: in the order of 55 ML 1+4 at 100°C — Background

Target reduced Mooney viscosity before hydrogenation: less than 30 ML 1+4 at 100°C — Background

Target reduced number average molecular weight before hydrogenation: M_n <70,000 g/mol — Background

Reported catalyst amounts in prior art: 307 ppm Ru and 61 ppm Ru based on nitrile rubber used — Background

Reported catalyst amount in prior art: 0.5 phr Grubbs (I) catalyst — Background

Reported catalyst amount in prior art: 614 ppm ruthenium based on nitrile rubber used — Background

#### Relevant Experimental Evidence

No experimental evidence extracted from available evidence.

#### Technical Relevance

This is the most directly relevant patent in the set because it explicitly uses nitrile rubber (NBR) as the substrate and addresses its molecular-weight reduction. While it does not synthesize high-ACN NBR, it is highly relevant to downstream processing of high-acrylonitrile grades because composition-rich NBR often requires careful molecular-weight management to maintain processability.

### Patent 3: US7592409B2 — Styrene acrylonitrile isoprene triblock copolymer

| Patent Number | US7592409B2 |
| --- | --- |
| Title | Styrene acrylonitrile isoprene triblock copolymer |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2009 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

Synthesis method: This patent discloses controlled emulsion polymerization using in-situ generated emulsifiers, controlled free-radical agents, and seed-latex or microemulsion strategies to make block polymers. The disclosed block architectures include A-B-A triblocks where the B block can contain acrylonitrile and isoprene, making the process conceptually relevant to controlled nitrile-containing elastomer synthesis.

Latent surfactant amount: about 0.2 grams — Example 1

Styrene amount: 5 milliliters — Example 1

Surfactant activator solution volume: 5 milliliters — Example 1

Styrene charge: 1,000 grams — Example 2

Oleic acid charge: 60.0 grams — Example 2

Dibenzyltrithiocarbonate charge: 7.2 grams — Example 2

RO water charge: 4,000 grams — Example 2

Potassium persulfate charge: 40.0 grams — Example 2

Tripotassium phosphate charge: 40.0 grams — Example 2

Potassium hydroxide charge: 16.4 grams — Example 2

Reaction temperature: 65°C — Example 2

Complete conversion time: less than 1.5 hours — Example 2

Final solids: 20.6% — Example 2

Mn: 54,000 — Example 2

PDI: 1.17 — Example 2

Styrene charge: 1,000 grams — Example 3

Hexadecyl half ester of maleic acid charge: 60.0 grams — Example 3

Dibenzyltrithiocarbonate charge: 7.2 grams — Example 3

RO water charge: 4,000 grams — Example 3

Potassium persulfate charge: 40.0 grams — Example 3

Tripotassium phosphate charge: 40.0 grams — Example 3

Potassium hydroxide charge: 16.4 grams — Example 3

Reaction temperature: 65°C — Example 3

Complete conversion time: less than 3 hours — Example 3

Final solids: 23.7% — Example 3

Mn: 48,000 — Example 3

PDI: 1.17 — Example 3

0.6 phr K/Oleate soap solution added — Example 3

RO water charge: 200 grams — Example 8

Styrene charge: 50 grams (0.48 moles) — Example 8

Oleic acid charge: 3.0 grams (0.0106 moles) — Example 8

Phenyl-t-butylnitrone charge: 0.44 grams (0.002485 moles) — Example 8

Potassium persulfate charge: 2.06 grams (0.00762 moles) — Example 8

Tripotassium phosphate charge: 2.13 grams (0.01 moles) — Example 8

Potassium hydroxide charge: 0.9 grams (0.014 moles) — Example 8

Reaction temperature: 65°C — Example 8

Complete conversion time: about 7 hours — Example 8

Mn: 35,000 — Example 8

Mw: 61,000 — Example 8

PDI: 1.74 — Example 8

Styrene charge: 200 grams (1.923 moles) — Example 10

Oleic acid charge: 12.0 grams (0.0424 moles) — Example 10

Phenyl-t-butylnitrone charge: 2.0 grams (0.0113 moles) — Example 10

Distilled water charge: 500 grams — Example 10

Potassium persulfate charge: 8.0 grams (0.296 moles) — Example 10

Tripotassium phosphate charge: 8.0 grams (0.0377 moles) — Example 10

Potassium hydroxide charge: 3.6 grams (0.056 moles) — Example 10

Reaction temperature: 75°C — Example 10

Complete conversion time: about 3.5 hours — Example 10

Mn: 39,000 — Example 10

Mw: 48,000 — Example 10

PDI: 1.22 — Example 10

Reaction temperature: 65°C — Example 11

Complete conversion time: about 7 hours — Example 11

Mn: 41,000 — Example 11

Mw: 70,000 — Example 11

PDI: 1.70 — Example 11

n-Butyl acrylate charge: 22.0 grams (0.171 moles) — Example 12

Potassium persulfate charge: 0.5 grams (0.00184 moles) — Example 12

Reaction temperature: about 65°C — Example 12

Weak exotherm: about 70°C — Example 12

Complete conversion time: about 2 hours — Example 12

Mn: 45,000 — Example 12

Mw: 77,000 — Example 12

PDI: 1.70 — Example 12

Benzaldehyde charge: 0.31 grams (0.00292 moles) — Example 13

N-isopropylhydroxylamine charge: 1.4 grams of a 15% aqueous solution (0.0028 moles) — Example 13

Reaction temperature: 75°C — Example 13

Complete conversion time: about 4 hours — Example 13

Mn: 31,000 — Example 13

Mw: 55,000 — Example 13

PDI: 1.76 — Example 13

Dodecylbenzenesulfonic acid charge: 3.0 grams (0.0092 moles) — Example 14

Sodium nitrite charge: 0.171 grams (0.002485 moles) — Example 14

Reaction temperature: 75°C — Example 14

Complete conversion time: about 3 hours — Example 14

Mn: 97,000 — Example 14

Mw: 147,000 — Example 14

PDI: 1.51 — Example 14

1,1-Diphenylethylene charge: 0.448 grams (0.002485 moles) — Example 15

Reaction temperature: 75°C — Example 15

Complete conversion time: about 2 hours — Example 15

Mn: 51,000 — Example 15

Mw: 92,000 — Example 15

PDI: 1.80 — Example 15

Styrene charge: 2,240 grams — Example 16

Oleic acid charge: 134.4 grams — Example 16

Dibenzyltrithiocarbonate charge: 16.0 grams — Example 16

RO water charge: 3,808 grams — Example 16

Potassium persulfate charge: 13.44 grams — Example 16

Tripotassium phosphate charge: 89.6 grams — Example 16

Potassium hydroxide charge: 36.96 grams — Example 16

Reaction temperature: 65°C — Example 16

Complete conversion time: less than 3 hours — Example 16

Final solids: 38.9% — Example 16

Mn: 45,500 — Example 16

PDI: 1.11 — Example 16

Sodium nitrite charge: 0.69 grams (0.01 moles) — Example 17

Oleic acid charge: 3.0 grams (0.0106 moles) — Example 17

Styrene charge: 50 grams (0.48 moles) — Example 17

Acetic acid charge: 1.0 grams (0.0167 moles) — Example 17

Distilled water charge: 2 grams — Example 17

Potassium persulfate charge: 2.0 grams (0.00739 moles) — Example 17

Tripotassium phosphate charge: 2.0 grams (0.01 moles) — Example 17

Potassium hydroxide charge: 2.35 grams (0.0367 moles) — Example 17

Reaction temperature: 75°C — Example 17

Complete conversion time: about 2.5 hours — Example 17

Final solids: 26.1% — Example 17

Mn: 96,300 — Example 17

Mw: 135,000 — Example 17

PDI: 1.4 — Example 17

Styrene charge: 50 grams (0.48 moles) — Example 18

Oleic acid charge: 3.0 grams (0.0106 moles) — Example 18

Crude 1-chloro-1,1-diphenylethane charge: approximately 0.01 moles — Example 18

Distilled water charge: 200 grams — Example 18

Potassium persulfate charge: 2.0 grams (0.0074 moles) — Example 18

Tripotassium phosphate charge: 2.0 grams (0.0094 moles) — Example 18

Potassium hydroxide charge: 1.55 grams (0.0242 moles) — Example 18

Reaction temperature: 75°C — Example 18

Complete conversion time: about 4 hours — Example 18

Final solids: 22.7% — Example 18

Mn: 40,000 — Example 18

PDI: 1.37 — Example 18

Styrene charge: 1,300 grams (12.5 moles) — Example 19

Oleic acid charge: 78.0 grams (0.2756 moles) — Example 19

Crude 1-chloro-1,1-diphenylethane charge: 39.0 grams — Example 19

Deionized RO water charge: 2,470 grams — Example 19

Potassium persulfate charge: 50.7 grams (0.1875 moles) — Example 19

Tripotassium phosphate charge: 50.7 grams (0.2388 moles) — Example 19

Potassium hydroxide charge: 29.5 grams (0.602 moles) — Example 19

Reaction temperature: 75°C — Example 19

Complete conversion time: about 5.5 hours — Example 19

Final solids: 38.6% — Example 19

Mn: 32,000 — Example 19

PDI: 1.85 — Example 19

1-hexene charge: 25 grams — Example 20

n-Butyl acrylate charge: 25 grams — Example 20

Dipyridyl charge: 0.38 grams — Example 20

Oleic acid charge: 4.0 grams — Example 20

Ethyl 2-bromoisobutyrate charge: 0.47 grams — Example 20

KOH charge: 1.7 grams of 85% KOH in 139 milliliters water — Example 20

Copper sulfate pentahydrate solution: 60.9 grams of a 1% aqueous solution — Example 20

Hydrazine hydrate: 2 drops — Example 20

Reaction temperature: about 67°C — Example 20

Reaction time: 1.5 hours — Example 20

Final solids: 10.9% — Example 20

Isoprene incorporation: 5.5 mole% 1-hexene incorporated into the copolymer — Example 20

#### Relevant Experimental Evidence

Example 1: Demonstrated in-situ emulsification using latent surfactant/surfactant activator pairs in styrene.

Example 3: Showed RAFT-controlled emulsion polymerization with in-situ generated surfactant and a nitrile-rubber block architecture containing acrylonitrile and butadiene.

Example 5: Prepared S-NBR-S triblock copolymer latexes from seed latex.

Example 12: Demonstrated seed-latex reinitiation to form a block copolymer with n-butyl acrylate.

Example 20: Showed ATRP emulsion copolymerization under microemulsion conditions and isolated a liquid copolymer.

#### Technical Relevance

This patent is relevant because it explicitly discloses a block polymer B segment containing acrylonitrile and a conjugated diolefin, and it provides a controlled emulsion framework that can be adapted to nitrile-rubber synthesis. Although the examples are largely styrene-based, the process concepts are useful for controlling composition, architecture, and particle formation in high-acrylonitrile NBR systems.

## 3. Cross-Patent Comparison & Synthesis Trends

US7875683B2 is the only patent that directly uses nitrile rubber as the substrate; it focuses on post-polymerization molecular-weight reduction rather than monomer feed control.

US7592409B2 provides the most relevant synthesis methodology for composition/architecture control, using in-situ emulsification, RAFT/NMP/ATRP-type control, and seed-latex strategies; it explicitly mentions acrylonitrile-containing B blocks.

US9296850B2 is only tangentially related: it centers on renewable isoprene production and polyisoprene claims, with acrylonitrile appearing only as one optional comonomer in a broad claim list.

No patent in the set discloses a direct high-acrylonitrile NBR copolymerization recipe with explicit acrylonitrile wt% feed ratios or final ACN content.

Temperature windows in the relevant process patents cluster around 65-75°C for controlled emulsion polymerization in US7592409B2, while US7875683B2 emphasizes metathesis degradation followed by hydrogenation rather than polymerization temperature.

US7875683B2 reports prior-art catalyst loadings in ppm Ru and phr catalyst terms, highlighting the catalyst-intensity issue in nitrile-rubber degradation; US7592409B2 instead uses persulfate/phosphate/KOH aqueous systems and organic control agents such as dibenzyltrithiocarbonate or PBN.

US7592409B2 repeatedly achieves complete conversion within about 1.5 to 7 hours depending on recipe, whereas US7875683B2 discusses long reaction times as a limitation of prior metathesis degradation processes.

For high-ACN NBR development, the most transferable evidence is controlled aqueous emulsion processing with surfactant generation and block-architecture control from US7592409B2, combined with molecular-weight tailoring concepts from US7875683B2.

## 4. Conclusion

The patent set does not contain a direct high-acrylonitrile NBR synthesis example, but it does provide two useful technical directions: controlled emulsion/block-copolymer methodology and nitrile-rubber molecular-weight reduction. For synthesis of high-ACN NBR, the strongest evidence supports aqueous controlled polymerization with tight monomer-feed control, in-situ emulsification, and low-polydispersity control agents, while US7875683B2 indicates that post-polymerization metathesis can be used to tune molecular weight and processability of nitrile rubber feedstocks. Based on the evidence, the most defensible recommended approach is controlled emulsion copolymerization of butadiene with acrylonitrile using a surfactant-controlled aqueous system at roughly 65-75°C, with careful control of initiator and chain-transfer/control-agent loading, followed if needed by molecular-weight adjustment to maintain processability.

## 5. References

US9296850B2 | Polymers of isoprene from renewable resources | Not disclosed | US | 2016 | https://patents.google.com/patent/US9296850B2/en

US7875683B2 | Process for the metathetic degradation of nitrile rubber | Not disclosed | US | 2011 | https://patents.google.com/patent/US7875683B2/en

US7592409B2 | Styrene acrylonitrile isoprene triblock copolymer | Not disclosed | US | 2009 | https://patents.google.com/patent/US7592409B2/en