# High Acrylonitrile NBR: Patent Landscape on Synthesis, Molecular-Weight Control, and Post-Polymer Processing

## 1. Abstract

This report synthesizes a patent set relevant to high acrylonitrile nitrile butadiene rubber (NBR), with emphasis on how acrylonitrile-rich compositions are made, isolated, modified, and processed. The evidence spans classic emulsion-polymerized NBR, solution-polymerized nitrile rubbers, and downstream handling routes that preserve or improve properties needed for oil-resistant elastomers. The core target is NBR containing a relatively high proportion of acrylonitrile units, typically disclosed in the context of improved oil resistance, heat resistance, processability, or compatibility with subsequent hydrogenation or compounding. Across the patents, the dominant synthesis route remains free-radical polymerization of acrylonitrile with butadiene, most often in emulsion, but solution polymerization is also disclosed as a route to better control molecular weight and architecture.

Several recurring process themes emerge. Older patents emphasize conventional emulsion or mass/mass-suspension polymerization with molecular-weight regulators such as alkylthiols or dodecyl mercaptans, and initiators selected for thermal windows compatible with high conversion and manageable viscosity. Later patents focus on more controlled architectures, including in-situ emulsifier formation, seed-latex strategies, and continuous polymerization to narrow molecular-weight distribution. One patent discloses solution polymerization of nitrile rubbers in organic solvent with special modifiers, explicitly addressing the long-standing industrial challenge of making NBR directly in solution. Another patent describes a continuous mass process for ABS-type polyblends that includes acrylonitrile and butadiene monomers, showing the broader utility of acrylonitrile/butadiene feedstocks in grafted systems. A more recent patent set shifts from synthesis to processing: one patent improves hydrogenated nitrile rubber isolation by a two-step coagulation sequence using halogen-free and divalent metal salts, while another uses seed-latex emulsion polymerization with at least 22 wt-% nitrile monomer for dip-molding latexes. Overall, the landscape indicates that high-ACN NBR is most robustly produced by emulsion polymerization with mercaptan-based molecular-weight control, but newer approaches increasingly prioritize controlled polymerization, cleaner coagulation, and process integration to support downstream hydrogenation and molding.

## 2. Primary Patent Evidence

### Patent 1: US7592409B2 — Styrene acrylonitrile isoprene triblock copolymer

| Patent Number | US7592409B2 |
| --- | --- |
| Title | Styrene acrylonitrile isoprene triblock copolymer |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2009 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

No polymerization parameters disclosed.

#### Relevant Experimental Evidence

Example Extracted Examples COMPARATIVE EXAMPLE 9
It shou:

Example Extracted Examples examples:

Example Extracted Examples example of substi:

Example Extracted Examples Examples of suita:

Example Extracted Examples example better co:

Example Extracted Examples example buffering:

Example Extracted Examples example mineral a:

Example Extracted Examples example succinic:

Example Extracted Examples example ROMP:

Example Extracted Examples example RAFT:

Example Extracted Examples example cleavage:

Example Extracted Examples examples:

Example Extracted Examples example thermopla:

Example Extracted Examples examples that are:

Example Extracted Examples EXAMPLE 1
Surfact:

Example Extracted Examples EXAMPLE 2
Polymer:

Example Extracted Examples EXAMPLE 3
Polymer:

Example Extracted Examples EXAMPLE 4
Prepara:

Example Extracted Examples Example 2
Isopren:

Example Extracted Examples Example 2:

#### Technical Relevance

Selected via deterministic pipeline scoring.

### Patent 2: US11136418B2 — Method for manufacturing hydrogenated nitrile rubber

| Patent Number | US11136418B2 |
| --- | --- |
| Title | Method for manufacturing hydrogenated nitrile rubber |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2021 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

No polymerization parameters disclosed.

#### Relevant Experimental Evidence

Example Extracted Examples Comparative Example 1
For 100:

Example Extracted Examples Comparative Example 2
Next:

Example Extracted Examples Comparative Example 3
For 100:

Example Extracted Examples Comparative Example 4
A solid:

Example Extracted Examples Comparative Example 2 except:

Example Extracted Examples Comparative Example 5
A solid:

Example Extracted Examples Comparative Example 1 except:

Example Extracted Examples Comparative Examples 1:

Example Extracted Examples Comparative Examples 1:

Example Extracted Examples Comparative Examples 2 and 4:

Example Extracted Examples Examples of the n:

Example Extracted Examples Examples thereof:

Example Extracted Examples Examples of the d:

Example Extracted Examples Examples of the o:

Example Extracted Examples Examples of the α:

Example Extracted Examples Examples of the α:

Example Extracted Examples Examples of the α:

Example Extracted Examples Examples of the a:

Example Extracted Examples Examples of the f:

Example Extracted Examples Examples of the c:

#### Technical Relevance

Selected via deterministic pipeline scoring.

### Patent 3: EP2478021B1 — Nitrile rubbers and production of same in organic solvents

| Patent Number | EP2478021B1 |
| --- | --- |
| Title | Nitrile rubbers and production of same in organic solvents |
| Assignee | Not available from source |
| Jurisdiction | EP |
| Publication Year | 2015 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

No polymerization parameters disclosed.

#### Relevant Experimental Evidence

Example Extracted Examples Comparative Examples A and B::

Example Extracted Examples example using hom:

Example Extracted Examples example
DE-A 25 3:

Example Extracted Examples example 2 of the:

Example Extracted Examples Example 5 of U:

Example Extracted Examples Examples of suita:

Example Extracted Examples Example 67:

Example Extracted Examples Example 69:

Example Extracted Examples example those whi:

Example Extracted Examples Examples of solid:

Example Extracted Examples Examples of radic:

Example Extracted Examples Examples of radic:

Example Extracted Examples Examples of radic:

Example Extracted Examples example
Polymer 4:

Example Extracted Examples Examples of
perox:

Example Extracted Examples example only::

Example Extracted Examples Examples of furth:

Example Extracted Examples example α:

Example Extracted Examples example in the fo:

Example Extracted Examples Examples of α:

#### Technical Relevance

Selected via deterministic pipeline scoring.

### Patent 4: US5807941A — Unsaturated nitrile-conjugated diene copolymer process for producing same and …

| Patent Number | US5807941A |
| --- | --- |
| Title | Unsaturated nitrile-conjugated diene copolymer process for producing same and … |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 1998 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

No polymerization parameters disclosed.

#### Relevant Experimental Evidence

Example Extracted Examples comparative examples and refe:

Example Extracted Examples COMPARATIVE EXAMPLE 1
Butadie:

Example Extracted Examples COMPARATIVE EXAMPLE 2
Butadie:

Example Extracted Examples COMPARATIVE EXAMPLE 3
Accordi:

Example Extracted Examples COMPARATIVE EXAMPLE 4
By the:

Example Extracted Examples Comparative Example 4 was pre:

Example Extracted Examples COMPARATIVE EXAMPLE 5
Butadie:

Example Extracted Examples Comparative Example 5:

Example Extracted Examples Comparative Example 5:

Example Extracted Examples COMPARATIVE EXAMPLES 6:

Example Extracted Examples COMPARATIVE EXAMPLE 8
Copolym:

Example Extracted Examples Comparative Example 8:

Example Extracted Examples example a method:

Example Extracted Examples Example 5:

Example Extracted Examples Example 5:

Example Extracted Examples examples of the u:

Example Extracted Examples examples of the c:

Example Extracted Examples examples of the c:

Example Extracted Examples examples of the a:

Example Extracted Examples examples of the c:

#### Technical Relevance

Selected via deterministic pipeline scoring.

### Patent 5: US12359010B2 — Polymer latex for dip-molding applications

| Patent Number | US12359010B2 |
| --- | --- |
| Title | Polymer latex for dip-molding applications |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2025 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

No polymerization parameters disclosed.

#### Relevant Experimental Evidence

Example Extracted Examples comparative examples:

Example Extracted Examples Examples of polym:

Example Extracted Examples examples do not d:

Example Extracted Examples examples for the:

Example Extracted Examples examples disclose:

Example Extracted Examples Examples of such:

Example Extracted Examples Examples are hydr:

Example Extracted Examples Examples of monoc:

Example Extracted Examples examples of dicar:

Example Extracted Examples Examples of other:

Example Extracted Examples Examples are ethy:

Example Extracted Examples Examples of monoc:

Example Extracted Examples examples of dicar:

Example Extracted Examples Examples of other:

Example Extracted Examples Examples of suita:

Example Extracted Examples Examples of such:

Example Extracted Examples Examples are hydr:

Example Extracted Examples Examples are ethy:

Example Extracted Examples Examples of such:

Example Extracted Examples examples of the c:

#### Technical Relevance

Selected via deterministic pipeline scoring.

### Patent 6: US4239863A — Process for the polymerization of acrylonitrile-butadiene-styrene resins

| Patent Number | US4239863A |
| --- | --- |
| Title | Process for the polymerization of acrylonitrile-butadiene-styrene resins |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 1980 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

No polymerization parameters disclosed.

#### Relevant Experimental Evidence

Example Extracted Examples example from a pr:

Example Extracted Examples examples wherein:

Example Extracted Examples EXAMPLE 1
A plura:

Example Extracted Examples EXAMPLE 2
Employi:

Example Extracted Examples Example 1:

#### Technical Relevance

Selected via deterministic pipeline scoring.

### Patent 7: US3903200A — Continuous mass polymerization process for ABS polymeric polyblends

| Patent Number | US3903200A |
| --- | --- |
| Title | Continuous mass polymerization process for ABS polymeric polyblends |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 1975 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

No polymerization parameters disclosed.

#### Relevant Experimental Evidence

Example Extracted Examples examples are set:

Example Extracted Examples EXAMPLE 1 The Sec:

Example Extracted Examples EXAMPLE 2 CONTINU:

Example Extracted Examples Example 1:

Example Extracted Examples EXAMPLE 3 Continu:

Example Extracted Examples Example 2 is esse:

Example Extracted Examples Example 1:

Example Extracted Examples Example 2:

Example Extracted Examples EXAMPLE 4 The pro:

Example Extracted Examples Example 2 were us:

Example Extracted Examples Example 2:

Example Extracted Examples Example 2 giving:

Example Extracted Examples Example 3 has the:

#### Technical Relevance

Selected via deterministic pipeline scoring.

### Patent 8: US11130832B2 — Modified conjugated diene-based polymer and rubber composition including the …

| Patent Number | US11130832B2 |
| --- | --- |
| Title | Modified conjugated diene-based polymer and rubber composition including the … |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2021 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

No polymerization parameters disclosed.

#### Relevant Experimental Evidence

Example Extracted Examples Comparative Example 1 accordi:

Example Extracted Examples Comparative Example 1
To a 20:

Example Extracted Examples Comparative Example 2
To a fi:

Example Extracted Examples Comparative Example 3
To a fi:

Example Extracted Examples Comparative Example 4
A both-:

Example Extracted Examples Comparative Example 5
An one-:

Example Extracted Examples Comparative Example 6
An one-:

Example Extracted Examples Comparative Example 1 except:

Example Extracted Examples Comparative Example 1:

Example Extracted Examples Comparative Example 1 except:

Example Extracted Examples Comparative Example 1:

Example Extracted Examples Comparative Examples:

Example Extracted Examples Comparative Examples and obta:

Example Extracted Examples Comparative Example 1 to Comp:

Example Extracted Examples Comparative Example 4:

Example Extracted Examples Comparative Example 1 in whic:

Example Extracted Examples Comparative Example 5 was pre:

Example Extracted Examples Comparative Example 6 was pre:

Example Extracted Examples Comparative Examples and Refe:

Example Extracted Examples Comparative Examples and Refe:

#### Technical Relevance

Selected via deterministic pipeline scoring.

### Patent 9: US10336853B2 — Polymer, process and composition

| Patent Number | US10336853B2 |
| --- | --- |
| Title | Polymer, process and composition |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2019 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

No polymerization parameters disclosed.

#### Relevant Experimental Evidence

Example Extracted Examples Comparative example 1 in WO20:

Example Extracted Examples Examples of such:

Example Extracted Examples example initiator:

Example Extracted Examples example as descri:

Example Extracted Examples example one prefe:

Example Extracted Examples examples demotiva:

Example Extracted Examples examples in:

Example Extracted Examples Examples 2:

Example Extracted Examples Examples:

Example Extracted Examples examples teach aw:

Example Extracted Examples example:

Example Extracted Examples Example 3:

Example Extracted Examples example from 700:

Example Extracted Examples example at least:

Example Extracted Examples example is substa:

Example Extracted Examples example is substa:

Example Extracted Examples example is substa:

Example Extracted Examples example component:

Example Extracted Examples example methyl:

Example Extracted Examples example less than:

#### Technical Relevance

Selected via deterministic pipeline scoring.

### Patent 10: US10731020B2 — Rubber composition for vulcanization molding, process for manufacturing the …

| Patent Number | US10731020B2 |
| --- | --- |
| Title | Rubber composition for vulcanization molding, process for manufacturing the … |
| Assignee | Not available from source |
| Jurisdiction | US |
| Publication Year | 2020 |
| Priority Date | Not available from source |
| Legal Status | Unknown |
| Polymer Type | Not available from source |
| Relevance Classification | PRIMARY |
| Relevance to Target | Automatically extracted candidate |

#### Polymerization / Synthesis Method

No polymerization parameters disclosed.

#### Relevant Experimental Evidence

Example Extracted Examples Comparative Examples of
Manuf:

Example Extracted Examples comparative examples 1 and 2:

Example Extracted Examples Comparative Examples of
Manuf:

Example Extracted Examples comparative examples of
manuf:

Example Extracted Examples Comparative example 1 of manu:

Example Extracted Examples Comparative Examples
1
2
3
4:

Example Extracted Examples Comparative Example 1
The mix:

Example Extracted Examples Comparative Example 2
The rub:

Example Extracted Examples Comparative Example 1 except:

Example Extracted Examples Comparative Example of
manufa:

Example Extracted Examples Comparative Example 1 except:

Example Extracted Examples Comparative Example 3
A rubbe:

Example Extracted Examples Comparative Example of
manufa:

Example Extracted Examples Comparative Example 1 except:

Example Extracted Examples Comparative Examples 4 to 6
I:

Example Extracted Examples Comparative Examples 4 to 6:

Example Extracted Examples Comparative Example 4:

Example Extracted Examples Comparative Examples 4 to 6 w:

Example Extracted Examples Comparative Example 1 except:

Example Extracted Examples Comparative Example 4:

#### Technical Relevance

Selected via deterministic pipeline scoring.

## 3. Cross-Patent Comparison & Synthesis Trends

US5807941A and EP2478021B1 are the most directly relevant synthesis disclosures for NBR: both center on acrylonitrile/butadiene copolymerization, but US5807941A emphasizes emulsion polymerization with an alkylthiol molecular-weight modifier added in two stages, whereas EP2478021B1 emphasizes solution polymerization in organic solvent with special modifier compounds.

US5807941A discloses 10 to 60 wt-% unsaturated nitrile units, preferably 20 to 50 wt-%; EP2478021B1 does not provide a specific acrylonitrile range in the extracted text, but it explicitly covers at least one conjugated diene and at least one α,β-unsaturated nitrile in solution.

US5807941A uses a free-radical initiator and an alkylthiol compound with 12 to 16 carbon atoms and at least three tertiary carbon atoms; 10 to 95% of the modifier is charged before polymerization and the remainder is added when conversion reaches 20 to 70%. EP2478021B1 uses free-radical polymerization in organic solvent with a modifier, and optionally hydrogenation, but the extracted text does not specify the modifier identity or feed strategy.

US5807941A targets Mooney viscosity of 15 to 150 and a low-molecular-weight fraction of 3 to 20 wt-% with Mn not larger than 35,000; EP2478021B1 focuses on solution-processable nitrile rubbers and on structural elements originating from the regulator compounds, indicating a stronger emphasis on architecture control than on a specific Mooney window in the extracted passages.

US4239863A and US3903200A are not NBR-only patents, but both include acrylonitrile/butadiene-containing systems. US4239863A is a mass or mass-suspension ABS process using tertiary-butyl peroxy esters with 10-hour half-lives between about 50 and 95 °C, initial plug-flow polymerization up to about 10 wt-% solids, then agitation from about 5 to 10% conversion to about 40% conversion, and overall 50 to 90 wt-% monomer conversion. US3903200A is a continuous mass process for ABS-type polyblends using 0.1 to 15 wt-% soluble diene rubber, 10 to 40% conversion in the first stage, then 25 to 80% conversion in the second stage, and devolatilization to a bimodal rubber-particle morphology.

US11136418B2 and US12359010B2 are downstream/process patents rather than primary NBR synthesis disclosures. US11136418B2 starts from nitrile rubber latex made by emulsion polymerization, then uses a first coagulation with a halogen atom-free metal salt, solution hydrogenation, and a second coagulation with a divalent metal salt; it specifies hydrogenated nitrile rubber with iodine value 120 or less and nitrile units of 10 to 60 wt-% in the precursor family. US12359010B2 uses free-radical emulsion polymerization of at least one conjugated diene and at least one ethylenically unsaturated nitrile compound in the presence of seed latex particles, with the nitrile monomer at least 22 wt-% based on total ethylenically unsaturated monomers.

US11130832B2 and US10336853B2 are broader polymer-process patents that inform the landscape but are not direct NBR synthesis disclosures. US11130832B2 emphasizes continuous polymerization, narrow molecular-weight distribution, and terminal functionalization in conjugated diene polymers. US10336853B2 focuses on low-Mn, high-Tg solution polymers based on itaconate monomers, with lower initiator, lower CTA, and lower temperature needs; it is not an NBR patent but illustrates the broader trend toward solution-process control and reduced reliance on styrene-like monomers.

US7592409B2 is a controlled emulsion polymerization patent that explicitly includes acrylonitrile/methacrylonitrile and conjugated diene blocks in block copolymer architectures, but it is not an NBR process patent. Its relevance is methodological: in-situ emulsifier formation and controlled radical polymerization concepts are adjacent to modern efforts to control nitrile-containing elastomer architectures.

US10731020B2 is a rubber compounding and vulcanization-molding patent that lists nitrile rubber and acrylonitrile-butadiene rubber among possible base rubbers, but it does not disclose NBR synthesis conditions. It is relevant only as a downstream processing reference.

Across the primary patents, the recurring historical approach is emulsion polymerization with mercaptan chain transfer and conventional coagulation; newer approaches add controlled polymerization, solution synthesis, seed-latex control, and cleaner coagulation/hydrogenation workflows.

## 4. Conclusion

The patent evidence supports high acrylonitrile NBR as a family most reliably made by free-radical copolymerization of acrylonitrile with butadiene, with emulsion polymerization remaining the industrial baseline and mercaptan-based molecular-weight control the most explicit recurring tactic. For higher-ACN grades, the most defensible synthesis window from the extracted record is an acrylonitrile content in the broad range of about 10 to 60 wt-% of nitrile units, with a preferred practical band around 20 to 50 wt-% where disclosed. For process control, the strongest evidence favors staged addition of chain-transfer agent, careful initiator selection, and conversion management to keep viscosity and molecular-weight distribution within workable limits. Where solution processing is desired, the patents indicate that organic-solvent free-radical polymerization with special modifiers can be used, but the evidence also shows that this route is less established than emulsion polymerization. For downstream performance, the best-supported workflow is emulsion polymerization followed by coagulation, isolation, and, if needed, hydrogenation using a two-step coagulation strategy with halogen-free and divalent metal salts. Overall, the recommended evidence-based synthesis strategy for high acrylonitrile NBR is emulsion polymerization with controlled mercaptan chain transfer, moderate-to-high acrylonitrile feed, and post-polymer isolation conditions designed to preserve molecular weight and enable clean conversion to HNBR when required.

## 5. References

US7592409B2 | Styrene acrylonitrile isoprene triblock copolymer | Not disclosed | US | 2009 | https://patents.google.com/patent/US7592409B2/en

US11136418B2 | Method for manufacturing hydrogenated nitrile rubber | Not disclosed | US | 2021 | https://patents.google.com/patent/US11136418B2/en

EP2478021B1 | Nitrile rubbers and production of same in organic solvents | Not disclosed | EP | 2015 | https://patents.google.com/patent/EP2478021B1/en

US5807941A | Unsaturated nitrile-conjugated diene copolymer process for producing same and … | Not disclosed | US | 1998 | https://patents.google.com/patent/US5807941A/en

US12359010B2 | Polymer latex for dip-molding applications | Not disclosed | US | 2025 | https://patents.google.com/patent/US12359010B2/en

US4239863A | Process for the polymerization of acrylonitrile-butadiene-styrene resins | Not disclosed | US | 1980 | https://patents.google.com/patent/US4239863A/en

US3903200A | Continuous mass polymerization process for ABS polymeric polyblends | Not disclosed | US | 1975 | https://patents.google.com/patent/US3903200A/en

US11130832B2 | Modified conjugated diene-based polymer and rubber composition including the … | Not disclosed | US | 2021 | https://patents.google.com/patent/US11130832B2/en

US10336853B2 | Polymer, process and composition | Not disclosed | US | 2019 | https://patents.google.com/patent/US10336853B2/en

US10731020B2 | Rubber composition for vulcanization molding, process for manufacturing the … | Not disclosed | US | 2020 | https://patents.google.com/patent/US10731020B2/en